## Slide 1
ELECTROMAGNETIC DESIGN
CONDUCTION COOLED SSR MAGNET ASSEMBLY FOR PIP-II
(FDR – Phase I)
Electromagnetic Applications & Instrumentation Division,
Bhabha Atomic Research Centre
Department of Atomic Energy (DAE), India
Team members:
Kumud Singh
Janvin Itteera
Mahima
Vikas Tiwari
Himanshu Bisht
R R Singh
R K Jalan
Sanjay Howal

## Slide 2
Vacuum pumps
Cryostat housing magnet
Electronics rack
Power diode connected in shunt with magnet
Outline
Introduction
  BARC contribution for LINAC magnets in PIP-II technology map
Electromagnetic Design of Conduction cooled magnet
  Functional requirement specification
  EM design for main solenoid
  Corrector coil design
  Fringe field on the cavity surface
  Bucking coil optimization & tolerance studies on BC dimensions
  Tolerance studies on bucking coil
  Superconducting wire selection
  Magnet load line & design operating margin
Quench Studies
  Quench initiated in main coil (variation in heat pulse, coil configuration & quench location)
  Quench initiated in Bucking coil
  Quench protection circuit

## Slide 3: Magnet Contribution- PIP-II LINAC Technology map
b=0.11
b=0.22
b=0.51
b=0.61
b=0.9
325 MHz
11-177 MeV
650 MHz
177-800 MeV
SC
162.5 MHz
0.03-11 MeV
LEBT
RFQ
MEBT
RT
IS
Section | Freq | Energy (MeV) | Cav/mag/CM | Type
RFQ | 162.5 | 0.03-2.1 |  | 
HWR (opt=0.11) | 162.5 | 2.1-11 | 8/8/1 | HWR, solenoid
SSR1 (opt=0.22) | 325 | 11-38 | 16/8/ 2 | SSR, Solenoid
SSR2 (opt=0.51) | 325 | 38-177 | 35/21/7 | SSR, Solenoid
LB 650 (G=0.61) | 650 | 177-480 | 33/22/11 | 5-cell elliptical, doublet*
HB 650 (G=0.9) | 650 | 480-800 | 24/8/4 | 5-cell elliptical, doublet*
*Warm doublets external to cryomodules |  |  |  | 
MEBT and HEBT Magnet assemblies
Quadrupoles magnets: 34 No.
Dipole Magnets : 15 No.
2. SSR Superconducting Magnet assemblies
SSR1 magnet assemblies: 10 (8+2) No.
SSR2 Magnet Assemblies: 23No.
(21+2)
3. LB650 and HB 650 warm doublet
Quadrupole magnets: 47 No.
Dipole corrector : 45 No.
DELIVERED
Construction phase : 9 triplets

## Slide 4: Pre-series magnet development
P2-SSR-BARC-A-PS-008
P2-SSR-BARC-A-PS-007
P2-SSR-BARC-A-PS-003
Pre-series Magnet development was carried out with 0.4mm bare diameter SC wire

## Slide 5: Pre-series magnet testing
Axial field mapping
Fringe field @35A - 4.1G
Fringe field @45A - 5.2G Integral strength

## Slide 6
Functional Requirement Specifications (FRS)
Parameters | SSR1/SSR2 New specification (Ver 2.) | SSR1/SSR2 New specification (Ver.3)
Focusing Strength | 4.5 T2m | 4.5T2m
Bending strength of Dipole correctors | 5 mT-m | 6.0 (5.0) mT-m
Beam pipe aperture | 40 mm | 40 mm
Uncertainty in the location of magnetic axis w.r.t Reference points (Transverse and angular alignment) | <0.1mm RMS <0.5 mrad RMS | <0.1mm RMS <0.5 mrad RMS
Effective length of solenoid (FWHM) | <18cm | <18.5cm
Active magnetic shielding requirements | ~ <10G | ~<10G
Maximum current in the solenoid | 100A | 90 A
Maximum current in the dipole correctors | 50 A | 12 A
Parameters | SSR1/SSR2 New specification (Ver 2.) | SSR1/SSR2 New specification (Ver.3)
Focusing Strength | 4.5 T2m | 4.5T2m
Bending strength of Dipole correctors | 5 mT-m | 
Beam pipe aperture | 40 mm | 40 mm
Uncertainty in the location of magnetic axis w.r.t Reference points (Transverse and angular alignment) | <0.1mm RMS <0.5 mrad RMS | <0.1mm RMS <0.5 mrad RMS
Effective length of solenoid (FWHM) | <18cm | <18.5cm
Active magnetic shielding requirements | ~ <10G | ~<10G
Maximum current in the solenoid | 100A | 90 A
Maximum current in the dipole correctors | 50 A | 12 A
Primary Design objectives:
High Field (focusing strength)
Low stray field as fringe field level on the adjacent spoke cavity surface is a major concern.
Dipole field and skew quadrupole field coils incorporated in the same magnet package.

## Slide 7
Arrangement of magnet assemblies in cryomodule
Magnet cavity string arrangement in SSR1 Cryomodule
Magnet cavity string arrangement in SSR2 Cryomodule

## Slide 8
Electromagnetic Design
Active shielding coils
Main Coil
Corrector Coils
Y Corrector Coils
X Corrector Coils

## Slide 9
Magnetic Field Due to a Solenoid
Peak magnetic Field is given by:-
Where
)= ,
The magnetic field (Bw) responsible for determining critical current density is close to the winding is proportional to B0 .
Bw= c0 B0 , where c0 is a function of shape factor and .
The magnetic field on axis of the solenoid is given by:-
+ }
where
= and =

## Slide 10
Focussing strength and spherical aberration
Spherical coil aberration 71.15982352
Focusing strength 4.42

## Slide 11
Electromagnetic Design
Configuration 1:
No extra benefit in spatial occupancy
Configuration 2:
Less axial field uniformity
More longitudinal foot print
Configuration 3:
Good axial field uniformity
Optimized axial and longitudinal footprint

## Slide 12
Electromagnetic Design
Sr. no | Parameter | Value | Unit
1. | Length of solenoid coils in the lens | 140 | mm
2. | Main coil inner radius | 38 | mm
3. | Main coil outer radius | 75 | mm
4. | Strand diameter bare (with insulation) | 0.51(0.55) | mm
5. | Winding fill factor | 0.85 | 
6. | Number of turns in the main coil | ~14554 | 
Sr. no | Parameter | Value | Unit
1. | Length of Bucking Coils | 64 | mm
2. | Bucking coil inner radius | 100 | mm
3. | Bucking Coil outer radius | 112.5 | mm
4. | Strand diameter | 0.51(0.55) | mm
5. | Bucking Coil Z location* | 38 | mm
6. | Winding fill factor | 0.85 | 
7. | Number of turns in the Bucking coil | ~2247 | 
Objective function :
4.5 T2m
Minimize at z= 0.42m cavity location
Optimization Parameters:
Nmain, OR main, IR main , IR BC , OR BC L BC , Z center-BC
Constraints:
≤ 185 cm +/- 30mm ; I exc < 90A
Operating current 78A

## Slide 13
Electromagnetic Design… continued
Bmod field vs axial distance plot
Main Coil Powered on
Main Coil Powered along with active shielding coil

## Slide 14
Electromagnetic design … continued
Zonal plot of Magnetic field at the magnet center (field homogeneity 1.1% @ r=18 mm)
B field plot and B2 Plot along the axial length
(Focusing strength of 4.57 T2m)
Focusing strength req. : 4.5 T2m
Achieved : 4.57T2m
Operating current 78A

## Slide 15
Dipole corrector design
Sr. no | Parameter | Value | Unit
1. | Straight Length of Dipole corrector coils (H1) | 10 | mm
2. | Width cross-Section in radial direction | 15 | mm
3. | Thickness cross-section in azimuthal direction | 35 | mm
4. | Radius of the Mandrel (R1) | 80 | mm
8. | Strand diameter (bare/insulated) | 0.51/0.55 | mm
9. | Number of turns in the dipole corrector coil | ~1475 | 
10. | Operating current density at nominal bending strength | 28 | A/mm2
11. | Winding fill factor | ~0.85 | 
Sr. no | Parameter | Value | Unit
1. | Designed value of Bending strength of corrector coils | 6.3 | mT-m
2. | Peak Magnetic field on the corrector coil wire strand | 2.8 | T
3. | Quadrupole Gradient in skew Quadrupole mode | 3.25 | T/m
5. | Nominal current | ~10 | A
6. | Transfer function of the corrector coils | 0.1525 | mT/A
Corrector coils used in space between the main solenoid and active shielding coil to reduce the operating current requirement

## Slide 16
Dipole corrector design … continued
Zonal field plot of dipole field at the magnet center
Magnetic Field plot for the dipole field (Dipole field Integral 6.3 mT-m)
Bending strength req. : 6 mT-m
Achieved : 6.3 mT-m
Operating current ~10A

## Slide 17
Dipole Corrector design (Quadrupole mode)
Magnetic Field (Bx or By) plot in the lens aperture at various radial locations when corrector coils are connected as skew quadrupole
Bx field plot vs radial distance in magnet aperture (Gradient = 3.25T/m)

## Slide 18
Fringe field on cavity surface
Φtr= * *
μ0=4π∙10-7H/m ; Φ0=2∙10-15Wb
ξ0=3.9∙10-8 m is the coherent length in Nb, f is the frequency of the cavity,
Rs is the surface resistance of Nb at this frequency,
V is the volume of the cavity,
Λ =
Completely defined by the properties of superconducting material
Cavity Specific
Acceptable degree of degradation η with allowed amount of the trapped flux.
Surface integral / line integral at the maximum magnetic energy density location needs to be minimized during the design of bucking coil
Placement of a focusing lens inside the SSR cryomodule

## Slide 19
Bucking coil optimization
B field vs axial distance plot for different cases of Bucking coil dimensions

## Slide 20
Tolerance studies on bucking coil geometrical parameters
Sr. no | BC-Coil IR | BC-Coil OR | BC-Coil L | BC-Coil Z center | B max On cavity surface | Field Surface Integral at Axial distance of 0.42 m)
 | mm | mm | mm | mm | Gauss | G-m2
1. | 100 | 112.5 | 64 | 38 | 7.33 | 2.47
2. | 101 | 113 | 64 | 38 | 11 | 1.908
3. | 101 | 114 | 64 | 38 | 20 | 6.79
4. | 99 | 112 | 64 | 38 | 12 | 6.018
5. | 100.5 | 113 | 64 | 38 | 8.89 | 2.988
6. | 102 | 115 | 64 | 38 | 25 | 8.42
Effect on fringe field level at different axial position of the Bucking coil w.r.t Main coil
Tight tolerance is required for the bucking coil winding dimensions and its placement w.r.t main coil.
The positional inaccuracy of the Bucking coil effects the fringe magnetic field on the cavity surface.
Two probable cases for detailed analysis

## Slide 21
Error Sensitivity studies – Case (a)
B field vs axial distance plot for +/- one layer of bucking coil
Minimization point

## Slide 22
Error Sensitivity studies …continued Case (a)
B field vs axial distance plot for +/- one layer of bucking coil
Fringe field levels are well within the specified limits with manufacturing tolerances

## Slide 23
Error Sensitivity studies – Case (b)
B field vs axial distance plot for +/- one layer of bucking coil

## Slide 24
Error Sensitivity studies … continued – Case (b)
B field vs axial distance plot for +/- one layer of bucking coil
Fringe field levels are well within the specified limits with manufacturing tolerances
Case b fringe field levels < Case a fringe field levels

## Slide 25
Validation with alternate solvers
B field vs axial distance plot for +/- one layer of bucking coil
Courtesy : Martin M Miao, FNAL

## Slide 26
Validation with alternate solvers
CST Low frequency Magnetostatic Solver

## Slide 27
Radial field plot at cavity location for case (a)
B field vs axial distance plot for +/- one layer of bucking coil

## Slide 28
Radial field plot at cavity location for case (b)
B field vs axial distance plot for +/- one layer of bucking coil
Case (a) selected for optimized design

## Slide 29
Surface plot at Cavity location
Case (a) selected for optimized design
Case (a) : BC Baseline 100-112.5
Case (b) : BC Baseline 100.5-113

## Slide 30
Combined-field-All coils-powered-on

## Slide 31
Vacuum pumps
Electronics rack
Power diode connected in shunt with magnet
Superconducting Wire strand material properties
All conduction cooled magnets are proposed to be wound using round 0.5 bare diameter /0.54 mm insulated strand (NbTi/ copper matrix 1:2 Sc:Cu Ratio).
The ratio of the maximum current density in the superconductor at any magnetic field and temperature to that at B = 5 T and T = 4.2 K can be found using the expression given below:
Jc(B,T) / Jc(5 T, 4.2 K)= C0/B∙bα∙(1-b)β∙(1-tn)γ
Where, C0 = 28.4 T, α = 0.80, β = 0.89, and γ = 1.87.
Bare Wire Dia | Filament Diameter | Cu/Sc Ratio | Filament twist pitch | RRR | Ic @ 3 T , 4.2K | Ic @ 5 T , 4.2K | Ic @ 7 T , 4.2K | Ic @ 9 T , 4.2K
0.51mm |  | 2:1 |  | 70 | 240 A | 140A | 105A | 32A

## Slide 32
Vacuum pumps
Electronics rack
Power diode connected in shunt with magnet
Superconducting Wire strand material properties

## Slide 33
Vacuum pumps
Electronics rack
Power diode connected in shunt with magnet
Magnet load line – New design
Comparing the manufacturer’s data it is clear that practically there is a margin of ~ 35A @ 4.2K

## Slide 34
Vacuum pumps
Electronics rack
Power diode connected in shunt with magnet
Magnet load line – Pre-series Magnet design (0.4mm bare dia wire)
Practically no Margin @ 4.2K
~ 30A @ 2.15K

## Slide 35
Quench Studies

## Slide 36
Vacuum pumps
Electronics rack
Power diode connected in shunt with magnet
Quench Studies (Quench initiated in main coil)
At t = 0s
At t = 0.01s
At t = 0.1s
At t = 0.4s
At t = 5s
At t = 20s
Flux initiated by ~4W of heat deposition at peak B field location
To study peak temperature & peak coil voltages

## Slide 37
Power diode connected in shunt with magnet
Quench Design (Variation in heat pulse)
4W for 0.1 second
4W for 0.05 second
Quench Characteristic for two coils sub-sections of main coil

## Slide 38
Power diode connected in shunt with magnet
Quench Design (Variation in heat pulse)
40W for 0.1 second
The amount of input heat energy does not play very significant role in determining the coil temperature
Once the quench has been initiated, by small amount of heat dissipation, the normal zone of the magnet will grow and decay the current
However the initial peak temperature of the hot spot (location at which quench is initiated) does depend slightly on the heat pulse.

## Slide 39
Quench protection circuit
+ PS -
Quench Protection by passive diodes
Differential Voltage sensed to detect Quench
Same Quench protection circuit for Dipole corrector coils
BC coil1
MC coil1
MC coil2
BC coil1

## Slide 40
Quench detection
Voltage taps to monitor and record any event of quench
Based on the theoretical studies and pre-series magnet quench measurement the quench detection circuit is considered to be efficinet to detect and protect the magnet in event of quench.

## Slide 41
Final Magnet parameters
Coil1 Coil2 Coil3 Coil4
Coil1 5.82H 4.823H -0.319H -0.3191H
Coil2 4.823H 9.297H -0.722H -0.722H
Coil3 -0.319H -0.722H 1.461H 0.521H
Coil4 -0.319H -0.722H 0.521H 1.461H
Engineering current density ~ 382 A/mm 2 | Excitation current 75A | Focusing strength 4.57 T2m | Solenoid
Engineering current density ~ 50.995 A/mm 2 | Excitation current 10A | Focusing strength 6.3 mT-m | Dipole Corrector
Peak coil to ground voltage = 1.1kV
Peak temperature in case of quench = 65K
Magnet physical length = 140 mm

## Slide 42
Conclusion
Parameters | SSR1/SSR2 New specification (Ver.3) | Achieved | Remarks
Focusing Strength | 4.5T2m | 4.57T2m | √
Bending strength of Dipole correctors | 6.0 (5.0) mT-m | 6.3 mT-m | √
Beam pipe aperture | 40 mm | 40 mm | 
Uncertainty in the location of magnetic axis w.r.t Reference points (Transverse and angular alignment) | <0.1mm RMS <0.5 mrad RMS | Majorly from the Mechanical design of magnet former and winding accuracy | 
Active magnetic shielding requirements | ~<10G | <10 G | √
Maximum current in the solenoid | 90 | 75 A | √
Maximum current in the dipole correctors | 12 (50) | 10 A | √
Parameters | SSR1/SSR2 New specification (Ver.3) | Achieved | Remarks
Focusing Strength | 4.5T2m | 4.57T2m | √
Bending strength of Dipole correctors |  | 6.3 mT-m | √
Beam pipe aperture | 40 mm | 40 mm | 
Uncertainty in the location of magnetic axis w.r.t Reference points (Transverse and angular alignment) | <0.1mm RMS <0.5 mrad RMS | Majorly from the Mechanical design of magnet former and winding accuracy | 
Active magnetic shielding requirements | ~<10G | <10 G | √
Maximum current in the solenoid | 90 | 75 A | √
Maximum current in the dipole correctors | 12 (50) | 10 A | √
Electromagnetic design of the SSR solenoid has been carried out meet the specified requirements
Predicted performance metrics and margins have been considered
In terms of (a) Operational margin (b) Manufacturing tolerance impact on performance (c) Fringe field on the cavity surface

## Slide 43
Conclusion
New design considerably has higher margin compared to pre-series magnets
Dipole corrector current requirements have been reduced for reducing thermal load
Based on the magnetic measurements and design performance of pre-series magnets predicted electromagnetic design will meet the design requirements
Manufacturing tolerances has been accounted for during design and positioning accuracies of main coil and bucking coil shall be maintained to meet fringe field requirements under all conditions.

## Slide 44
References
[1] PIP-II SSR2 CRYOMODULE FRS : ED0001829-D
[2] FOCUSING LENS FOR SSR1 AND SSR2 - Technical Requirements Specification (TRS)"
[3] BCR: SSR Solenoid design/validation test, PIP-II BCR
[4] “SSR1 Cavity Quenching in the Presence of Magnetic Field,” FNAL TD note TD-12-007, June 2012 , T. Khabiboulline, D. Sergatskov, and I. Terechkine,
[5] “Acceptable Level of Magnetic Field on the Surface of a Superconducting RF Cavity,” FNAL, TD note TD-12-008, June 2012T. Khabiboulline, T. Nicol, and I. Terechkine
[7] Electromagnetic design and performance of conduction cooled superconducting magnet for spoke resonator cryomodule for Proton Improvement Plan (PIP)-II, Kumud Singh, Janvin Itteera, Mahima , Vikas Tiwari , Himanshu Bisht , Sanjay Malhotra ,R.R. Singh , Rajesh Jalan , Sanjay Howal , Rajesh Chimurkar , Sunil Kumar , S. Stoynev ,M. Turenne , M. Yub, B. Hanna , J. Hayman , C. Boffo, July 2024 Elsevier, Superconductivity

## Slide 45: Thank you for your kind attention

## Slide 46: Back up slides

## Slide 47
Summary of quench studies
Sr. no. | Series dump resistor value | Peak voltage in coil 1 Peak Voltage in coil 2 | Voltage across Coil1 Voltage across Coil2 | Coil 1 temperature Coil 2 temperature
1. | 0 Ohms | 600V 1100 V | 4V 4V | 60K 60K
2. | 0.005 Ohms | 60V 200V | ~ 4.5V ~ 4.5V | 45K 38K
3. | 5 Ohms | 100 V 120 V | ~ 400 V ~128 V | 38 K 27 K
Sr. no. | Configuration | Peak voltage in coil 1 Peak Voltage in coil 2 | Voltage across Coil1 Voltage across Coil2 | Coil 1 temperature Coil 2 temperature
1. | Radial Coil split (middle quench) No dump resistor 0.4J of energy deposition | 600V 1100 V | ~4V ~4V | 65K 60K
2. | Axial Coil split (middle quench) No dump resistor 0.4J of energy deposition | ~ 850V ~850V | ~4V ~4V | 75K 75K
3. | Axial Coil split (corner quench) No dump resistor 0.4J of energy deposition | ~ 850V ~850V | ~4V ~4V | 75K 75K
With dump resistor in series with back to back diodes
With only back to back diodes in parallel with coil