## Slide 1: 302.4.01 Magnets Vertical Test at BNL Weekly Status
Febin Kurian
06-Jan-2025

## Slide 2: MQXFA 12B Thermal Cycle-2
Magnet cooldown started today (1/6/25) morning, currently at about 219K
Has not started making liquid yet
Assuming smooth cool down, we expect to be cold by end of the week

## Slide 3: MQXFA12b-Quench Summary-So Far
Chart: MQXFA 12b Vertical Test All tests at 1.9 K, 20A/s unless specified otherwise
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26 | 27 | 28 | 29 | 30 | 31 | 32 | 33 | 34 | 35
Trip | 14.732
Quench(Q1) | 16.419 | 16.273
Quench(Q2) | 15.88
Quench(Q3) | 15.283 | 15.783 | 15.964 | 16.097 | 16.334 | 16.341 | 16.157 | 16.332 | 16.419
Quench(Q4)
Inominal(kA) | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23
I_Acceptance (kA) | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53
No Quench | 16.53 | 16.53 | 16.23 | 16.53 | 16.23 | 16.23 | 16.23 | 16.23

## Slide 4: MQXFA12b-Quench Locations
Chart: MQXF12b Longitudinal quench location from Quench Antenna
| 1311 | -1989
Q1 (224) | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18
Q2(159) | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18
Q3 (225) | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18
Q4(148) | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18
Quench No. | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16

## Slide 5: Second Top Hat Repair
  V-taps:
    All passed Hipot
    VT5 replaced with VT7
  Heaters:
    There was inconsistent behavior on heater box2, upon hipot on individual wires, two wires found to be the reason
    Currently those wires are being replaced with unused wires in the bundle

## Slide 6: CRYOGENIC STATUS
CTI 4000 system and Linde 1610 system
  Currently being started up