## Slide 1: MQXFA20 Structure and Status
Dan Cheng, for the AUP team
23-Jan-2025
LBNL

## Slide 2: MQXFA20 Structure Assembly
Coil Pack Assembly Plans
Tapered Loading Shim
Improving the “LQ Effect”
Status and Summary

## Slide 3: MQXFA20 Proposed Coil Arrangement
142
146
121
125
~0.001” Undersized R
Neglected
~0.0035” Undersized per Midpl.
Add 0.003” shim per side
~0.001” Undersized R
Neglected
~0.0015” Undersized per Midpl.
Add 0.002” shim per side
~.001” Undersized R
Neglected
~0.002” Undersized per midpl.
Add 0.002” shim per side
~0.001” Undersized R
neglected
~.003” Undersized per Midpl.
Add 0.003” shim per side
8 x dmidplane = 2 p x dROR
Coil Electrical Order: A :121 – 142 – 146 – 125: B
Conforms to a favorable order based on RRR data
Q1
Q2
Q3
Q4

## Slide 4: MQXFA20 Coil Pack Build 1 (Fuji)
 | 121 | 146 | 125 | 142
Kapton Ground plane insulation | 0.0045” (0.114 mm) |  |  | 
Coil Specific Radial Shim | 0 | 0 | 0 | 0
Coil-specific midplane shim | 0.002” 0.050 mm | 0.003” 0.075 mm | 0.003” 0.075 mm | 0.002” 0.050 mm
Fuji paper | 0.007” (0.175 mm) |  |  | 
Radial Shim | 0.005” Polyimide + 0.003” Kapton (~0.200 mm) |  |  | 
Nominal Collar R: 114 mm
Nominal Coil R: 113.376 mm
Nominal Radial shim = 0.025” (0.624 mm)
  But we still target ~0.020”
Fuji radial stack up is ~0.021” (~0.54 mm)
  0.0045” Coil GPI + 0.007” Fuji + 0.005” Kapton & 0.003” Kapton
Add Kapton to various midplanes

## Slide 5: MQXFA20 Coil Pack Build (Final)
 | 121 | 146 | 125 | 142
Kapton Ground plane insulation | 0.0045” (0.114 mm) |  |  | 
Coil Specific Radial Shim | 0 | 0 | 0 | 0
Coil-specific midplane shim | 0.002” 0.050 mm | 0.003” 0.075 mm | 0.003” 0.075 mm | 0.002” 0.050 mm
Fuji paper | 0.000” (0.0 mm) |  |  | 
Radial Shim | 0.005” Polyimide + 0.005” Polyimide + 0.003” Kapton (~0.33 mm) |  |  | 
Nominal Collar R: 114 mm
Nominal Coil R: 113.376 mm
Nominal Radial shim = 0.025” (0.624 mm)
  But we still target ~0.020”
Actual radial stack up is ~0.020” (~0.51 mm)
  0.0045” Coil GPI + 0.005” Kapton + 0.005” Kapton & 0.003” Kapton
Add Kapton to various midplanes

## Slide 6: Tapered Loading Shims
Shell 1 is now instrumented
  As with recent magnets, shell 1 will be monitored during cold testing
  Shell 2 no longer has instrumentation
LE strain gauges will be installed on Coils
  Coil 121 cannot have LE SG due to presence of Pre-Series voltage tap traces
    It will be an Upper coil with extra FBG instrumentation though

## Slide 7: Improving the “LQ Effect”
MQXFA20 will replace the 0.005” (125 µm) G11 radial shim layer with 0.003” (75 µm) Kapton
  Similar to CERN’s implementation of 0.003” (75 µm) radial shim layer on collar in MQXFB08
  Net effect may also increase preload shim packages from ~41-43 mils to ~43-45 mils
Will observe Fuji impression to verify

## Slide 8: Coil-pack sub-assembly Coil OR and radial shims
Nominal radial gap coil to collars
  0.624 mm (GPI + radial shims)
Final layers of radial shims depend on
  Coil size: larger/smaller coils after mid-plane shimming can be compensated by less/more radial shims
  Missing shims for “LQ effect”
    0.175 remove from radial shims (MQXFA20 removing 50 µm more)
So, from 0.624 mm to 0.450 mm

## Slide 9: MQXFA20 Structure Status
MQXFA20
  Shell-yoke assembly complete
  Dressing coils now
  Fuji pack build prep this week
  Expected completion in March
MQXFA19
  Preload operations took place this week
  Expect to ship out ~3rd week of Feb
MQXFA21
  Processing pad-collar assemblies
  Shells, Rods being instrumented
MQXFA19
MQXFA20
Coil 146

## Slide 10: Supplemental MQXFA20 Coil Pack Build Plans
Two primary concerns were raised
  Coil 146 midplane delamination
    Is the midplane contact condition properly sized, even without the inclusion of the 6 axial data points in the calculations?
  Use of 0.003” Kapton radial layer instead of 0.005” G11
    Not tested or reviewed yet for MQXFA magnets
    Earliest this can be reviewed will be for MQXFA21
    Use normal 0.005” G11 radial build up for MQXFA20

## Slide 11: Supplemental MQXFA20 Coil Pack Build Plans
To address the Coil 146 Midplane issue
  Remove the 003 midplane shims from Coil 146 (both sides)
  Remove the 002 midplane shim from the Coil 121 side facing 146
  Remove the 003 midplane shim from the Coil 125 side facing 146
  Place Fuji paper sections in place of 146 midplane shims
Build Fuji pack #1 on the A20 Pad-collar set with 003 Kapton radial layers
Build Fuji pack #2 on the A21 Pad-collar set with 005 G11 (normal) radial layers
  For both builds: Verify Fuji exposures on both midplanes and radial contact
  Midplane condition will not change between builds
Complete MQXFA20 Final coil pack using the A21 set of pads-collars using (normal) 0.005” G11 radial shims

## Slide 12: MQXFA20 Fuji Build Specific Shim Plan
142
146
121
125
~0.001” Undersized R
Neglected
~0.0035” Undersized per Midpl.
Add 0.003” shim on 142 side
~0.001” Undersized R
Neglected
~0.0015” Undersized per Midpl.
Add 0.002” shim on 142 side
~.001” Undersized R
Neglected
~0.002” Undersized per midpl.
Add 0.002” shim per side
~0.001” Undersized R
neglected
~.003” Undersized per Midpl.
Add ~0.007” Fuji per side
8 x dmidplane = 2 p x dROR
Coil Electrical Order: A :121 – 142 – 146 – 125: B
Conforms to a favorable order based on RRR data
Q1
Q2
Q3
Q4

## Slide 13: Summary
MQXFA20 is ready to be assembled
Tapered loading shims (TLS) will be used
Will test the effect of removing 50 µm radial shim for the “LQ Effect” in the Fuji build
Will also verify Coil 146 midplane shimming with the use of Fuji paper in the midplane interfaces
MQXFA20 is expected to ship in ~April 2025

## Slide 14: Additional Slides