## Slide 1: SUNSTAR: Sub-mm UNdulator test at the Advanced Superconducting Test AcceleratoR
A. Garraud1, B. A. Peterson2, J. C. Thangaraj3,
M. G. Allen2, D. P. Arnold1
1Dept. Electrical & Computer Engineering, University of Florida
2School of Electrical and Computer Engineering, Georgia Institute of Technology
3Accelerator Physics Center, Fermilab
July, 24th 2013
ASTA Users’ Meeting, Fermilab, IL

## Slide 2: DARPA AXiS Project
Develop X-ray source technology
that will enable high contrast
when imaging soft biological tissues
(low-Z materials: C-H-O-N)
↓
Realize a compact X-ray source that is
mono-energetic, directional and tunable

## Slide 3: Outline
Magnetic mini undulator
ASTA beam advantages
Considered experimentations
Expected outcome
Demonstrate the generation of monochromatic photons with a mini undulator

## Slide 4: Overview of Magnetic Undulators
State-of-the-art undulator
  Period ~ 5-50 mm
  Peak field: B0 ~ 0.1-1 T
  Large total system size
  Manual assembly
Micromachined undulator
  Period ~ 5-500 µm
  Peak field: B0 > 0.2 T
  Hard X-rays at lower beam energies
  Microfabrication advantages
up to 1000x
reduction

## Slide 5: Laser-Cut Magnets Process Overview
Bulk SmCo ~300 µm thick
Laser-cut into comb structures
Magnetize out-of-plane
Assemble and polish
Laser-machined SmCo comb array
(400-µm period)
Assembled magnetic array

## Slide 6: Assembled Prototype Undulator
200 – 400 µm airgap (Cu spacer shims)
400-µm period
20 mm × 2 mm active area
Easily disassembled / assembled
Tailored undulator holder
Longer undulators on the way
Laser-machined SmCo undulator array
Assembly
views
26 mm
20 mm, 50 periods
2 mm

## Slide 7: High-Resolution Magnetic Field Mapping
High-resolution Hall effect sensor (1 µm x 1 µm area)
3-axis stage with 100 nm step size (x, y axes)
Currently implementing automatic scan height control
Sample platform
x- y- and z-stages
Sensor module
1 µm x 1 µm
sensing area

## Slide 8: Scanning Hall Probe Results
Example of single 400-µm-period magnetic array scans
z (mm)
By (T)
y (mm)
By (T)
z (mm)
at ~100 µm scan height

## Slide 9: Scanning Hall Probe Results
Resulting field of a mini undulator (200 µm airgap)
On-axis B-field of a 400-µm period mini-undulator:
B0 = 0.22 ± 0.02 T
Bx
By
B (T)
z (m)

## Slide 10: Why ASTA Beam is the best place to test the mini undulator?
  Low emittance
    High quality of the beam
  Flat beam generation
    Compatible with the small airgap of the mini undulator
    Expertise in flat beam generation with demonstrated experiments
  High repetition rate
    Will help in photon detection
Large range of beam energy and charge
    Provides flexibility for experiments

## Slide 11: Why the ASTA 50 MeV beam for SUNSTAR?
Enable 1st demonstration
of photons generation
with mini undulators technology

## Slide 12: Planned Experimental Setup
  Location of the mini-undulator
CAV1
CAV2
RTFB
BC1
X113
RTFB
Mini-undulator
e-
e-
VUV detector
e-
Dipole
Beam dump
20 mm, 50 periods
2 mm

## Slide 13: Required Beam Parameters
Parameter | Value/Range | Units
Beam energy | 15, 50 | MeV
Bunch charge | 0.01 – 0.5 | nC
Bunch length | 3 | ps
Bunch repetition rate | 3 | MHz
Number of bunch/macropulse | 1 – 1000 | 
Undulator airgap x / y directions | 2 / 0.2 | mm
Emittance ratio | 100 : 1 | 
Estimation of 2 periods of 5 shifts each

## Slide 14: Considered Experimentations
15 MeV e-beam (switch off cavity CAV2)
  Alignment of the e-beam with the undulator axis
    Beam position monitor + laser + corrector magnets upstream
    Undulator mounted on an actuator
  Expected wavelength: 220 nm (UV radiation)
  Detectable by commercially available photodiode

## Slide 15: Considered Experimentations
2. 50 MeV e-beam (switch on cavity CAV2)
  Expected wavelength: 20 nm (VUV radiation)
  0.5 nC electron beam: ~ 1012 photons/s
Simulated flux density [photons/(s.mm2.0.1%BW)] vs. output energy [eV]

## Slide 16: Summary
Sub-mm undulator and ASTA flat beams capabilities
  2 periods of 5 shifts (estimated)
  Unique experiment on the pathway to novel, compact light sources
Mini undulator (400 µm period)
  reliable fabrication process
  B-fields quantitatively characterized
More sub-mm undulators on the way
  Halbach array (400 µm period)
  micro undulator (50 µm period)

## Slide 17: Acknowledgments
DARPA AXiS Project #N6601-11-1-4198
Pr. Philippe Piot (Fermilab/NIU) for clarifying the physics of flat-beam generation

## Slide 18: Future Magnetic Undulators from UF/GT
  Halbach mini undulator
  higher on-axis magnetic field
  Micro undulator
  magnetic period ~ 50 µm
  selective magnetization process
Soft magnet magnetizing head (microscope view)
Patterned 5–µm–thick NdFeB film (magneto-optic image)

## Slide 19: Selective magnetization process
Begin with unmagnetized electroplated Co80Pt20 or sputtered NdFeB film
Flood magnetize the film (high B-field)
Bring film in contact with magnetizing head Apply a lower reversal B-field
Magnetic patterns are formed based on the features of the magnetizing head