## Slide 1: Fiber Laser Amplifier Technology Based on Photonic Crystal Fibers
Donald L Sipes, Jason D Tafoya and Daniel S Schulz
Optical Engines Inc.

## Slide 2: Topics
Amplifier Design goals
PCF Fiber
Monolithic Components
Amplifier Design
Pulsed Amplifiers

## Slide 3: Optical Engines Inc.
Founded 2004 in Crystal Lake, IL
6 Full and Part time Employees
Background
  Novel Fiber Devices, Fiber Lasers and Mid IR lasers
  First SSL Pumped by BA Diode (1984)
    532nm: 5mW @ $15k (1987) to 100mw @$80 today
  First YbEr Amp:
    21dBm @ $95k (1992) to 32dBm @ $3k today
  Largest Distributed Amplifier Systems (Verizon)
Device Types
  Multi Fiber Pumps and Combined Pumps to over 2kW
  Co and Counter Pump Combiners
  Fiber Amplifier Harnesses and Complete Amplifiers
  Seed Sources

## Slide 4: MOPA Hybrid Lasers Sources
Diode Laser Seed - Compact, Narrow Linewidth, High Speed Modulation
Fiber Laser Mid Stage – High Gain, Flexible Beam path High Average Power
Bulk Amplifier Stage - Low Gain, High Energy Storage, High Hold off
Seed
Source
Beam
Shaping
Isolated Fiber Stages
Bulk Stages
The challenge is to create a fiber amplifier that has enough energy handling capability to consolidate these stages
Issues:
Fiber Nonlinearities
Total Gain
Gain per Stage
Thermal distortions

## Slide 5: NKT Photonics PCF Fibers
Advantages
  Large Core
  Low NA
  High NA Clad
  Advanced Structures Possible
  High F of M
Disadvantages
  Expensive
  Hard to Cleave, Splice
  Custom Combiners
40 um Core, 500um .55 NA Clad
PM Yb Doped Gain Fiber
Current Records: approx 1mj in 2-4nsec
Over 1MW in the psec regime

## Slide 6: Why PCF Active Fibers?

## Slide 7: Segmented Acoustic core with three different domains
990 W output power
73% slope efficiency
300 MHz linewidth
<1.3 M2 value
Fabrication risk: Index matching of Yb-2 and Si has to be very precise in order to obtain perfect mode quality and modal stability.
Yb-1
Si
Yb-2
Si
Yb-2
Si
Yb-2
Craig Robin, Iyad Dajani, Clint Zeringue, Benjamin Ward and Ann Lanari, "Gain-tailored SBS suppressing photonic crystal fibers for high power applications", Proc. SPIE 8237, 82371D (2012)

## Slide 8: Better SBS suppression with smaller domains

## Slide 9: µSAT fiber core with three different components

## Slide 10
Gain Tailored uSAT Core Design
A domain size of 2µm instead of 10µm improves SBS suppression.
Six identical outer cores provide better index homogeneity.
Successful SAT design
Improved µSAT design

## Slide 11: Collaboration with Lt. Col Ben Ward
Delivered
uSAT Fiber
3 Yb-1
8 Yb-2
8 Si
Simulated
uSAT Fiber
4 Yb-1
6 Yb-2
9 Si
uSAT
Shows an
Up to
7.3dB
SBS
Improvement

## Slide 12: Fiber with mode suppressing side cores (MSS)
Un-doped mode suppressing side core on either side of the central Yb-doped core.
First higher order mode couples out of the central core by coupling to the side core.
Due to the airhole in the center, the fundamental mode does not couple to the side core.

## Slide 13: Passive MSS fiber tests
Slow axis, 1064nm, Ø28cm coil
Fast axis, 1064nm, Ø28cm coil
Same seed power

## Slide 14: Etched Air Taper Combiner for Large Diameter PCF Fiber

## Slide 15: Etched Air Taper Combiner Fabrication

## Slide 16: Combiner Fabrication Results: 2 Combiners Fabricated
 | Pump Port Loss (dB) |  |  |  |  |  | Average
Port # | 1 | 2 | 3 | 4 | 5 | 6 | 
Combiner 1 | .21 | 0.10 | 0.14 | 0.13 | 0.08 | 0.09 | .125
Combiner 2 | 0.14 | 0.12 | 0.17 | 0.15 | 0.11 | 0.08 | .128
Combiner Pump efficiency at 97% - 60W heat load at 2kW Pump
PER: 20dB - Signal Efficiency Difficult to measure

## Slide 17: New Fiber PCF Cleaving
40/500 um PCF Web clad (2008)
40/525 um PCF Web Clad (2012)
40/200 um PCF beam Clad
All Excellent Cleaves
All Fibers delivered for this program are 40/530/875 with Beam type Air Clad
All have 20-30um Center Protrusion
Optical Engines has developed a “reinforcing” cleaving process that reduces protrusion to approximately 10um. Sufficient to progress – yet improvement is needed

## Slide 18: PCF Passive – PCF Active Fiber Splice
97.4% Pump Efficiency
95.2% Signal Efficiency
No Detectable
Air Hole Collapse
Improve Cleaving
Process to
10um Protrusion

## Slide 19: Power Amplifier Stage
Fiber Coupled Pumps
PCF Fiber on Water cooled Ring
PCF P to PCF A Splice
Fiber Output
Pump Combiner
The first fiber to be integrated is the AFRL2 SAT Fiber. This fiber does not have Coil Control, so it needs to be mounted on a large water cooled ring. The remaining fibers have coil control and can be mounted in the spiral mount

## Slide 20: 3X fiber Coupled Stacks
3.8kW of available Laser Diode power, 1.8 – 2 kW of fiber coupled power into 6 400um.22NA fibers. Working to achieve over 3kW.
Possibilities: over 4kW fiber coupled pump, factor of 2-3 size reduction. Costs below $10/W
Fiber Outputs

## Slide 21: Current Status: AFRL2 PCF Fiber Results
Stage 4 Pump (W) | Core Power (W) | BWD Power (uW) | PER* (dB) | M2 (U) | M2 (V) | Absorbed Pump (W)
0 | 46.2 | 38 | 11.46 |  |  | 
51 | 80.8 | 38 | 11.94 |  |  | 
153 | 153.4 | 38 | 12.64 | 1.23 | 1.17 | 
255 | 239.5 | 42 | 12.66 | 1.21 | 1.14 | 
362 | 314.2 | 53 | 12.77 | 1.19 | 1.14 | 284
470 | 382.2 | 140 | 12.33 | 1.19 | 1.13 | 
At “Bring Up” stage to Check for thermal performance
20m AFRL2 SAT GT fiber, Co pumped – Monolithic
> 80% Slope Efficiency - 150 and 600MHz Modulation
SBS – MI: Begin to see first signs
* PER Might be affected by slight amount of cladding light

## Slide 22: Current Status: AFRL2 PCF Fiber Results
Combiner
PCF P-A Splice
End Cap
@ 500w Input 976 nm Pump
96% Pump Efficiency
60% Signal Efficiency
97.4% Pump Efficiency
95.2% Signal Efficiency
~ 20W unabsorbed Pump
10% of Signal in Cladding

## Slide 23: Pulsed PCF Amplifier Stage
1-3m Passive PCF Delivery Cable

## Slide 24: Best of Both Worlds Amplifier
PCF Fiber Amplifiers
    500uj in nsec pulses
    Femtoseconds to CW
    Doesn’t need coiling for mode control
    Active and Passive Delivery Cables
Fiber Pumping
Can Remote pumps for bulk stages and deliver via fiber.
Bulk amplifier is a rod in the bundle

## Slide 25: Summary and Conclusions
PCF Amplifiers have many Design “Handles”
  Pumping Options to kW
  Wide Array of Seed Options
  Wide Array of Input and Output Options
  High Degree of Hybrid Options
  Wide array of integration options
Need to look at the whole pulse generation system
Call Us!