## Slide 1: Progress of dielectric loaded gas-filled RF test at MTA
K. Yonehara
APC, Fermilab

## Slide 2: Goal of the project
Make a compact RF system by loading a dielectric material in a RF system
  A compact accelerator system is attractive in general
  Dielectric loaded RF system has been investigated for long time
Especially, a helical cooling channel requires a small radius RF system
  λHCC ~ λRF (V. Balbekov & KY, EPAC’08 THPC110)
HCC RF cell
(F. Marhauser)
Ceramic disk
Be RF win
RF power feeding line
(Access from z direction)

## Slide 3: Goal of the first experiment (I)
Critical issue is a Surface Breakdown
  Ceramic has relatively large secondary electron emission (SEE) yield (SEE > 1)
  Primary electron generates more than one electron
  It induces a cascade process
  Similar as a multipactor process
Fill a buffer gas to eliminate the surface breakdown
  Electrostatic accelerator, e.g. Van der Graaff
  RF power window, e.g. High power Klystron
No application for RF accelerator system
  This concept works only for muon accelerator/cooler
Electron cascade
Ceramic
E
Van der Graaff tube

## Slide 4: Goal of the first experiment (II)
Surface breakdown process can be terminated in a gas-filled RF cavity
Verify this model
  Since this is the first proof of principle test we do not care about a RF power dissipation in a loaded ceramic material
  Material search will be the next step

## Slide 5: Design test cell
Minimize field gradient at triple junction
  Metallic body, ceramic rod and GN2
Frequency = 814.544 MHz @ 1 atm
QL = 4,250 from RF calibration
Donut shape copper electrode
Triple junction

## Slide 6: Simulated RF field distribution
Simulated RF field
  Parallel field on a ceramic rod
  Field enhancement 1.5
  @Electrode
  Low field at triple junction
RF field distribution in SF simulation
Triple junction

## Slide 7: Maximum gradient search on surface of a ceramic rod
In order to avoid permanent damage of ceramic rod, applied RF amplitude was gradually ramped up
  0.5 MV/m step
  RF system was recovered even we had a breakdown
• N2 gas pressure = 1,000 psi
• Observed unusual BD event at
Esurface < 10 MV/m
• Observed usual BD event at
Esurface > 10 MV/m
• Long run at Esurface = 12 MV/m
• No BD during 2 hrs long run
(RF rep rate = 10 Hz)
• Multiple BD at 14.5 MV/m
long run

## Slide 8: Observed quality factor
Observed Quality factor = 4554.02 ± 569.40
Observed frequency = 800.566 ± 0.004 MHz in 2 hrs
RF decay signal
Decay constant
Optical signal
Reflected pwr
Forward pwr
RF pickup

## Slide 9: Weak breakdown at low RF gradient
No breakdown
Weak breakdown
PU
PU
Optical signal
Optical signal
• Continuously build
weak light with offset
• Some current flow on
PMT GND (?)

## Slide 10: Breakdown at high RF gradient
RF signal
Optical signal
τ = 3.6 ns
τ = 73.9 ns
τ = 106.9 ns
τ = 162.5 ns
• Observed decay time constants, τ
• Various τ at various BD locations

## Slide 11: Gas pressure dependence
Old cavity test
RF gradient at highest point
(convex of electrode)
RF gradient on ceramic rod
• Open blue circle: peak E at electrode
Close blue circle: surface E
• Orange triangle:
Compare old HPRF test with GN2
• At p < 200 psi, observed peak E
(open circle) shows gas BD
• At p > 200 psi, observed peak E
shows a plateau
• The plateau seems to be determined
by the dielectric strength of ceramic
rod
Gas BD slope
Metallic BD

## Slide 12: Consider breakdown mechanism
Weak breakdown
  Some amount of BD light came out from test cell
  Never seen such a BD in past gas-filled RF test
  It looks like a multipactor in a vacuum cavity
  It disappeared in higher RF gradient
  Is it a surface breakdown?
Regular breakdown
  Observed intense BD light at high RF gradient
  Maximum RF gradient is close to the dielectric strength of alumina rod

## Slide 13: Open cavity after first run
• Saw a small piece of broken ceramic
• Saw one breakdown spot on a Cu
electrode

## Slide 14: Inspect ceramic rod after test
Crack
Bottom
Top
Crack
• Since bottom part of rod is inserted to the rod holder deeper than top
location of cracks is the middle of cavity that is the highest RF gradient
Top
Bottom

## Slide 15: Summary
Pressure measurement shows that there is a transition of BD mechanisms at p ~ 200 psi
  Gas BD at p < 200 psi
  New BD (plateau) at p > 200 psi
Saw weak BD
  Surface BD?
The plateau can be the dielectric strength of ceramic rod (15 ~ 16 MV/m)
  This can explain why ceramic rod is broken

## Slide 16: Discussion and future plan
These are just hypothesis although everything can be explained
We do not know when the ceramic was broken
Plan in near future (in 2013)
  Measure maximum RF gradient w/o ceramic rod
  Repeat the same test with a new ceramic rod (same material)
  Repeat the same test with different materials
    TiO
    Teflon