## Slide 1: Mode-Locking in an Erbium-Doped Fiber Laser
Ethan Lane
Rose-Hulman Institute of Tech.

## Slide 2: Overview
Purpose
Theory
  Lasers
  Mode locking
Piecewise testing of fiber laser parts
  Amplifier
  Enclosed laser
  Mode locked laser
Conclusion

## Slide 3: Purpose- Why Erbium?
~femtosecond pulses from large bandwidth
Erbium is cheaper due to the telecommunication industry
Erbium doping offsets dispersive effects from standard fiber

## Slide 4: Theory
Parts to a laser
  Pump
  Lasing material
  Optical cavity
Lasing occurs in the erbium-doped fiber as electrons are excited by pump light

## Slide 5: Laser Schematic

## Slide 6: Mode Locking Intro
The most common way to get picosecond or smaller pulse durations is through mode locking
Mode locking works by locking all of the different modes within a laser cavity to a fixed phase
In our case, achieved with wave plates

## Slide 7: Mode Locking Continued
The sum of the time-domain powers of each mode reduces to:
The top figure shows the normalized time-domain power for different n.
  - Notice the decrease in peak width for increased n.
The bottom figure shows the power dependence on n at t=0 (the max power)
  - This shows the large increases in peak power as more wavelengths are added.
MORE BANDWIDTH = MORE WAVELENGTHS = MORE POWER + SHORTER PULSES

## Slide 8: EDFA (Erbium-Doped Amplifier) Test
Use pump to excite erbium fiber and a 1550 nm Menlo laser to stimulate photon emission
Able to measure pump power vs. input current
Close to 15 dB theoretical value
Chart: .5m Erbium Amplifier Test
| 0 | 50 | 100 | 150 | 200 | 250 | 300 | 350 | 400
 | -4.1098 | -4.1011 | 2.7443 | 6.7961 | 8.7679 | 10.0649 | 11.0233 | 11.7774 | 12.3932

## Slide 9: Enclosed Laser Schematic

## Slide 10: Enclosed Laser Test
Output coupler installed and a loop created to make a laser cavity.
Creates a loop from the amplifier for amplification of power with every pass.
Limited in maximum power by gain saturation
Chart: .5m Erbium Laser Test
| 0 | 50 | 100 | 150 | 200 | 250 | 300 | 350 | 400 | 450 | 500
 | -7.5007 | 0.47275 | 3.2201 | 4.8643 | 6.0249 | 6.9135 | 7.6938 | 8.275 | 8.7633
Chart: .5m Laser Spectrum Test

## Slide 11: Mode-Locked Schematic

## Slide 12: The Final Product

## Slide 13: Mode Locking Tests
Polarizers installed and rotated to achieve mode locking
Broad optical spectrum consisting of many wavelengths
Oscilloscope output shows pulse travelling in cavity; depends on cavity length
Data taken at 254 mA of pump laser current
~400 femtosecond pulse width measured
Chart: Optical Spectrum
Chart: Oscilloscope Output
~25 ns

## Slide 14: Conclusion
Currently have a working mode locked erbium fiber laser with a 2.66 mW power output and pulse width of ~400 femtoseconds.
Future plans to optimize the system further to yield shorter pulse widths by attempting to get a broader optical spectrum.

## Slide 15: Acknowledgments
Winter, Axel. Fiber Laser Master Oscillators for Optical Synchronization Systems.
Diss. Zugl.: Hamburg, Univ., Diss., 2008, 2008. N.p.: n.p., n.d. Print.
Special Thanks to Jinhao Raun, Andrea Saewert, Victor Scarpine, David Peterson, SIST program workers

## Slide 16: Autocorrelation and Pulse Width
Achieving a small ~fs pulse width for this fiber laser is one of the main goals
Autocorrelator used to convert the small pulses into something measurable.
Works much like a Michaelson interferometer
Measured pulse width of ~400 femtoseconds
Chart: Auto-Correlator Output

## Slide 17: Autocorrelator Calculation
Conversion from mirror distance into time traveled:
Full-width half-maximum from autocorrelator is -19.839 µs
Slope from calibration is -27.369
Chart: Auto-Correlator Calibration
| -110.5 | -134.9 | -160.19999999999999 | -183.4 | -207.4 | -232.2 | -257
 | 0 | 666 | 1332 | 1998 | 2664 | 3330 | 3996

## Slide 18: Radiofrequency (RF) Spectrum
Shows the frequency at which laser light circulates within the cavity
Peak location depends on the cavity length
This plot was obtained as a final optimization of the laser parameters.
A good RF spectrum will resemble a single, sharp peak and have no fringes