## Slide 1: Status of R&D at UCSB
Paul Szypryt
Mazin Lab
August 26, 2013

## Slide 2: Status as of Palomar 2012

## Slide 3: SCI-4
TiN inductors and capacitors, Nb feedlines
Energy resolution of around 10%
2024 (44x46) pixel array
222 micron pixel pitch
resonator yield after fabrication
70% good pixel yield

## Slide 4: ARCONS
Operated at 110 mK
8 ROACH boards for readout
350–1100 nm bandwidth, after filters
20x20 arcsecond field of view

## Slide 5: Science Results
Crab Pulsar
SDSS J0926+3624
3% enhancement in optical flux coincident with Crab Giant Radio Pulses (GRPs)
Period change of

## Slide 6: Current Work

## Slide 7: X-ray MKIDs
  KID inductor on SiN Membrane, capacitor on bulk Si
  Thermal Kinetic Inductance Detectors (TKIDs)
  X-ray hits absorber on island, heats island, breaks quasiparticles changes surface impedance

## Slide 8: X-ray MKIDs
Pulse lifetime of up to 1.6 ms
Saturated, but noise and pulse shape imply <10 eV at 6 keV

## Slide 9: Optical Membrane Devices
Inductor suspended on SiN membrane, no absorber
Eliminates location dependent response of photon events
Phonon noise limited, due to heat transfer between island and heat bath,
Theoretical energy resolution of 100 at 300 nm and 100 mK.

## Slide 10: Optical Membrane Devices
  Membrane legs successful, even with 1x125 μm dimensions
  Some defects, but fairly high yield
Tapered membrane edge and extra step plug to alleviate step coverage problems

## Slide 11: Trenched Devices
Trenching in Si near capacitor legs
TiN capacitor remains on hills
Reduce TLS noise

## Slide 12: Trenched Devices

## Slide 13: Carbon Nanotube Absorbers
Currently growing CNTs on MKIDs to act as photon absorbers – potential for near 100% QE over a huge band!
Ni catalyst added to inductor
Plasma enhanced chemical vapor deposition using C2H2 and NH3 gas
Can be used with TKIDs, where inductor is separate from absorber

## Slide 14: Carbon Nanotube Absorbers
Vertically aligned CNT forests are the only material that currently emulates a blackbody across the range of MKID sensitivity (~0.2-10μm).
Can be placed near MKID inductors without increasing TLS noise
Can currently grow CNTs on MKIDs, still need to refine photon detection process

## Slide 15: Focused Ion Beam Milling
Resonant frequency dependent on capacitance and inductance
Very sensitive to inductor shape, less sensitive to capacitor shape
Can remove capacitor material to reduce capacitance, and therefore increase resonant frequency

## Slide 16: Focused Ion Beam Milling

## Slide 17: Focused Ion Beam Milling

## Slide 18: Focused Ion Beam Milling

## Slide 19: SCI-5 Array
Connection to ground at center of inductor, where fields should be smallest. May help with issues caused by floating pixels.
Refined process to take advantage of NIST multilayer TiN, which is destroyed by HF etch in our current process.

## Slide 20: SCI-5 Array
JPL TiN film
NIST Multilayer TiN film

## Slide 21: SCI-5 Array
Deposit TiN Outline
Nb Feedline/Ground Plane
Dielectric for Crossovers
Nb Feedline Center strip
Gold Bond Pads
Pattern TiN

## Slide 22: Future Projects

## Slide 23: Palomar 2013
Improve quantum efficiency
  Microlens alignment stage
  Improving filtering
  Realuminizing Coudé flat
Improve energy resolution
  Low-noise HEMT amplifiers
  ROACH-2
Eliminate hot pixels
  Virtual ground strap

## Slide 24: ROACH-2
More FPGA resources
Faster clock rates
Better digital filters
Increase pixels per ROACH board
https://casper.berkeley.edu/

## Slide 25: Other Projects
DARKNESS
  DARK-speckle Near-IR Energy-resolved Superconducting Spectrophotometer
KRAKENS
  Keck Radiometer Array using KID Energy Sensors
  180x180 pixels, 54x54” field of view, R = 20, Cassegrain focus
Mega-z

## Slide 26: Summary
Palomar 2012 successful, but much room to improve
Recent efforts:
  X-ray MKIDs
  Trenched Devices
  Carbon Nanotube Absorbers
  Focused Ion Beam Milling
  SCI-5 Array Design
Aiming to improve QE, energy resolution, and yield, and to eliminate hot pixels, for next run