## Slide 1: Technology Development Summary
  MAP Collaboration 2013
  FNAL
  June 22, 2013

## Slide 2: The Key Technical Issues
High-gradient, Low-frequency (200-1000 MHz) RF Cavities
High-field Solenoids (≥ 20T)
Muon beam decay in storage rings
Fast-pulsed (400Hz) RCS dipoles

## Slide 3: The RF Program
NCRF
    Vacuum RF
      201 MHZ
      805 MHz
    HPRF
SRF

## Slide 4: 805 MHz
All-Season Cavity
29 MV/m gradient achieved at B = 0T
20 MV/m gradient achieved at B = 3T
La b G magnet re-trained to 5T Cavity will be re-measured with 5T background field

## Slide 5: 805 MHz Modular Cavity
Cavity design at LBNL and SLAC with new coupler design
Cavity Fabrication at SLAC
Delivery to MTA at end of FY13
Test with different windows (Cu/Be) and body lengths
Cornerstone of FY 14, 15 vacuum RF program

## Slide 6: HPRF Program
Beam test with 400 MeV proton beam (up to 3x1011)
Beam induced plasma-loading effect
Result with dopant (1% dry air) added

## Slide 7: 805 MHz HPRF
Goal:
Demonstrate that HPRF cavities can be used in the HCC
Results:
50 MV/m gradient achieved with H2 gas above 400 PSI
No dependence on magnetic field observed up to B=3T
(Can now test to 5T)
First test with dielectric material
(Al2O3)

## Slide 8: Development of 201 MHz Cavity
42-cm
Cavity fabrication technique development, in collaboration with JLab; The cavity has been high power tested at MTA, Fermilab

## Slide 9: MICE Prototype Cavity Test at MTA
Installation of required infrastructure at the MTA
Testing to commence Q1 FY14

## Slide 10: MP Simulation Studies
  Collaboration with SLAC using ACE3P, including some code development
  Simulation studies using MICE B-field map & cavity and coupler geometry
Studies providing valuable insight into high-power rf coupler issues

## Slide 11: The 200 MHz SRF Cavity
Electro-polished half cell
Magnetron Nb film (1-2 mm) sputtering
DC voltage: 400-650 V
Gas pressure: 2 mTorr
Substrate T: 100 °C
RRR = 11
Tc = 9.5 K

## Slide 12: Search for Nb/Cu Bonding
Two technologies are under consideration
Explosion Bonding
Electro-forming

## Slide 13: The Spinning Process

## Slide 16: Path to Demonstrate a 30+ T Solenoid
Step-by-step R&D approach consisting of three (or more) coils:
>10 T HTS solenoid (midsert): SBIR Phase II with PBL
>12 T HTS (insert): SBIR Phase II with PBL
>8 T LTS (outsert): Not yet started
1
2
3
≥20 T HTS Solenoid (1 & 2):
≥30 T Solenoid (1, 2 and 3):

## Slide 17: Fully Constructed (insert + midsert) HTS Solenoids for 20+ T Test
Achieved 6T with 12 of 24 pancakes (each pancake made with 100 m HTS)
Achieved 15T with 14 pancakes (each pancake made with 50 m HTS)

## Slide 18
77 K Test of Full HTS Midsert (full midsert contains 24 pancakes)
Tests performed in Nov. 2012

## Slide 19: Resent Retest at 770 K
16
15
8
11
5
1
6 out of 24 coils show degradation

## Slide 20: Repairing of the Coils
Start with coil #15&#16 (the worst pair).
Splice joint is replaced with a new type of diagonal joint (used in another program)
First turn is removed from each pancake
Became Good
Was Bad
Became Good
Was Bad
Became Better (but not good enough)
Was Bad

## Slide 21: The cable Jc is significantly improved by overpressure processing
OP 10 bar
Ends sealed; no leakage
10 bar overpressure processing increased the Jc by 4 times, and improved n-values.
Shen (FNAL), Jiang (FSU)
Bi2212 Solenoids
Tengming Shen, FNAL

## Slide 22: Fast Pulsed Magnets Don Summers, UMiss
Grain oriented steel
±1.8T
1410 Hz achieved

## Slide 23
Test magnet construction status
0 to 1.8 T pulses
40 Hz Achieved
HTS coil being inserted into magnet core
HTS coil installed in magnet core
Rapid-cycling HTS magnet test arrangement
Magnet cryostat
Leads
Ramping PS
Rapid Cycling HTS Magnet Henryk Piekarz, FNAL

## Slide 24: Radiation-Hard Insulation Studies A. Zlobin, FNAL
Epoxy limits magnet radiation life-time
Search for radiation-hard material to replace epoxy started at FNAL 10 years ago (D. Chichili et al, ASC 2002)
  MATRIMID 5292 - a bismaleimide solution
  high radiation resistance
  tolerable viscosity and pot-life
  excellent mechanical, electrical and thermal properties
A 1 m long Nb3Sn quadrupole coil was impregnated with MATRIMID and tested in 2012
  excellent impregnation quality
  quadrupole mirror structure (FNAL)
  good quench performance
MATRIMID is a potting material for future Nb3Sn accelerator magnets
  LHC IRQ, ILC BDS, MC-NF-HF
R. Bossert et al., ASC2012, September 2012.
Matrimid
CTD101K epoxy
Coil Test Structure (quadrupole mirror)
Coil training comparison
Quadrupole coil impregnated with Matrimid

## Slide 25: MATRIMID Coil Next Steps A. Zlobin, FNAL
Technology scale up
  2-m long Nb3Sn dipole coil with 60 mm bore and 15 mm wide cable has been impregnated with MATRIMID in Feb 2013
  Coil inspection is in progress
When resources allow
  5.5 m long dipole practice coil impregnation with MATRIMID
  1-2 m dipole coil fabrication and test in dipole mirror structure
The test stack program will be completed
  mechanical, thermal and electrical testing of stacks at room temperature and 4.5 K using cables of various types
Radiation testing of MATRIMID coil samples is planned in collaboration with CERN
‘Synergistic’ interaction with LARP program
  directly applicable to MAP IR Magnets
A.V. Zlobin et al., IPAC2013, May 2013.
R. Bossert et al., CEC/ICMC2013, June 2013.

## Slide 26: The High-Power-Target System
V. Graves, ORNL

## Slide 27: Taper Length Study
H. Sayed, BNL
Taper Lengths 5 to 7m optimal

## Slide 28
Magnet Coil Configurations
Bob Weggel (MORE/PBL) [IPAC13, TUPFI073]
Baseline (IDS-NF)
Revised coil configuration has essentially no ``stops bands (H. Sayed):
Field perturbations at the ends of the 5-m-long Decay channel magnets can lead to “stop bands.”
Axial field profile for a 7-m taper:
2 configurations with 7-m taper and 15-T peak

## Slide 29: Comparison of Meson Production
At 3 GeV,
Carbon gives more production than Ga or Hg.
X. Ding, UCLA
Preliminary

## Slide 30: Looking Forward FY 14,15
NCRF
Retest of 805 RF cavities up to 5T
Testing of MICE prototype 201 MHz cavity (with CC by end of FY15)
Testing the 805 Modular cavity at the MTA
Design, fabricate and test dielectric loaded HPRF cavity
Goal—test HPRF cavity with 2x 1012 ppp
SRF
Test of bonding techniques (explosion, electroforming)

## Slide 31: Looking Forward FY 14,15
Magnets
25T Solenoid demonstration
Design of 35T Solenoid
Design of fast-pulsed dipole system
100+m of Biscco cable
Radiation reduction in ring magnet cold-mass
Target Systems
Target configuration for 1MW, 3GeV proton beam

## Slide 32: Backup Slides

## Slide 33: Two Solenoids are being built and tested
Solenoid #1
(Mid-sert)
ID = 10cm
OD=17cm
24 Pancakes
Solenoid #2
(Insert)
ID = 2.5cm
OD=9.1cm
14 Pancakes

## Slide 34: The Capture Solenoid
A Neutrino Factory and/or Muon Collider Facility requires challenging magnet design in several areas:
  Target Capture SC Solenoid (15T with large aperture)
  Stored Energy ~ 3 GJ
  10MW, 5T resistive coil in high radiation environment
  Liquid Hg Jet
  Possible application
  for High
  Temperature Superconducting magnet technology