## Slide 1: IRRADIATION DAMAGE AND MATERIAL LIMIT: ILLUSTRATION OF A WAY TO CODIFY RULES WITH RCC-MRx CODE
Cécile Pétesch, Thierry Lebarbé CEA
Sophie Dubiez-Le Goff, Claude Pascal AREVA

## Slide 2: Contents
RCC-MRx presentation
Code philosophy
Consideration of irradiation effect in mechanical design rules
  Code approach
  Border lines
  Design rules
Conclusion

## Slide 3: Contents
RCC-MRx presentation
Code philosophy
Consideration of irradiation effect in mechanical design rules
  Code approach
  Border lines
  Design rules
Conclusion

## Slide 4: RCC-MRx, one of the Afcen Codes
RCC-C
Fuel Assemblies
ETC-C
Civil Engineering
Structures
RCC-M
Design and construction of PWR Mechanical components
ETC-F
Fire protection
BOARD &
Executive Committee
Editorial committee
Training committee
RCC-E
Electrical – I&C Systems and components
RSE-M
In-Service Inspection rules PWR Mechanical components
RCC-MRx
Design and Construction Rules HT/Irr. Mechanical Components

## Slide 5: RCC-MRx Code Background
AFCEN
RCC-MR
1985 -1993 – 2002 - 2007
RCC-MX
2005 - 2008
RCC-MRx
Draft 2010 - 2012

## Slide 6: RCC-MRx Code Background
RCC-MR
AFCEN Code
components operating at high temperature ASTRID
Specificities: high temperature, slender structures
2007 version Integrates Iter VV + european standards + new French regulations (ESPN)
RCC-MX
one CEA, Areva TA and Areva NP Committee
Irradiated components, Osiris, Orphée, irradiation devices,JHR
Specificities : irradiated structures, aluminium and zirconium alloys

## Slide 7: Contents
RCC-MRx presentation
Code philosophy
Consideration of irradiation effect in mechanical design rules
  Code approach
  Border lines
  Design rules
Conclusion

## Slide 8: Philosophy of the existing rules
To design components
  mechanical components
  For nuclear installations
  Safety relevant
For dedicated installations
  design of components operating at high temperature
  design and construction of new research reactors, their auxiliaries and their associated experimental devices
Based on existing practices and available data
  As a consequence, the code is always evolving
Within a certain scope

## Slide 9: Scope of the existing rules
To design components
  pumps,
  valves,
  pipes,
  bellows,
  box structures,
  heat exchangers,
  irradiation devices,
  supports,
  handling and driving mechanisms.
For dedicated installations
  Neutron flux, standard nuclear installations,
  Temperatures up to 700°C,
  Possibility to apply complementary requirements to comply to a given regulation (PED or French ESPN).

## Slide 10: Scope of the existing rules
RCC-MRx subsection Z - Appendix A3 or Probationary Phase Rules | A3.4 : Basic data | A3.5 : Creep data | A3.6 : Irradiation data | A3.8 : Fracture Mech. data
Non Alloy Steels (13 RPS in Tome 2) |  |  |  | 
A3.10NAS : P235GH | X |  |  | 
A3.11NAS : P265GH | X |  |  | X
A3.12NAS : P295GH | X |  |  | X
Alloy Steels (16 RPS in Tome 2, 4 RPS in RPP)) |  |  |  | 
A3.11AS : 25CrMo4, 42CrMo4, 30CrNiMo8 | X |  |  | 
A3.13AS : 16MND5 | X and Bolts |  |  | 
A3.14AS : 10CrMo9-10 fully annealed | X | X |  | 
A3.15AS : 13CrMo4-5 quenched and tempered | X | X |  | 
A3.16AS : 2.25% Cr, 1% Mo normalised tempered or quenched tempered | X | X |  | 
A3.17AS : X10CrMoVNb9-2 quenched tempered | X | X |  | 
A3.18AS : X10CrMoVNb9-1 normalised tempered or quenched tempered | X | X |  | X
A3.19AS : Eurofer X10CrWVTa9-1 normalised tempered | X |  |  | 
Stainless Steels (25 RPS in Tome 2) |  |  |  | 
A3.1S : X2CrNiMo17-12-2(N) solution annealed | X | X | X | X
A3.2S : X6CrNi18-10 et X5CrNi18-10 solution annealed | X | X |  | 
A3.3S : X2CrNiMo17-12-2, 17-12-3, X2CrNiMo18-14-3 | X | X | X | 
A3.4S : X2CrNi18-9, X2CrNi19-11 | X | X |  | 
A3.6S : X15CrNiW22-12 solution annealed followed by aging | X | X |  | 
A3.7S : X2CrNiMo17-12-2 around 20% work hardening | X and Bolts | X | X | 
A3.8S : X4CrNiMo16-05-01 quenched and annealed | X and Bolts |  |  | 
A3.10S : X6NiCrTiMoVB25-15-2 heat treated structural hardening | X and Bolts | X |  | 
Special Alloys Ni-Cr-Fe (5 RPS in Tome 2) |  |  |  | 
A3.5SA : X5NiCrTiAl33-21 after annealing heat treatment at 980°C | X | X |  | 
Aluminium alloys (7 RPS in Tome 2, 1 RPS in RPP) |  |  |  | 
A3.1A : 5754-O | X | X | X | 
A3.2A : 6061-T6 | X | X | X | 
Zirconium alloys (4 RPS in Tome 2) |  |  |  | 
A3.1Z : Zircaloy 2 | X | X | X | 
A3.2Z : Zircaloy 4 | X | X | X | 

## Slide 11: Contents
RCC-MRx presentation
Code philosophy
Consideration of irradiation effect in mechanical design rules
  Code approach
  Border lines
  Design rules
Conclusion

## Slide 12
Effects of neutron irradiation on steels (316LN tensile curves)
Code approach
Impact on parameters relevant for
the mechanical design :
Tensile strength
Yield strength
Ductility
Elongation at maximum force
Swelling
Creep irradiation strain

## Slide 13: Code approach
Significant irradiation?
Design rules without effect of irradiation
Design rules without effect of irradiation
Design rules with effect of irradiation
NO
MAXIMUM ALLOWABLE IRRADIATION CURVE
NEGLIGIBLE IRRADIATION CURVE
YES
Excessive deformation
Plastic instability
Fatigue
Progressive deformation
Fast fracture
Above irradiation has to be considered
Above rules are not validated anymore

## Slide 14: Border lines
Irradiation data supplied
  In Section III / Tome1 / Subsection Z / Appendix A3
  Data given in function of parameters considered as driven the material mechanical behavior
  For
    Stainless steels (material mechanical behavior driven by dpa NRT)
      A3.1S: X2CrNiMo17-12-2(N) solution annealed (« 316L(N) »)
      A3.3S: X2CrNiMo17-12-2, X2CrNiMo17-12-3, X2CrNiMo18-14-3 solution annealed (« 316L»)
      A3.4S: X2CrNi18-9, X2CrNi19-11 solution annealed (« 304L »)
      A3.7S: X2CrNiMo17-12-2 around 20% work hardening (« 316L work hardening»)
    Aluminum alloys (material mechanical behavior driven by Fluence in conventional thermal neutrons (E= 0.0254eV), corresponding to the most probable neutron energy in water at 20°C)
      A3.1A: 5754-O (solution annealed)
      A3.2A: 6061-T6 (structural Hardening)
    Zirconium alloys (material mechanical behavior driven by irradiation flux in fast neutrons E>1MeV per cm2)
      A3.1Z: Zircaloy 2
      A3.2Z: Zircaloy 4

## Slide 15: Cr-Ni-Mo stainless steels irradiation border lines
Definition of the negligible irradiation condition
  Data from steels 316, 316L and 316L(N) after irradiation have been analyzed
    Irradiations performed in Sodium Fast Reactors and Experimental Fission reactors between 60 to 800°C
    Effect of irradiation similar on these grades results given without distinguishing the grades as regards carbon and nitrogen contents
  In order to define the negligible irradiation conditions, various properties are compared:
    Tensile strength,
    Yield strength,
    Ductility,
    Elongation at maximum force,
    Swelling,
    Creep irradiation strain
  INCREASE  favorable effect on the rules limiting the allowable stresses
  No observed at low doses
  ≈ Not observed at low doses
  DECREASE
  DECREASE
  Criterion on ductility is chosen (Elongation at maximum to scattered)
  A%= 0.7x the minimum value of A% (unirradiated)
Definition of the maximum allowable irradiation condition
  Saturation of the effect of irradiation on tensile properties  not possible to link the maximum allowable irradiation to the evolution of the ductility properties.
  A criterion based on swelling and its dimensional consequences is therefore used.
  ΔV/V ≤ 3% by volume or ΔL/L ≤ 1 % in linear dimensions

## Slide 16: Cr-Ni-Mo stainless steels irradiation border lines
Maximum allowable irradiation
Significant irradiation
Negligible irradiation

## Slide 17: 6061 T6 irradiation border lines
Definition of the negligible and maximum allowable irradiation condition
  Data from tensile test, impact test, and toughness test after irradiation have been analyzed
    Irradiations performed in HFIR, HFBR and BR2 reactor
    Temperature range: 50-100°C
  In order to define the negligible irradiation conditions, various properties are compared:
    Tensile strength,
    Yield strength,
    Ductility,
    Elongation at maximum force,
    Impact tests
    Toughness,
    Swelling
  INCREASE  favorable effect on the rules limiting the allowable stresses
  ≈ Not observed at low doses
  DECREASE
  DECREASE
  Slightly affected
  Not affected
  Criterion on ductility is chosen
  A% (irradiated) = Agt% (unirradiated)
Definition of the maximum alllowable irradiation condition
  Criterion on ductility is chosen
  A%= 0 (by extrapolation of the minimum curve)

## Slide 18: 5754-O irradiation border lines
Definition of the negligible and maximum allowable irradiation condition
  Data from tensile test, impact test, and toughness test after irradiation have been analyzed
    Irradiation performed in Osiris and Melusine experimental reactors
    Temperature range <50°C
  In order to define the negligible irradiation conditions, various properties are compared:
    Tensile strength,
    Yield strength,
    Ductility,
    Elongation at maximum force,
    Impact tests
    Toughness,
    Swelling
  INCREASE  favorable effect on the rules limiting the allowable stresses
  ≈ Not observed at low doses
  DECREASE
  DECREASE
  Slightly affected
  Not affected
18
  Criterion on ductility is chosen
  A%= 9.5%
Definition of the maximum allowable irradiation condition
  Criterion on ductility is chosen
  • A%= 0 (by extrapolation of the minimum curve)

## Slide 19: 6061 T6 irradiation border lines

## Slide 20: Zirconium alloys irradiation border lines
Definition of the negligible irradiation condition
  Tensile data from Zy4 (mainly)
    Irradiations performed in Pressurized Water reactors (fuel cladding tubes) and NaK (plates for grids)
    Temperature range at 20°C and 315 and 350°C
  In order to define the negligible irradiation conditions, various properties are compared:
    Tensile strength,
    Yield strength,
    Ductility,
    Elongation at maximum force,
    Anisotropic swelling
  INCREASE  favorable effect on the rules limiting the allowable stresses
  No observed at low doses
  DECREASE
  DECREASE
  Criterion on ductility is chosen (provisionally)
  • A%= 2.5%
Definition of the maximum allowable irradiation condition
  Criterion on ductility is chosen (provisionally)
  • A%= 0 (by extrapolation of the minimum curve)

## Slide 21: Zirconium alloys irradiation border lines

## Slide 22: To sum-up the criteria
 | Negliglible irradiation | Maximum allowable irradiation
A3.1S: « 316L(N) » | Ductility |  Swelling
A3.3S: « 316L» | Ductility |  Swelling
A3.7S: « 316L work hardening» | Ductility |  Swelling
A3.4S: « 304L » | Ductility | Not supplied
A3.1A: 5754-O (solution annealed) | Ductility | Ductility
A3.2A: 6061-T6 (structural Hardening) |  Ductility | Ductility
A3.1Z: Zircaloy 2 | Ductility | Ductility
A3.2Z: Zircaloy 4 | Ductility | Ductility

## Slide 23
Mechanical codes prevent from the usual damages:
  Excessive deformation
  Plastic instability
  Elastic and elastic-plastic instability
  Progressive deformation
  Fatigue
  Creep
  Fast fracture
Possible methods:
  Direct verification:
    Experimental Analysis
    Elastic-plastic Analysis
  Elastic analysis:
    Detailed elastic analysis
    Simplified elastic analysis: use of flexibility and stress indices for standard components
Design Rules for significant irradiation

## Slide 24: Design Rules for significant irradiation
Excessive deformation/plastic instability
Fracture mechanic
J(a,C)≤ JIC
Progressive deformation
  P et Q to compare to kSm
Fatigue
  tot  
  Usage factor V = specified Ncycles / allowable Ncycles < 1
Excessive deformation/plastic instability
Fracture mechanic
J(a,C)≤ JIC (irradiated)
Progressive deformation
  Analyse non irradiated material
Fatigue
  Fatigue curve without irradiation:  increase

## Slide 25
Principle of determination of Sem and Set
SemX and SetX are « materials » limits, functions of irradiation G, temperature q, level of criteria X, and stress redistribution factor r
G dependant on materials (dpa, fluence of fast or thermal neutrons,…)
Design Rules for significant irradiation
Slope = -E/r
r = 0 : strain controlled
r = ∞ : load controlled
Sem(B)
Set(C*)
Exact formulas
 Rm, At, Agt, ep(Smx) are dependent on G (irradiation) and q
r has to be determined (r=3 is generally a good value except for pipes)
kX is the design margin (2.5, 2, or 1.35)
kB=1 for brittle materials, 1.5 for ductile (general formula given in A3.GEN)

## Slide 26: Contents
RCC-MRx presentation
Code philosophy
Consideration of irradiation effect in mechanical design rules
  Code approach
  Border lines
  Design rules
Conclusion

## Slide 27: Conclusion
A first set of rules included in RCC-MRx 2012, associated to a defined scope.
Still a work to done:
  To clarify the scope of considered irradiation in the existing rules and clearly indicate their limitation : flux? He? Irradiation creep?
  To improve the existing rules: need the feedback of their application
Irradiation data driving the mechanical behavior are dedicated to type of irradiation
  not transposable without analyse
Rules have to be relevant with regard to damage prevention specific to an irradiation type
  damage have to be prevented by a dedicated ( for each irradiation type) set of rules.
But we can think that prevention of damages for given mechanical data may be transposed as long as there is no other damage that may impair the irradiated material mechanical behavior.

## Slide 28: THANK YOU FOR YOUR ATTENTION