## Slide 1: Design, optimization and operation of beam intercepting devices for CERN’s fixed target physics
M. Calviani (CERN)
5th High Power Target Workshop, FNAL
With contribution from: R. Losito, A. Perillo-Marcone, V. Venturi, C. Torregrosa, V. Vlachoudis, R. Catherall, A. Ferrari, R. Folch, T. Stora, R. Jacobsson and many others

## Slide 2: Outline
CERN’s fixed target physics program
Review of CERN’s accelerator complex
Low-Z devices
High-Z devices
Conclusions

## Slide 3: Review of CERN’s fixed target physics
CERN has a long and varied history of fixed target experiments, contributing to a diverse program of research
  Essential part of the lab’s scientific program
Hadrons physics (COMPASS, NA61...)
Nuclear physics (ISOLDE)
Neutron physics (n_TOF)
Antimatter physics (AD)
Neutrino physics (WANF, CNGS...)

## Slide 4: Review of CERN’s fixed target physics
Some of the challenges:
  Cohabitation with collider physics and beam sharing
  Different facilities operating at the same time
  High intensity pulsed beams
  High reliability required

## Slide 5: CERN’s accelerator complex
~1015 proton/year to LHC
>1020 protons/year to fixed targets

## Slide 6: Low-Z targets
Operational experience:
  North Area general purpose targets
  CNGS HE neutrino target
Future projects
  CENF LE neutrino target

## Slide 7: North Area targets
4 multipurpose target stations
  Beryllium S-200-F
  Slowly extracted 400 GeV/c
  2.5*1013 p/spill  1.6 MJ/spill
  Beam energy ~330 kW over spill, ~100 kW over supercycle
Why beryllium?
  Most of the time physics requires mixed hadron/electron beams  largest X0/lint are preferred
  Target lengths from 5 to 50 cm
TCC2
T2
T4

## Slide 8
Plate targets (air cooled)
Operational temperature ~280 °C, ~60 MPa tensile stresses
High reliability required – no exchange expected in 20 years operation!
Global consolidation ongoing, irradiated Be plates ~O(several 1020 POT)
Rod targets (air cooled)
beam
beam

## Slide 9: CNGS target design
Long baseline neutrino appearance experiment
Optimized for high energy (~15-20 GeV) neutrino production – segmented target, outside horn
Designed for 750 kW, operated at max ~500 kW
4 mm Ø, 0.53 mm (0.32 mm) 1s beam

## Slide 10: CNGS engineering challenges
CNGS target unit conceived as a static sealed system with 0.5 bar of Helium
  130 cm long graphite target (~3l)
  Radiative-cooled target ~1200 °C
  Radiation resistance of employed graphite (2020PT, C-C composites, etc.)
Target rod support structure
Sealed cooling finned tube (Al 5083 H111)
Target support tube (C-C composite)

## Slide 11: CNGS operational experience
No physical failure of the target observed at the end of operation (1.85*1020 POT)
  1.5 DPA
  Advantage of operating at high temperature
FLUKA estimation for 1.85*1020 POT
…But failure of target rotation mechanism
  Rust/pitting corrosion due to use of low grade X46Cr13 balls
  ZrO2 bearings tested and presently under analysis
2010: 6.7*1019 POT 2.7 MGy
2012: 3.9*1019 POT ~2.0 MGy
Notes: Minimization of shrinkage and reduction of thermal conductivity + favour annealing and reduction of imperfection

## Slide 12: Future projects (CENF)
5 GeV pion focusing – central nm energy ~1.8 GeV
Target inside horn, followed by a reflector
See poster session C. Strabel & V. Venturi
CERN is designing a short baseline shallow installation (link)
Design include the study for a 200 kW graphite target

## Slide 13: CENF target R&D
100 cm long, 12 mm Ø
  ~2 kW deposited power, He-cooled graphite 2020PT
Graphite to be maintained at 600-700K
Baseline fully cantilever inside horn
External retaining structure in beryllium
  Guarantee sufficient rigidity and low pion reabsorption
Full FEM/CFD analysis performed
He gas cooling test loop will be studied in 2014/2015
See poster session V. Venturi

## Slide 14: High-Z targets
Operational experience:
  n_TOF - neutron spallation source
  Antiproton production (AD)
  ISOLDE – radioactive beam
Future projects:
  SHIP

## Slide 15: n_TOF
CERN’s 20kW neutron spallation source!
  White neutron source, natPb based
  TOF experiment, 3800 hours operation
  20 GeV/c proton, 8.5*1012 p/spill, 7 ns spill
Pb
Neutron window
Neutron window material budget is <3 mm
  Material selection extremely important
    EN AW-5083-H111
  Water chemistry control
    O2, r, pH

## Slide 16: n_TOF target operation
Cooling circuit:
  H2O flow, 6 m3/h demineralized water
Separated moderator circuit
  1.28% 10B enriched water, 0.5 m3/h
  Nuclear-grade cationic resin IRN9882

## Slide 17
O2 content maintained <80 ppb
Conductivity at 0.045 mS/cm (ultra-pure water!)
  Maintained by purified N2 flush via a Liqui-Cel® membrane
Constant boron concentration maintained by a recirculating box at low temperature
  Conductivity ~60 mS/cm
  Boron crystal formation @end of run

## Slide 18: n_TOF material selection
Unavoidable galvanic contact between Pb and Al alloys
Dedicated analyses allowed to quantify max. of 6 mm/y (~50 mm/y for 10B circuit) for AW5083-H111
  Thanks to water chemistry control
Erosion/corrosion of 99.99% Pb significant
  ~900 mm/y average
4
b
a
Material test bench

## Slide 19: n_TOF target inspection
External inspection performed in April 2014
Only surface oxidation stains have been observed, due to humid atmosphere
COMPLETE ANALYSIS ONGOING

## Slide 20: Antiproton Decelerator (AD)
Antiproton production for CERN’s antimatter physics
  ELENA ring under construction (100 keV pbars)
  Operation foreseen for the next 20 years
26 GeV/c primary beam
0.5x1mm 1s
1.5*1013 p/pulse
430 ns pulse length
Rep rate ~60 s
Iridium core

## Slide 21: Antiproton Decelerator (AD)
Consolidation of target area until 2018, including the construction of a new optimized production target
Requirements for physics:
  Compact target
  High-Z material
  Very focused primary beam
Point-like source of p-bars for the magnetic horn
Challenges:
  Thermal shocks can damage target material
  Extremely high energy density coupled with short pulse
    7.5 kJ/cm3/pulse
    ~17 GJ/cm3/s

## Slide 22: Antiproton Decelerator (AD)
2000 °C in <0.5 ms
Temperature gradient of 1500 °C in <1.5 mm
Dynamic stresses ~10 GPa
Strain rates 4*104 s-1
Hydro codes being used to fully simulate plastic wave propagation
  Material strength beyond plasticity
  Material damage and failure
Pulse time influences dramatically the dynamic response
Experimental tests under proton beam is necessary
  Validate numerical results & gain experimental insights on material response
HiRadMat tests foreseen in 2015

## Slide 23: ISOLDE
On-line Isotope Mass Separator (ISOLDE)
  Facility dedicated to the production of radioactive ion beams
Class-A labs
Target area
Experimental Hall

## Slide 24: ISOLDE targets
Different target materials employed
  UCx, SiC, Pb, Ta, Ti, MgO, CeO
  ~30 units produced and operated per year
  Remote handling and monitoring
Lots of development going on
ISOLDE beam parameters:
  0.8-2.4*1013 p/pulse @1-1.4 GeV/c
  1.4-5.7 kW
  2.4-40 ms pulse, 1.2 cycle
See talks of M. Delonca, A.-P. Bernardes on LIEBE project

## Slide 25: SHIP – Search for Hidden Particles
New proposal at CERN aiming for a new fixed target experiment searching for very weakly interacting and longlived particles ~O(MeV-GeV)
  http://arxiv.org/abs/1310.1762
  Production through mesons decays (p, K, D, B)
  Need a heavy target to minimize background
~530 kW @400 GeV/c
Slow extraction (~few seconds)
High intensity (4.5-7.0*1013 p/pulse)
R. Jacobsson (CERN)

## Slide 26
W-based target
  Inermet® and Densimet ® alloys being investigated
  Target must be segmented to withstand beam power
Preliminary
Preliminary
~1 GPa compressive stresses
Challenges:
  High water flow rate (~10 m/s)
    Corrosion/erosion - Water chemistry
  High compressive stresses due to pulsed beam
  R&D on material properties, degradation of properties with radiation (RaDIATE?)

## Slide 27: Conclusions
Fixed target experiments a backbone of CERN’s programs
Several different operating target stations
Consolidation programs ongoing
New challenging projects are being proposed

## Slide 29: North Area targets