## Slide 1: SQXF Coil Design and Fabrication Winding and Curing
Miao Yu
February 17, 2014

## Slide 2: Outline
Introduction
QXF Coil Design
  Coil Cross-section
  Coil Layout
  Coil Pole and End Parts
QXF Coil Fabrication-Winding and Curing
  Winding and Curing Tooling
  Winding and Curing Procedures (Traveler)
  Winding Test
Summary

## Slide 3: Introduction
Based on LARP successful R&D Quadrupole coil TQ/LQ/HQ/LHQ experience.
  Coil parts design (BEND program)
  Tooling design
  Fabrication technology and procedure (winding – curing – reaction – impregnation)
  Coil size control at each fabrication step (insulation and shim) to reach the final coil size
To meet CERN’s requirement
  Field quality (x-section and end design)
  Magnetic length (coil length)
  Electrical requirement (plasma coating of metallic end parts)
  Heat extraction (cooling channels in coil pole)

## Slide 4: QXF Coil Design - Coil Cross-section
Magnetic design
Fabricated Coil
Backup slides:
Coil cross-section at each step
for ground insulation

## Slide 5: QXF Coil Design - QXF Coil Layout
Cooling channel
RE
LE
1.51 m
Ti-6Al4V pole and bronze wedge: used for LQ/HQ/LHQ.
Stainless steel end spacer, saddle and splice block: used for HQ/LHQ.
LQXF is 4.3 m long by adding 7 more center pole pieces.

## Slide 6: QXF Coil Design - Coil Pole
> 80 % of the heat is evacuated via the pole piece with Φ8 mm holes and 50 mm spacing
Strain Gauge

## Slide 7: QXF Coil Design - Coil End Spacer and Saddle
End parts are designed based on the nominal coil size after coil reaction
During winding, the coil is not fully constrained inside the envelope. This effect is most pronounced at the ends. Prior to curing, the cable separates from radial surface of the mandrel in these areas (springback), causing the shape of the turn to not match the shape of the end parts.
The springback is larger with larger coil aperture and cable size.
Therefore flexible features (slits) have been introduced in LHQ and QXF coil.
  Incremental change with respect to single slit design previously used.
End parts are plasma coated to increase the dielectric strength.
temporary saddle during W&C
QXF slits design with bridges

## Slide 8: QXF Coil Fabrication - SQXF Winding and Curing Tooling Design
Rollover Station
Curing Mold
Coil Inner Layer
Winding

## Slide 9: QXF Coil Fabrication - SQXF Winding and Curing Tooling Design
Rollover Station
Curing Mold
Winding
Coil Outer Layer

## Slide 10: QXF Coil Fabrication - Winding and Curing Tooling
Tooling for SQXF coil was inspected and assembled.
Winding and Curing Tooling
Rollover Fixture
Curing Mold

## Slide 11: QXF Coil Fabrication - LQXF Winding and Curing Tooling
The design of LQXF W&C tooling was finished
Procurement will start this summer
Curing mold
348” long
5 sections (2: 66” and 3: 72”)
Stacking, welding and inspection
Final assembly and inspection
Use the same rollover fixture for SQXF
Winding table will be tested in April
Selva winder will be commissioned by this Dec

## Slide 12: QXF Coil Fabrication - Winding and Curing Procedures (Traveler)
Online version based on HQ/LHQ winding and curing traveler
Typically, it takes 15 days for winding and curing

## Slide 13: QXF Coil Fabrication - Winding Test
Cured Coil
Coil Winding
Reduce the risk of turn-turn short due to popped strands
Two 1 m coils, winding-curing
End parts inspection and design optimization
  Pre-check tooling and W&C procedures
  Fabrication of SQXF coils is starting this February

## Slide 14: Summary
QXF coil is designed based on HQ/LHQ coil experience
Tooling is ready for SQXF coil winding and curing
LQXF coil winding and curing tooling will be procured this summer.
Winding and curing procedures are based on HQ/LHQ coil procedures
SQXF coil fabrication is starting this month.

## Slide 15: Backup Slides - Coil Size at Each Step

## Slide 16: IL Winding and Curing
Midplane
760 µm (30 mil) =
3 layers 10 mil Mylar
250 µm
(10 mil)
1.5 mm (60 mil)
Curing Retainer
250 µm (10 mil)
SS shim
Curing Shell
OR: 113.126 mm
IR: 94.168 mm
250 µm (10 mil) Mylar + 100 µm (4mil) shrink wrap

## Slide 17: OL Winding and Curing
Midplane
OR: 113.126 mm
760 µm (30 mil) =
100 µm shrink wrap + 660 µm SS Shim
250 µm
(10 mil)
1.5 mm (60 mil)
Curing Retainer
250 µm (10 mil)
SS shim
250 µm (10 mil)
SS shim

## Slide 18: Coil Reaction
125 µm (5 mil)
MICA
125 µm (5 mil )
MICA
125 µm (5 mil)
MICA
125 µm (5 mil)
MICA
Midplane
250 µm (10 mil)
S2 glass
125 µm (5 mil)
MICA
125 µm (5 mil)
MICA

## Slide 19: Coil Impregnation
150 µm (6 mil)
S2 glass
100 µm (4 mil )
Polyimide trace
150 µm (6 mil)
S2 glass
100 µm (4 mil)
Polyimide trace
250 µm (10 mil)
MYLAR
(mold released, removed after impregnation)
125 µm (5 mil)
MYLAR
(mold released, removed after impregnation)
125 µm (5 mil)
G11
Midplane
RTV (removed after impregnation)