## Slide 1: MQXF Quench Protection
G. Ambrosio
02/17/14

## Slide 2: Outline
Status at MT23 (First complete analysis)
Recent progress
Plans

## Slide 3: Status at MT23
Simulations performed with QLASA and ROXIE using MATPRO material property database
  Using preliminary MQXF requirements
  Assuming heaters only on the outer layer
  With conservative assumptions:
    Layer-layer propagation
    Impact of bronze in strands
    No dynamic effects
Hot spot temp. ~ 350 K
  Without margin and redundancy
  Close to epoxy glass transition temperature
    ~max acceptable temp. if there is no earlier detraining

## Slide 4: “Bubbles” Issue
“Bubbles” on coils inner surface
  Coil-insulation separation
  Heater-coil separation
Seen in TQ, LQ, HQ coils only non inner layer
  TQ coils showed small “bubbles” (no heaters on IL)
  HQ coils showed small “bubbles” and cracks along heaters
  LQ coils had long “bubbles”
LQ coil
HQ coil

## Slide 5: Progress so far
Demonstrated beneficial effect of bronze
   Hot spot temperature lower by ~ 30K
Compared property databases
   MATPRO is most conservative
Performed QP tests on HQ
  Next slides
Compared HQ test data with simulations (using MT23 assumptions)
  Next slides

## Slide 6: Feedback from HQ02 test
Measurement of quench propagation from Outer Layer to Inner Layer
Measurement of Quench Integral with different dump resistors
  simulating MQXF conditions

## Slide 7: Simulations vs. Measurements
Under the assumptions used for MQXF, the heaters-induced quench simulations are conservative.
At the current of interest (0.8 of SSL), the MIITs are overestimated by about 13 % (~ 65 K)
Margin is due to:
  dI/dt effects
  conservative assumptions in modeling of heaters and propagation OL to IL
Current/SSL | 0.8 | 0.7 | 0.6 | 0.5 | 0.4
MIITs difference % (no dump case) | 14.5 | 13.2 | 9.6 | 10.7 | 8.1
MIITs difference % (3 mΩ dump case) | 13.4 | 11.1 | 6.4 | 5.3 | 0.9
Most significant case for MQXF

## Slide 8: Plans
The recent improvements may not be sufficient to provide redundancy and margin
  This is a risk, therefore:
We are addressing it by:
  Optimization of heater design and materials
  Development of heaters for Inner Layer w/o bubbles
  Exploring the use of CLIQ
    Coupling Loss Induced Quench
  Test max acceptable temperature (HQ02b)
Longer magnets with lower gradient are the back up solution (with several drawbacks)

## Slide 9: CLIQ
Developed at CERN for 120mm NbTi quads
May be an option for MQXF
Note: most effective on inner layer
Complementary to heaters on outer layer
To be tested on HQ02b

## Slide 10: Heater development
Pattern optimization
  LHQ coil test
  HQ03 (MQXF style heaters)
Material optimization
  Reduce heater delay time
Minimization of polyimide coverage of coil inner surface using copper plated heaters
  Better heat extraction
  Avoid bubbles

## Slide 11: Conclusion
Quench Protection is the only part of the design that still needs some R&D
We are aware of this risk and are addressing it intensively developing alternative solutions in collaboration with CERN
A workshop is planned after HQ02b test to assess QP and finalize MQXF lengths
  Temptative time: end of April

## Slide 12: Back up Slides

## Slide 13: Coils after Test
Some “bubbles” on coils inner layer
  Coil-insulation separation
Possible causes:
  Superfluid helium and heat during quench
    Seen in TQ coils
  Heat from heaters on inner layer
    Only in LQ coils
Plans:
  Strengthen insulation or
  Change heater location or
  Add support on coil ID

## Slide 14: Coil Processing: Impregnation
Instrumentation traces
  Do laminated polyimide trace materials pose problems for impregnation?
  Trace behavior (bubbles) on inside bore after testing cycle have continued
Bubbles on inside bore of
LQS03 after magnet test
Inside bore of HQ02a during
assembly (Coil 15 was previously
tested in HQ mirror)