## Slide 1: Rapid Cycling Dipole Magnet

## Slide 2: Overview
RCS Dipole Design
Materials
Losses
Performance
Engineering
Why do it this way?

## Slide 3: Magnet Geometry
Gap: 25 mm
Pole width: 120 mm
Good field region
  Horizontal: 60 mm
  Vertical: 10 mm
  Aperture: 60x25 mm2
Geometry
  Allows to use two different materials
Combine advantages of materials
  Pole: 3% SiFe (FeCo)
  Yoke: 6.5% SiFe
3% SiFe
6.5% SiFe
Coil
645 mm
463 mm

## Slide 4: Materials
6.5% SiFe
  Low losses at high frequencies
  High permeability
  Low saturation
3% SiFe
  Higher saturation
  Higher losses
J. Degauque and F. Fiorillo. Alliages magnétiques doux enrichis en silicium. Matériaux magnétiques en génie électrique 1, A. Kedous-Lebouc (ed.), Lavoisier, Chapter 4, pp. 227-286, 2006.

## Slide 5: Losses – Frequency Effects
Loss mechanisms
  Hysteresis + eddy current losses
  Anomalous loss
Effect of frequency
  All losses increase…
  (includes Hysteresis)
Deformation of hysteresis loop
Need measured data
  Core loss data available
From: Energy Savings with Thin Gage. Steve Constantinides, Arnold Technologies, 2009.

## Slide 6: Materials - Core Losses

## Slide 7: Coil
Eddy current losses
  Conductor shape
Conductor geometry
  Copper sheets
  80 mm wide, 1 mm thick
  Insulation: 25 μm thick
Coil position
  Field leakage from yoke
  Optimized to minimize dB/dt
Losses: evaluated using FEA
  750 kW for all dipoles in ring (1.5T, 2.2 km length)
  1 kHz pulse, 15 pulses per second
Cu sheet
Kapton
?

## Slide 8: FEA: Eddy Current Simulation
Technique developed ~10a ago
Pulsed high field magnets (60-100T)
  Normal conducting solenoids
  10 ms pulse
  Operate at 77K
  DOI:10.1109/TASC.2005.864485
Verified experimentally
Herlach et al. DOI:10.1109/TASC.2005.864269

## Slide 9: Total Power Loss

## Slide 10: Field Quality
Dipole field: 1.53T
Gap: 25 mm

## Slide 11: Engineering
Courtesy of Paul Kovach
BNL Magnet Division
240 kN
Imax=15 kA
W = 3.65 kJ/m

## Slide 12: Cooling Excitation Coil
Coil
  350 W/m in total (1.5T)
  Cooling: outer faces
  q < 0.1 l/s
Finite element simulations
  Temperature gradient: <1K

## Slide 13: Cooling Yoke
6.5%SiFe
3%SiFe
Total average power dissipation: 820 W/m
20 W/kg
80 W/kg

## Slide 14: Heating Core
ΔT<8K
Worst case: all heating in pole
  q < 0.3 l/s

## Slide 15: Yoke 3% SiFe?
80%
80%
How much worse is a yoke made of 3% SiFe?

## Slide 16: Power Loss
1 MW
30% difference
(yoke)

## Slide 17: Comparison SiFe

## Slide 18: Power Supply
Required: 8m long dipoles
Challenge: voltage
Minimize inductance: 4 PS per dipole
Magnetic energy: 3.65kJ/m
AC voltage: 650 V/m (assuming 15 kA PS)

## Slide 19: Superconducting Option
Wall plug power superconducting version?
How good does a SC dipole have to be?
Break even for SC version: 1.3W/m
  Normal conducting loss: 800 kW (2.2 km)
  P300K = 360 W/m
  P4K: 1.3W/m (Carnot efficiency 280)
Additional heat losses
  Power leads: P4K = 3-5 W (20 kA lead, CERN/NHMFL)
  Power loss conductor

## Slide 20: Conclusion
Concept of dipole magnet
  Combines strength of two materials
Performance
  Good field quality up to 1.5T
Power losses
  Acceptable losses at 1000Hz (1.5T: 2.75 MW for ring)
Engineering concept
  External clamp to deal with forces
  Cooling seems manageable

## Slide 21: Acknowledgements
The authors would like to acknowledge fruitful discussion and support from
  Carsten Bach, Vacuumschmelze
  Hironori Ninomiya, JFE Steel Corporation
  Rob Riley, Fermilab
  Don Summers, University of Mississippi
  John Zweibohmer, Fermilab

## Slide 22: Additional Slides

## Slide 23: Multipole Components
3D Finite Element Simulation
  Time-harmonic
Evaluated for 1.5/0.75T
Table: normalized multipole components
Field quality not affected by eddy currents
N | 1 Hz | 50Hz | 400Hz
1 | 10000 | 10000 | 10000
2 | 0.00000 | 0.00000 | 0.00000
3 | -0.00021 | -0.00021 | -0.00021
4 | 0.00000 | 0.00000 | 0.00000
5 | 0.00000 | 0.00000 | 0.00000

## Slide 24: Activation
Muons decay into electrons
Showers can produce neutrons that activate cobalt
  Half-life 60Co: 5.27 a
  60Co→ 60Ni+e-+ν+γ
  γ: 1.17/1.33 MeV
Decays occur in the midplane, avoid pole
Need simulations to determine activation
  Need to design shielding to minimize activation
  Determine whether residual activation is operationally tolerable

## Slide 25: Rapid Cycling Synchrotron
Final acceleration Muon Collider: RCS
  Interleaved cold and warm dipoles
Warm dipoles: correct average bend field
  must change rapidly (>400 Hz)
Maximum warm dipole field: significant impact
  Larger energy range
  Higher maximum energy
  Shorter circumference
  Fewer accelerator stages