## Slide 1: Low radioactivity argon from underground sources
Henning O. Back – Princeton University
LArTPC14

## Slide 2: Pulse shape
Grosjean, Vidal, Baragiola, And Brown, Phys. Rev. B 56 (1997) 6975-6981
Excited Ar dimer has 2 lowest energy states
  Singlet
    lifetime ~ 7 ns
  Triplet (forbidden decay)
    Lifetime ~1.6 μsec
  States populated differently depending on ionization density
Allows for pulse shape discrimination

## Slide 3: Pulse shape for different radiation
Hitachi, et al., Phys. Rev. B 27 (1983) 5279

## Slide 4: Pulse shape for nuclear recoils
Boulay and Hime, Astropart. Phys. 25 (2006) 179
Dark matter will only scatter off of argon nucleus
Recoiling nucleus cause argon excitation and ionization

## Slide 5: Atmospheric Argon Limit
Atmospheric Argon (AAr) | Underground Argon (UAr)
Contain beta emitter 39Ar at a concentration of 8x10-16 Radioactivity of AAr = 1 Bq/kg | Concentration of 39Ar is at least 150 times less than AAr Radioactivity of UAr < 7mBq/kg

## Slide 6: Terrestrial argon sources As I understand them
40Ar comes from 40K decay
Atmosphere
  39Ar produced by cosmic ray neutrons
  40Ar(n, 2n)39Ar
Crust
  No cosmic ray
  Neutrons from U and Th
Mantle
  Very low U and Th
  Lowest 39Ar levels
Mantle
Low U and Th
(lowest 39Ar)
Crust – 1ppm U and Th (low 39Ar)
Atmosphere (8×10-16 39Ar/40Ar)

## Slide 7: CO2 well in SW Colorado
There are geological formations that trap gases underground
We found CO2 well in SW Colorado (near Cortez)
Contains 600 ppm Argon
39Ar activity < 0.65% of atmospheric argon
(arXiv:1204.6011)

## Slide 8: Low-radioactivity Argon is a National Resource
Sole supplier of UAr to programs requiring low radioactivity argon
  Dark matter
    Darkside
    DEAP
  Low-level radioactivity detection
    Argon radiometric dating (calibration gas)
      Argonne – ATTA
      Heidelberg, Germany – ATTA
      Bern, Switzerland – gas proportional counters(?)
    National Security
      PNNL – gas for proportional counters
Radio-dating gas samples
Our gas – 10 racks 4000 psi each
Inches
Feet

## Slide 9: Getting to the argon
Extraction
  In Colorado we extract a crude argon gas mixture (Ar, N2, and He)
Purification
  The gas from Cortez is then sent to Fermilab for further purification

## Slide 10: Absorption of CO2 on 4A zeolite
Siriwardane et al., Energy & Fuels, Vol. 17, No. 3, 2003
VPSA range
0-1.7 bar

## Slide 11: Vacuum Pressure Swing Absorption (VPSA)
Capitalize on pressure dependence of absorption
Absorb CO2 under pressure
Regenerate column under vacuum
Use 2 columns for (near) continuous operation
Gas delivered to FNAL
  He – 85-95%
  N2 – 0.1-10%
  Ar – 5%
He, Ar, N2 mixture
Gas from well
Absorbed gas returned to company
Zeolite column
Zeolite column
Gas flows through one column under pressure. CO2, O2, H2O and CH4 are absorbed on zeolite
Simultaneously the other column is pumped on to remove the trapped gases

## Slide 12: Our plant
Gas heaters
First stage
Second stage
Warms gas to avoid liquefaction by to Joule-Thomson cooling
(total ΔP > 750 psi)
Absorbs CO2 and other unwanted gases
Allows Ar, He, and N2 to pass
Reduces N2 content

## Slide 13: VPSA plant
Operated locally by technician Chris Condon – Managed by H. Back

## Slide 14: Purification at FNAL
Great Initial Success
First commissioning with atmospheric argon (from Airgas)
  input mix: 6% Ar, 55% He, 44% N2
  output: 100% Ar, <500ppm N2
Waste
Cryogenic Distillation Column (CDC)
Input
Product
Booster
Transportation cylinder racks
The 2010 plan – commissioned Oct. 2011

## Slide 15: Purification at Fermilab The Cryogenic Distillation Column
Column is filled with high surface area material
Boiling and condensation happens on the surface of column packing material
Controlling temperature and gas/liquid flows allows for continuous purification
Inject liquefied Ar/N2into column
Waste gas (He and N2)
Product (pure Argon)
Lower boiling point gas preferentially moves up column
Higher boiling point liquid preferentially moves down column
Packed column
Temperature gradient
5.5 cm
Column packing material

## Slide 16: Distillation Column
2 – 600W cryocoolers
  Balanced with 700W heaters for temperature control
Reboiler cooled by liquid from column
  Temperature controlled with 700W heater
Active PID temperature control
Active mass flow control
Pressure and temperature monitoring throughout
Multiple input RGA measures gas at three points
  Column Input
  Condenser Output (column top)
  Reboiler Output (column bottom)

## Slide 17: First Underground Argon (UAr) purification
Processed 500k liters gas (at STP)
Reached 99.7% pure argon
Issues:
  Gas flow stopped abruptly – Clogging from impurities
  Different gas mix stalled distillation – High He content
  Very slow – Not enough cooling
  Never reproducible – Not without large UAr losses
  Column flooding – Column too small

## Slide 18: Plant Expansion
1) Briefly summarize the current state of the program, discussing what has been learned and what are the remaining issues.

## Slide 19: Plant systems
Helium Separator
Waste Stream Argon Capture
Contaminant Freeze Out
Distillation
1) Briefly summarize the current state of the program, discussing what has been learned and what are the remaining issues.

## Slide 20: Plant systems simplified
Waste
Condenser Booster Helium Separator
(CB)
Input
Product
Waste
CB
Charcoal Trap
(CBCT)
Input
Product
Waste
CDF Organics Cold Traps
Input
Product
Reboiler
Cryogenic Distillation Column (CDC)
Input
Vent
Vent
pumped out
Buffer Volume
Transportation cylinder racks
Booster
Condenser
Booster
Product
Storage

## Slide 21: Condenser Booster Helium Separator
Pressurize Booster with Ar-He-N2 mixture
Cool with LN2
Ar and N2 condense
Remaining pressure is He, which is then vented
Pumping on LN2 drives down temperature below 77K

## Slide 22: Argon collection efficiency
Condenser booster pressurized to 2600 psi (175 bar) = ~3500 L @ stp
Operation at 77K
  Ar vapor press. at 77K = 0.3 bar
  Ar concentration in 175 bar He at 77K = 0.17%
  Input gas = 5% argon
  Argon lost = 3.4%
Operation at 65K (subatmospheric LN2 jacket)
  Ar vapor press. @ 65K = .035bar
  Ar concentration in 175 bar He at 65K = 0.02%
  Input gas = 5% Ar
  Ar lost = 0.4%

## Slide 23: Recovering Ar in waste streams
Argon is lost in the waste streams of the Condenser Booster
Argon traps readily on charcoal at LAr temps

## Slide 24: Solidifying impurities
Residual impurities solidified in the Column
Impurities are below the sensitivity of the VPSA RGA
Need to remove impurities before reaching the column
Contaminant | Concentration (v/v) | After 500,000 standard liter of gas |  | 
 |  | contaminants | gas vol. | Liq./solid vol.
H2O | 25 ppm | 61.2 ppm | 30.6 L | >30 mL
CO2 | 30 ppm |  |  | 
CH4 | 1.4 ppm |  |  | 
Isopentane (C5H12) | 3.0 ppm |  |  | 
N-pentane (C5H12) | 1.8 ppm |  |  | 

## Slide 25: CDF cold traps
Originally used to remove alcohol from argon/ethane mix
Repurposed to remove our residual contaminants

## Slide 26: Improved condensation efficiency
Cryocooler
Copper heater
Copper sealing flange
Copper heat exchanger
Cryocooler
Copper heater
Copper flange + heat exch.
Original configuration
Surfaces only bolted together
Too many interfaces
Improvements
Surfaced thermally couple with grease
Heat exchanger integrated into sealing flange
2-600W
condensers
We have always struggled with condensation efficiency
Assumed that it was due to the helium
Troubles persisted even after removing helium from gas
After thermal conductivity upgrades 1 condenser can truly condense at full power of cryocooler (600W @ 80K)
600W cooling equivalent to about 100 slpm of argon

## Slide 27: 80 mm separation column
Original column (2 cm) was too small
With improved condensation efficiency we were producing more liquid than could flow down column (flooding)
Included better temperature monitoring inside packing material
Added differential pressure transducers along column to check for flooding

## Slide 28: Commissioning 80 mm Column
waste
feed
product
No UAr losses in Distillation Column
UAr/N2 < 10-4

## Slide 29: New Column Distillation
RGA N2 limit
~300 ppm
Final cylinder consumed at hour 11:25
RGA N2 limit reached about 12 hours after final cylinder consumed

## Slide 30: Distillation product
UAr
N2
O2
N2/UAr <300ppm (RGA limit)
He/Uar <~10ppm (RGA limit)

## Slide 31: The 2014 issues
In-depth accounting relieved significant losses
  Thought we had 200 kg, only had 113kg
  Inaccurate gauge (-2.5%)
  Compressibility factor (-15%)
  Real losses in purification commissioning plants
Methane contaminated gas (from early VPSA operations)
  Actually an old problem
  BUT, needed to recover this gas to make up for losses
Oxygen contaminated gas
  Increased production at VPSA plant to make up for losses
  Production increase came with Oxygen contamination

## Slide 32: Compressibility Factor - PV=nRTZ for 5% Ar, 7% N2, 88% He
Chart: Pressure (psig)
~pressure of our cylinders
For cyl. with this mix, there is 11.5% less than than PV=nRT tells you

## Slide 33: Distilling Methane from Argon
Chart: Vapor pressure versus temperature (Antoine equation parameters from NIST)
| 84.0 | 85.0 | 86.0 | 87.0 | 88.0 | 89.0 | 90.0 | 91.0 | 92.0 | 93.0 | 94.0 | 95.0 | 96.0 | 97.0 | 98.0 | 99.0 | 100.0 | 101.0 | 102.0 | 103.0 | 104.0 | 105.0 | 106.0 | 107.0 | 108.0 | 109.0 | 110.0 | 111.0 | 112.0 | 113.0 | 114.0 | 115.0 | 116.0 | 117.0 | 118.0 | 119.0 | 120.0 | 121.0 | 122.0 | 123.0 | 124.0 | 125.0 | 126.0
Argon | 0.64691 | 0.73512 | 0.83203 | 0.93811 | 1.0539 | 1.1798 | 1.3164 | 1.4641 | 1.6234 | 1.7948 | 1.9788 | 2.1758 | 2.3862 | 2.6106 | 2.8493 | 3.1027 | 3.3713 | 3.6554 | 3.9554 | 4.2717 | 4.6046 | 4.9545 | 5.3216 | 5.7063 | 6.1089 | 6.5296 | 6.9686 | 7.4263 | 7.9029 | 8.3985 | 8.9134 | 9.4477 | 10.0017 | 10.5754 | 11.1689 | 11.7825 | 12.4162 | 13.0701 | 13.7443 | 14.4389 | 15.1538 | 15.8892 | 16.6451
Nitrogen | 2.0757 | 2.2876 | 2.515 | 2.7585 | 3.0188 | 3.2964 | 3.592 | 3.9061 | 4.2394 | 4.5925 | 4.9659 | 5.3602 | 5.776 | 6.2137 | 6.674 | 7.1574 | 7.6643 | 8.1952 | 8.7507 | 9.3311 | 9.9369 | 10.5686 | 11.2266 | 11.9112 | 12.6229 | 13.362 | 14.1288 | 14.9237 | 15.747 | 16.599 | 17.48 | 18.3902 | 19.3299 | 20.2993 | 21.2987 | 22.3282 | 23.3881 | 24.4784 | 25.5994 | 26.7512 | 27.9339 | 29.1477 | 30.3925
Methane | 0.048352 | 0.055871 | 0.064342 | 0.073855 | 0.084509 | 0.096405 | 0.10965 | 0.12437 | 0.14067 | 0.15868 | 0.17854 | 0.20039 | 0.22436 | 0.25062 | 0.27931 | 0.31061 | 0.34467 | 0.38168 | 0.42182 | 0.46526 | 0.51221 | 0.56286 | 0.61742 | 0.67609 | 0.73908 | 0.80662 | 0.87892 | 0.95622 | 1.0387 | 1.1267 | 1.2204 | 1.3201 | 1.4259 | 1.5382 | 1.6572 | 1.7831 | 1.9163 | 2.057 | 2.2054 | 2.3618 | 2.5265 | 2.6998 | 2.8819
Greater boiling point separation between Ar-Ch4 than N2-Ar
Distillation should be easier

## Slide 34: Methane contaminated gas recovery
Ar, N2, & CH4
N2
Waste
Ar & CH4
Ar & N2
Storage
Ar & CH4
Ar
Product
CH4
Distill in our “normal” configuration
Input UAr & N2 with a CH4 contamination.
Vent N2 and collect UAr with CH4 contamination in reboiler
Once we have vented as much N2 without losing UAr, we start collecting the UAr/N2 mix into storage until all the N2 is gone
We then collect the pure UAr until CH4 starts moving up the column.

## Slide 35: Methane contaminated gas recovery Gas analysis
Gas analysis during UAr collection
  UAr – 99.96%
  N2 < 200 ppm (RGA limit)
  CH4 < 5ppm
  CO2 - 166 ppm (?)
Waiting for profession analysis
Collection of UAr
RGA gas scan of Distillation Column Condenser Output

## Slide 36: What we’ve achieved to date
Total Mass waiting for purification = 48.9 --- Total Purified Mass = 87.6 kg
TOTAL UAr MASS – 136.5 kg
152 kg required for Darkside50
Not available = waiting for results.
Cylinder | Mass | Ar | N2 | O2 | CH4 | CO2
UAr#2 | 6.6 kg | 99.97% | 240 ppm | 80 ppm | < 10 ppm | < 10 ppm
UAr#3 | 10.7 kg | 99.993% | 30 ppm | < 10 ppm | 40 ppm | < 10 ppm
UAr#4 | 10.7 kg | 99.917% | 30 ppm | 740 ppm | 60 ppm | < 10 ppm
UAr#5 | 10.7 kg | 99.944% | 30 ppm | 420 ppm | 110 ppm | < 10 ppm
UAr#6 | 10.7 kg | 99.956% | 50 ppm | 250 ppm | 120 ppm | 20 ppm
UAr#7 | 9.2 kg | Not avail. | Not avail. | Not avail. | Not avail. | Not avail.
UAr#8 | 8.0 kg | Not avail. | Not avail. | Not avail. | Not avail. | Not avail.
UAr#9 | 12.9 kg | Not avail. | Not avail. | Not avail. | Not avail. | Not avail.
UAr #10 | 8.1 kg | Not avail. | Not avail. | Not avail. | Not avail. | Not avail.
recovered from CH4 contamination

## Slide 37: Oxygen contamination (new problem)
With increased productivity at VPSA plant in Colorado came an oxygen contamination
Distillation difficult due to similar boiling point as Argon
Working with consultant to identify solution
Current plan:
  Copper getters can absorb as high as 10s of grams of Oxygen per kg of catalyst
  Plant will be big enough to process all Darkside50 gas without regeneration
  However, regeneration capabilities will exist
Chart: Vapor pressure versus temperature (Antoine equation parameters from NIST)
| 84.0 | 85.0 | 86.0 | 87.0 | 88.0 | 89.0 | 90.0 | 91.0 | 92.0 | 93.0 | 94.0 | 95.0 | 96.0 | 97.0 | 98.0 | 99.0 | 100.0 | 101.0 | 102.0 | 103.0 | 104.0 | 105.0 | 106.0 | 107.0 | 108.0 | 109.0 | 110.0 | 111.0 | 112.0 | 113.0 | 114.0 | 115.0 | 116.0 | 117.0 | 118.0 | 119.0 | 120.0 | 121.0 | 122.0 | 123.0 | 124.0 | 125.0 | 126.0
Argon | 0.64691 | 0.73512 | 0.83203 | 0.93811 | 1.0539 | 1.1798 | 1.3164 | 1.4641 | 1.6234 | 1.7948 | 1.9788 | 2.1758 | 2.3862 | 2.6106 | 2.8493 | 3.1027 | 3.3713 | 3.6554 | 3.9554 | 4.2717 | 4.6046 | 4.9545 | 5.3216 | 5.7063 | 6.1089 | 6.5296 | 6.9686 | 7.4263 | 7.9029 | 8.3985 | 8.9134 | 9.4477 | 10.0017 | 10.5754 | 11.1689 | 11.7825 | 12.4162 | 13.0701 | 13.7443 | 14.4389 | 15.1538 | 15.8892 | 16.6451
Nitrogen | 2.0757 | 2.2876 | 2.515 | 2.7585 | 3.0188 | 3.2964 | 3.592 | 3.9061 | 4.2394 | 4.5925 | 4.9659 | 5.3602 | 5.776 | 6.2137 | 6.674 | 7.1574 | 7.6643 | 8.1952 | 8.7507 | 9.3311 | 9.9369 | 10.5686 | 11.2266 | 11.9112 | 12.6229 | 13.362 | 14.1288 | 14.9237 | 15.747 | 16.599 | 17.48 | 18.3902 | 19.3299 | 20.2993 | 21.2987 | 22.3282 | 23.3881 | 24.4784 | 25.5994 | 26.7512 | 27.9339 | 29.1477 | 30.3925
Methane | 0.048352 | 0.055871 | 0.064342 | 0.073855 | 0.084509 | 0.096405 | 0.10965 | 0.12437 | 0.14067 | 0.15868 | 0.17854 | 0.20039 | 0.22436 | 0.25062 | 0.27931 | 0.31061 | 0.34467 | 0.38168 | 0.42182 | 0.46526 | 0.51221 | 0.56286 | 0.61742 | 0.67609 | 0.73908 | 0.80662 | 0.87892 | 0.95622 | 1.0387 | 1.1267 | 1.2204 | 1.3201 | 1.4259 | 1.5382 | 1.6572 | 1.7831 | 1.9163 | 2.057 | 2.2054 | 2.3618 | 2.5265 | 2.6998 | 2.8819
Oxygen | 0.49469 | 0.55847 | 0.6286 | 0.70551 | 0.78967 | 0.88151 | 0.98152 | 1.0902 | 1.208 | 1.3354 | 1.473 | 1.6213 | 1.7807 | 1.9519 | 2.1354 | 2.3317 | 2.5413 | 2.7649 | 3.003 | 3.2562 | 3.525 | 3.8099 | 4.1117 | 4.4307 | 4.7677 | 5.1231 | 5.4975 | 5.8915 | 6.3056 | 6.7404 | 7.1965 | 7.6743 | 8.1745 | 8.6976 | 9.244 | 9.8144 | 10.4092 | 11.0289 | 11.674 | 12.3451 | 13.0425 | 13.7669 | 14.5186

## Slide 38: Final Gettering
UAr requires final polishing to become detector grade
Using heated Zirconium getters from SAES
We will run all the UAr through the getters at one time
System build, waiting for control system
Plan to retrofit Oxygen scrubber to this plant

## Slide 39: Verifying UAr detector usability
Could there be a contaminant that makes it through all purification steps and is below our sensitivity?
Verify our UAr can scintillate and drift e- - before putting into Darkside50
Propose to use Scene-LAr detector - Phys. Rev. D., 88, 092006 (2013)
  Uses 3-4 kg of UAr
  Need recovery system (use existing infrastructure)

## Slide 40: Schedule and conclusions
Schedule
  Final gas extracted in Colorado end of August
  He separation & N2 distillation completed end of Sept.
  Oxygen scrubbing mid Oct.
  Final getting completed end of Oct.
  Quality assurance test completed mid Nov. – ready to ship
Conclusions
  A reliable source of low-radioactivity argon has been established
  Extraction and purification of the UAr is possible on a large scale
  However, there have been issues along the way
  AND, we still have not shown that our UAr is detector grade

## Slide 41
BACK UP SLIDES

## Slide 42
Chart: Nitrogen:Argon ratio in the Product gas
| 40834.4097222222 | 40835.42638888889 | 40835.67638888889 | 40836.26666666661 | 40836.44791666666
N2/Argon | 0.014431 | 0.0036998 | 0.0027391 | 0.0011743 | 0.0010026
Consumed test gas
6 days from start
8.5 days from start
Argon purity = 99.9%

## Slide 43
Chart: Nitrogen:Argon ratio in the product gas

## Slide 44
Chart: Pure Argon RGA Spectrum
NOTE: Uncorrected pressures
Nitrogen/Argon = 4.3×10-4

## Slide 45
Chart: Distillation product compared to pure argon
Argon peaks
Nitrogen
Nitrogen
H2O background
Other backgrounds
Other backgrounds
Input gas:
5% Ar
40% N2
55% He
First Commissioning of Distillation Column