## Slide 1
Studies of Degradation of CMOS Devices at Cryogenic Conditions for the LBNE Electronics
Guoying Wu and Ping Gui
SMU, Department of Electrical Engineering, Dallas, TX USA
James Hoff and Grzegorz Deptuch
Fermilab, PPD/EED, Batavia, IL USA

## Slide 2: Motivation
In the LBNE, the integrated electronics for readout of the liquid argon (87 K) time projection chamber will be operated in cold for the duration of the experiment (more than 20 years)
Research and design of the highly reliable circuits with the capability of operating at low temperature and maintaining a more than 20-year lifetime is imperative
Focus on the operation of electronics in the liquid nitrogen (77 K) temperature because this temperature allows extensive tests conveniently in laboratory's conditions and allows comparison with prior literature data for older processes
The reliability investigation of single devices is the first step to the circuit design
The Accelerated-Stress test is the method to investigate the hot-carrier degradation of devices using minimum sample size and shortest test time (days to weeks)
    It is defined as test carried out under larger voltages than the nominal power supply condition
    The damage in a shorter time at stronger electric field can be related to the damage at weaker electric field in a longer time

## Slide 3: Hardware Setup for the Test
PCB with chip
NI PXIe-1085
Vacuum Pump & Compressor
Vacuum Chamber
Cryogenic vacuum chamber (built @ Fermilab in 2011)
National Instrument PXIe-1085 embedded controller (acquired in 2014) with 12 source-measurement units (3x4)
MOSFET transistors of different widths and lengths in 130nm and 65nm technologies are available to test
Cryocooler

## Slide 4: Software Setup for the Test
Procedure Used in the Lifetime Measurements
Labview program is developed to the new tests based on 4-point measurement for precision
Stress conditions of VGS=VDS and VGS=(1/2)VDS are utilized
  The degree of degradation is estimated using ID-VGS curves in the linear region, which is detected as the most severe degradation
  Transconductance (gm), drain current (IDS) and threshold voltage (VTH) are extracted to estimate the degradation level of devices

## Slide 5: Verifications of the Setup
I-V curves in the Cryostat and in LN Bath (for comparison)
Degradation f(time) in the Cryostat and in LN Bath (for comparison)
Setup operated safely, no ESD problems
Cross-check of operation inside cryostat and in liquid nitrogen
    Equivalent I-V curves of fresh devices
    Equivalent stress degradation curves

## Slide 6: Hot-Carrier Degradation--130 nm
Devices are tested for longer times than it was possible before (> 100 ks) and at lower stress voltages for more accurate predictions of lifetime
Tests include broad ranges of transistor dimensions (W & L)
Extraction of basic parameters (VTH, gm, ID) and their degradations are investigated---- guidelines for circuit design
10%
10%
Degradation vs time for transistor with different WIDTHS
Degradation vs time for transistor with different LENGTHS

## Slide 7: Lifetime Prediction--130 nm
The smallest length transistors at stress condition of VGS=VDS have the shortest lifetime (2µm/0.13µm transistor as an example)
  The width dependence of degradation at 77 K is not evident
  The degradation at stress condition of VGS=VDS is worse than that of VGS=(1/2)VDS for small length transistors (0.13 µm)
To get to the 20 years lifetime, the power supply voltage should be less than 1.49 V at the worst stress condition (Nominal supply=1.5V)
The lifetime predictions of the 2µm/0.13µm transistor at 77 K by 10% degradation of gm and ID and by 50 mV increase of VTH at VGS=VDS and VGS=(1/2)VDS stress conditions

## Slide 8: Hot-Carrier Degradation--65 nm
Up to now, the similar conclusion as 130 nm technology is obtained for the 65 nm technology
  The width dependence of degradation at 77 K is not evident
  The degradation at VGS=VDS is worse than that at VGS=(1/2)VDS for small length transistors
10%
Degradation vs time for transistor with different
WIDTHS
Degradation vs time for transistor with different LENGTHS
10%

## Slide 9: Lifetime Prediction--65 nm
The smallest length transistors at stress condition of VGS=VDS have the shortest lifetime (10 µm/0.06µm transistor as an example)
  The width dependence of degradation at 77 K is not evident
  The degradation at stress condition of VGS=VDS is worse than that of VGS=(1/2)VDS for small length transistors (60 nm)
To get to the 20 years lifetime, the power supply voltage should be less than 1.30 V at the worst stress condition (Nominal supply=1.2V)
The lifetime predictions of the 10µm/0.06µm transistor at 77 K by 10% degradation of gm and ID and by 50 mV increase of VTH at VGS=VDS stress condition

## Slide 10: Summary
What was done already
  26 transistors in 130 nm technology
    Length=0.13µm, Width=1, 2, 5, 10, 20, 50 µm
    Length=0.2 µm and 0.4 µm, Width=2 µm
  11 transistors in 65 nm technology
    Length=0.06µm, Width=0.5, 1, 2.5, 5, 10, 25 µm
    Length=0.1µm and 0.2 µm, Width=10 µm
What will be done next according to the plan
    Length=0.2 µm, Width=10 µm at different stress condition
What is to be achieved at the end of the test
  Which technology to be used for the circuit design
  What guidelines to be used for the circuit design
  Obtain basic modeling parameters for the circuit design

## Slide 11: Acknowledgement
Thanks to Albert Dyer for his help on the setup of the cryostat and bonding wires of the chips
Thanks to Theresa Shaw, Steve Chappa and Erik Voirin for their helps on the setup of the cryostat
Thanks to URA award for support on this work