## Slide 1: MAP Cooling Solenoid (Tuesday, April 15th)
F. Borgnolutti

## Slide 2: Latest version of the System

## Slide 3: Magnetic field on the axis
-13.7 T
13.7 T

## Slide 4: Peak field
Peak field in the coils at nominal current
Inner solenoid: 15.07 T
Middle solenoid: 7.13 T
Outer Solenoid: 6.77 T

## Slide 5: Load line
Chart: B (T)
| 6.77 | 0
outer solenoid | 153 | 0
Middlesolenoid | 135 | 0
Inner Solenoid | 220 | 0
Nb3Sn, 4.2 K, 5% degra., SF corr | 1912.1053 | 1846.8259 | 1784.0793 | 1723.715 | 1665.5959 | 1609.5962 | 1555.6007 | 1503.5035 | 1453.2071 | 1404.6211 | 1357.6625 | 1312.2538 | 1268.3233 | 1225.8045 | 1184.6352 | 1144.7574 | 1106.117 | 1068.6634 | 1032.349 | 997.1293 | 962.9626 | 929.8095 | 911.9938 | 866.3978 | 836.0714 | 806.6225 | 778.0216 | 750.2408 | 723.2537 | 697.0353 | 671.5617 | 646.8104 | 622.7598 | 599.3894 | 576.6798 | 554.6124 | 533.1695 | 512.3341 | 492.09 | 472.4219 | 453.3148 | 434.7547 | 416.728 | 399.2217 | 382.2233 | 365.7209 | 290.2612 | 225.6527 | 170.8322 | 124.9088 | 87.1278 | 56.8439 | 33.5009
Nb3Sn, 1.9 K, 5% degra., SF corr | 2250.4874 | 2178.9386 | 2110.1252 | 2043.8829 | 1980.0616 | 1918.5241 | 1859.1446 | 1801.8075 | 1746.4061 | 1692.8422 | 1641.0249 | 1590.87 | 1542.2994 | 1495.2404 | 1449.6253 | 1405.3911 | 1362.4789 | 1320.8334 | 1280.4033 | 1241.1399 | 1202.9978 | 1165.9343 | 1145.9945 | 1094.8845 | 1060.8245 | 1027.6953 | 995.465 | 964.1034 | 933.5819 | 903.8732 | 874.9516 | 846.7926 | 819.373 | 792.6706 | 766.6643 | 741.334 | 716.6606 | 692.6258 | 669.2121 | 646.4028 | 624.1819 | 602.5343 | 581.4452 | 560.9006 | 540.8872 | 521.3919 | 431.2726 | 352.4433 | 283.7624 | 224.2745 | 173.1719 | 129.7655 | 93.4621
Nb-Ti, 1.9K, no degra, no SF | 2017.8639 | 1629.5878 | 1339.5769 | 1106.7324 | 910.7119 | 739.995 | 587.3723 | 447.9082 | 317.8345 | 193.6636 | 70.2212 | 1.5229
Nb-Ti, 4.2 K, no degra.,no SF | 1245.6137 | 970.7498 | 762.106 | 591.868 | 446.0687 | 316.5101 | 197.4928 | 83.4026 | 4.4073
Nb-Ti:
  Bottura’s formula
  No sf correction
  No cabling degradation
  Cable filling factor = 0.26
Nb3Sn:
  QXF jc
  5% current degradation due to cabling
  Self-field corrected
  Cable filling factor = 0.33
 Nb-Ti can be used for the Middle and Outer solenoids.
 Nb3Sn is required for the Inner solenoid.
Nb-Ti (1.9 K)
Nb3Sn (1.9K)
Nb3Sn (4.2K)
Nb-Ti (4.2 K)
Inner solenoid
Middle solenoid
Outer solenoid

## Slide 6: Solenoids in Nb3Sn
 | % of the load line at operational current |  | 
 | Inner solenoid | Middle solenoid | Outer solenoid
Nb-Ti, 4.2 K | - | 78% | 76%
Nb-Ti, 1.9 K | - | 61% | 59%
Nb3Sn 4.2 K | 86% | - | -
Nb3Sn, 1.9 K | 79% | - | -
 Middle and Outer solenoids: Nb-Ti at 4.2 K can be used (22-24% margin).
 Inner solenoid: Nb3Sn at 4.2 K gives 14% margin on the current. If not enough operating at 1.9 K would give 21% margin

## Slide 7: Magnetic Forces
Global forces applied to the coils:
y

## Slide 8: Mechanical Model (Ansys)
RF cavity
Nb-Ti Coils
Nb3Sn Coil
Stainless-steel casings

## Slide 9: Mechanical Model (Ansys)
20 mm
Stainless-steel
Nb3Sn
NbTi
NbTi
20 mm
18 mm
10 mm
15 mm
15 mm
20 mm
2 mm gap
18 mm
2 mm gap
10 mm
10 mm

## Slide 10: Mechanical Model (Ansys)
 | 300 K | 4.2 K
316 LN | 210 GPa | 210 GPa
Coil X-section | 45 GPa | 45 GPa
Coil azimuthal | 90 GPa | 90 GPa
Young Modulus

## Slide 11: Mechanical Model: Loading Sequences

## Slide 12: Mechanical Model: Loading Sequences
50 μm shim
1 – Coil Pre-stress
2 – Cool-Down
3 – Powering
(magnetic forces)

## Slide 13: Results: Stainless-Steel structure

## Slide 14: Structure: Application of the pre-stress
Stress in the structure < 141 Mpa
(yield strength 316LN at RT 350 MPa )

## Slide 15: Structure: Cool-Down
Stress in the structure < 116 Mpa
(yield strength 316LN at 4.2K  1 GPa )

## Slide 16: Structure: Powering
Stress in the structure < 470 Mpa
(yield strength 316LN at 4.2K  1 GPa )

## Slide 17: Results: Coils

## Slide 18: Coils: Peak stress values
 | σx (Mpa) | σy (Mpa)
Key | -34 | -58
C-D | -25 | -44
Powering | -264 | -317
Inner Coil (Nb3Sn)
Peak stress in the middle coil < 170 Mpa
Peak stress in the outer coil < 70 MPa
Nb-Ti coils
Nb3Sn safe limit: 200 MPa

## Slide 19: Stress in the Nb3Sn coil @ Powering
σx
σy
-70 MPa
-180 MPa

## Slide 20: Hoop Strain
Maximum hoop strain in the Nb3Sn coil is 0.22 %
Irreversible strain limit with Ti doped Nb3Sn strand ~ 0.25 %

## Slide 21: CONCLUSION
Nb-Ti @ 4.2 K provide enough margin for the outer coils
Need Nb3Sn for the inner coil. Small margin at 4.2 K (14%). Good at 1.9 K (21%).
Peak stress in the Nb3Sn coil: Singularities around 300 Mpa > 200 MPa safe limits
Hoop strain in the Nb3Sn coil: Close to the irreversible strain limit.