## Slide 1: Radiation Heat Load and Coil Lifetime Calculations in Support of FRIB Dipole Magnet Design
Dali Georgobiani, Mauricio Portillo, Marc Hausmann
Facility for Rare Isotope Beams, Michigan State University

## Slide 2: Outline
Introduction
  Radiation Transport Scope within FRIB project
  Superconducting Dipole SCD1 in FRIB Preseparator
Calculation Formalism
Analysis Examples:
  Dipole beam blocker design challenge
  Dipole component heat loads and coil lifetimes
Summary and Conclusions
References

## Slide 3: FRIB Radiation Transport Scope Radiation Transport Calculations Support Technical Design and Safe Operation of Entire Project
Experimental Systems
  Bulk, local shielding
    Personnel doses, public doses (skyshine, emissions)
  Component and material choices
    Component life
  Hands-on capabilities, remote handling
    Personnel doses
  Non-conventional utilities
    Personnel doses, public doses (emissions)
Accelerator Systems
  Bulk, local shielding
    Personnel doses, public doses (emissions)
  Component and material choices
    Component life
  Hands-on capabilities
    Personnel doses
  Non-conventional utilities
    Personnel doses, public doses (emissions)
Experimental areas
  Bulk, local shielding
    Personnel and public doses
  Component and material choices
1 kW rare isotope beams
400 kW beam (~ 100 kW at target, ~ 300 kW at beam dump)
1 W/m beam losses

## Slide 4: Radiation Transport Group
Reg Ronningen is Radiation Transport Department Manager
Radiation Transport Group members:
Dali Georgobiani
Mikhail Kostin
Jeremy Northum
Reg Ronningen

## Slide 5: Fragment Separator
Three stage fragment separator for production and delivery of rare isotopes with high rates and high purities to maximize FRIB science reach
Primary beam power of 400 kW
  Beam energies of ≥ 200 MeV/u
Hot cell: High radiation environment
Radiation heat loads to magnets
Component lifetime concerns

## Slide 6: Preseparator Components
Target Vacuum Vessel
Beam Dump Vacuum Vessel
Wedge Vacuum Vessel
Target Assembly
Beam Dump Assembly
Wedge Assembly
Beam
SC dipoles
SCD1
SCD2

## Slide 7: SCD1 Mechanical Design
Superconducting dipole SCD1

## Slide 8: Unique Position of the SCD1 Magnet
Beam induced effects on magnets and other components are important to FRIB operations
  Power losses need to be removed efficiently
  Lifetimes depend on radiation doses
Beam optics modes affect the loss characteristics
  Requires beam physics and radiation transport calculations
  Optics modes developed to maximize rare isotopes to experiment yet minimize damage
Losses studied for SCD1 because it has the largest chance for beam power deposition
  No separation upstream of it
  Nominally no primary beam after the beam dump following this dipole
Target
SCD1
Beam Dump
FRIB preseparator magnets and other elements
Wedge

## Slide 9: Radiation Transport Calculations
Calculations based on models developed from mechanical and facility design
Model, materials updated as needed
  Updates provided by mechanical design group and magnet systems department
    Magnetic fields used correspond to those needed for beam optics
  Different situations/settings that place beam in different locations provided by fragment separator group
Detailed power deposition information provided to the magnet designers and engineers for final magnet design
Calculations include coil radiation dose leading to coil lifetime estimates
Magnet heat loads drive the design of cooling water loops and cryogenic components
Radiation transport model
Beam
SCD1

## Slide 10
Introduction
  Radiation Transport Scope within FRIB project
  Superconducting Dipole SCD1 in FRIB Preseparator
Calculation Formalism
Analysis Examples:
  Dipole beam blocker design challenge
  Dipole component heat loads and coil lifetimes
Summary and Conclusions
References

## Slide 11: Improvements in Design of SCD1
Settings for neutron-rich light rare isotopes lead to large deflection of primary beam in SCD1 (e.g. 18O primary beam in 8He setting)
  Primary beam (~ 300 kW beam power) would have hit cryostat
Cryostat interference identified with primary beam at exit corner
Design of exit corner opened up to remove interference
  Primary beam clears magnet hardware
Beam blockers introduced to control power deposition into cryostats
  Beam blockers optimized to protect dipole cryostats from direct beam
Heat load calculations performed to guide the dipole design and blocker optimization
Optimum beam blockers
Cryostat interference with primary beam

## Slide 12: Calculation Input and Methodology
Radiation transport code PHITS and beam optics codes COSY and LISE++ results are compared to validate the codes against each other
A specific set of beam parameters used:
  18O beam incident on 2.48 g/cm2 graphite target
  Beam energy 200 MeV/u; beam power 400 kW
  Beam rigidity for fragment of interest (8He) is 8 T-m

## Slide 13: Angular and Energy Straggling Comparison
Best match between available models of angular and energy straggling selected via side-by-side comparisons.
RMS values calculated after target for both the primary beam and fragments, as well as average energies, are in reasonable agreement as shown in the tables.
Average energy of the primary beam after the target
Angular and energy straggling RMS values calculated with LISE++ and PHITS for the primary beam and fragments

## Slide 14: Beam Optics Comparison
Beam envelopes for 12C fragments from target shown
Beam optics and fragment distributions are similar in PHITS and LISE++

## Slide 15: Particle Flux Maps
Both the primary beam 18O and reaction products shown
Total heat loads into the bottom blocker calculated by PHITS and by LISE++ are in reasonable agreement

## Slide 16: SCD1 Beam Blocker: Design Summary
Based on PHITS calculations, beam interference conditions in the SCD1 components were identified and resolved as follows:
  Increasing width of dipole exit window opening
    Primary beam clears magnet hardware safely
  Adding top and bottom beam blockers inside of dipole gap
    Stops intense fragments near the primary beam
    Reduces the radiation heat load to cryostat
  Optimizing the blocker shape
    To minimize direct beam losses while maintaining adequate shielding
  Developing optimal beam optics settings
    To minimize losses to all surrounding dipole components
Calculations of induced thermal losses with PHITS aid designs of water and helium cooling

## Slide 17: SCD1 Design Improvements: Analysis Summary
Radiation transport code PHITS -- with particular settings for straggling and energy loss as well as its fragment production model -- was validated against beam optics codes LISE++/COSY
  Good agreement demonstrated
    Flux maps from both codes show similar distributions
    Power deposition to the lower blocker is calculated to be 3 kW for LISE++/COSY and 2.1 kW for PHITS
    The lower value can be explained by the lower angular spread for reaction products using the PHITS model
The outcome of this study provides design requirements for SCD1 in terms of the beam conditions

## Slide 18
Introduction
  Radiation Transport Scope within FRIB project
  Superconducting Dipole SCD1 in FRIB Preseparator
Calculation Formalism
Analysis Examples:
  Dipole beam blocker design challenge
  Dipole component heat loads and coil lifetimes
Summary and Conclusions
References

## Slide 19: Change from HTS to LTS Technology
  Calculations performed to support Low Temperature Superconductor (LTS) magnet choice
  Model has changed by moving coils into yoke by 5 cm at each side
Beam
direction
Power density map position
SCD1
Original coil location
New coil location
d
d+10cm
Pole tips
Coils

## Slide 20: Extreme Cases
Benchmark cases defined having potential for the most extreme conditions on the magnets
Oxygen primary beams tend to pose the most extremes
  Large fraction of the beam reacts
  Products and primary beam characterized by some of the highest phase spaces after the target
Production of 8He from 18O
  Due to large 8He magnetic rigidity:
    Causes large overfocusing of most products
    Causes large deflection in dipole, hence high losses towards lower region
Production of 9C from 16O
  Due to low 9C magnetic rigidity:
    Causes large underfocusing of most products
    Low deflection in dipole, hence most losses towards upper region
Overfocusing and underfocusing may cause more losses at focusing magnet before the dipole

## Slide 21: Calculation Input
    Beam Physics group provided beams and magnetic fields
    16O, 294 MeV/u, 400 kW; product 9C
      Worst case for the upper region of the dipole
    18O, 200 MeV/u, 400 kW; product 8He
      Worst case for the lower region of the dipole
    18O, 266.4 MeV/u, 400 kW; product 10Be
      Worst case for the poletips
Coil material assumed to be NbTi + Cu + Cyanate Ester
Coil lifetimes calculated assuming radiation tolerance of 100 MGy
Radiation tolerance in various materials

## Slide 22: Power Density Maps
Power density (heat load) map examples in the dipole
Width (cm)
Height (cm)
Power density (W/cc)
Width (cm)
Height (cm)
Power density (W/cc)
HTS
LTS
Width (cm)
Height (cm)
Power density (W/cc)
Width (cm)
Height (cm)
Power density (W/cc)
HTS
LTS
16O, 294.4 MeV/u
18O, 266.4 MeV/u

## Slide 23: Dipole Coil Heat Load and Lifetimes
18O, 200 MeV/u
  Peak coil heat load, mW/cc: 5 (HTS), 2 (LTS)
  Coil lifetimes, years: 16 (HTS), 41 (LTS)
  Higher than life of facility
16O, 294.4 MeV/u
  Peak coil heat load, mW/cc: 100 (HTS), 7 (LTS)
  Coil lifetimes, years: 0.8 (HTS), 12 (LTS)
  LTS design improves lifetime dramatically
LTS
HTS
Heat Load (W/cc)
Heat Load (W/cc)
Heat Load (W/cc)
Heat Load (W/cc)
HTS
LTS
Beam

## Slide 24: Coil Lifetimes: Other Examples
18O, 266.4 MeV/u
  Peak coil heat load, mW/cc: 30 (HTS), 20 (LTS)
  Coil lifetimes, years: 2.7 (HTS), 4.1 (LTS)
48Ca, 261 MeV/u
  Peak coil heat load, mW/cc: 20 (HTS), 10 (LTS)
  Coil lifetimes, years: 4.1 (HTS), 8.2 (LTS)
  Coil heat loads and lifetimes greatly vary depending on the primary beam conditions (magnetic field settings, path, etc.)
  Keep in mind: Most of the time, we expect to run different beams that do not present extreme cases in terms of heat loads

## Slide 25: Dipole Cryostat Heat Load
18O, 200 MeV/u
  Total heat load, W: 27 (HTS), 15 (LTS)
Worst cases for HTS; but implementing LHS sharply reduces heat load:
16O, 294.4 MeV/u
  Total heat load, W: 714 (HTS), 81 (LTS)
18O, 266.4 MeV/u
  Total heat load, W: 807 (HTS), 69 (LTS) (maps not shown)
LTS
HTS
Heat Load (W/cc)
Heat Load (W/cc)
Heat Load (W/cc)
Heat Load (W/cc)
HTS
LTS
Beam

## Slide 26: Pole Tip Heat Load
18O, 200 MeV/u
  Total heat load, W: 93 (HTS), 116 (LTS)
  25% increase to pole tip; eliminates having this loss at the cryostat
16O, 294.4 MeV/u
  Total heat load, W: 2533 (HTS), 3252 (LTS)
  28% increase
18O, 266.4 MeV/u
  Total heat load, W: 5160 (HTS), 5690 (LTS)
  10% increase (maps not shown)
LTS
HTS
Heat Load (W/cc)
Heat Load (W/cc)
Heat Load (W/cc)
Heat Load (W/cc)
HTS
LTS
Beam

## Slide 27: SCD1 Component Heat Load Conclusions
  Calculations performed support Low Temperature Superconductor (LTS) magnet choice
  Heat load maps used as a diagnostic tool and to optimize design
  Calculated heat loads define requirements for the cryogenic system
  Geometry changes reflecting LTS design reduce radiation heat loads into coils and cryostats
  LTS coils provide adequate lifetime for operation in radiation environment

## Slide 28: Summary
Radiation transport code PHITS and beam optics codes COSY and LISE++ results were compared to validate the outcome of radiation transport calculations
  Good agreement between the radiation and beam transport codes has been demonstrated
Based on PHITS calculations, beam interference conditions in the SCD1 components were identified and resolved
  Beam blocker designs have been optimized
  SCD1 component heat load calculations support Low Temperature Superconductor (LTS) magnet choice
    Reduced radiation heat loads into coils and cryostats

## Slide 29: References
T. Sato, K. Niita, N. Matsuda, S. Hashimoto, Y. Iwamoto, S. Noda, T. Ogawa, H. Iwase, H. Nakashima, T. Fukahori, K. Okumura, T. Kai, S. Chiba, T. Furuta and L. Sihver, "Particle and Heavy Ion Transport Code System PHITS, Version 2.52 ", J. Nucl. Sci. Technol. 50:9 (2013) 913-923.
K. Makino, M. Berz, "COSY INFINITY Version 9“, Nucl. Instr. and Meth. Phys. Res. A 558 (2005) 346-350.
O.B. Tarasov, D. Bazin, "LISE++: Radioactive beam production with in-flight separators “, Nucl. Instr. and Meth. Phys. Res. B 266 (2008) 4557-4664.

## Slide 30: Acknowledgements
I would like to express my gratitude to the RESMM’15 organizers…
…To my colleagues at FRIB for all their help and guidance…
…And to fellow participants for their attention!
This material is based on work supported by the U.S. Department of Energy Office of Science under Cooperative Agreement DE-SC0000661, the State of Michigan and Michigan State University. Michigan State University designs and establishes FRIB as a DOE Office of Science National User Facility in support of the mission of the Office of Nuclear Physics.