## Slide 1: Study of the Displacement Per Atom in the n-alpha Reaction on MgB2 in the Frame of the Hi-Lumi-LHC Project Workshop on Radiation Effects in Superconducting Magnets and Materials 2015 (RESMM'15)
F. Broggi, A. Bignami, C. Santini
RESMM’15 East Lansing 10-14 May 2015

## Slide 2
LASA Laboratorio Acceleratori Superconduttività Applicata
Francesco.Broggi@mi.infn.it
Francesco.Broggi@cern.ch
Francesco Broggi

## Slide 3: Outline
HiLumi-LHC
WP 6 Cold Powering
What’s new since last year
Irradiation test simulation on MgB2
What is the relative a and Li importance to DPA ?

## Slide 4: Hi-Lumi-LHC Project

## Slide 5
Task 1
Coordination
CERN/INFN
Task 2
Cryogenics
CERN
Task 3
Electr. Transf.
Cryostat
Univ. South
Task 4
Energy Dep.
Material
INFN
CERN activity
Integration
Civil engineering
Interfaces
(mech, vacuum, electr)
Vacuum
SC cables/SC link
Cryostat of SC link
Current leads
Protection
CERN activity
Prototypes construction
Cryostat
- Prototypes test
- System design
- Series specification
- Series construction
- Integration
- Operation
Fluka team
WP6 Structure (Coordinator A. Ballarino (CERN),
Deputy coordinator F. Broggi (INFN))
“Cold Powering”

## Slide 6
Cold Powering via Superconducting Links
Advantages of remote powering:
Safer long-term operation of powering equipment (power converters, current leads and associate auxiliary devices) located in a radiation-free environment;
Safer access of personnel to equipment for maintenance, repair, diagnostic and routine tests interventions;
Reduced time of interventions on power converters, current leads and DFBs if the powering equipment is located outside of the tunnel areas – gain in machine availability ;
- Free space in the beam areas which becomes available for other equipment.
Courtesy of Amalia Ballarino
2nd Joint HiLumi LHC-LARP Annual Meeting
Frascati 14-16 November 2012

## Slide 10: What’s Next (May 2014)
Implement the Links geometry in the LHC Layout in FLUKA (DONE see Andrea’s talk)
Simulations for Point 5 (to be done)

## Slide 11: SCL Routing into the tunnel
Two possible routings of the SCL have been investigated:
2) Arrive from surface
after D1
1) Arrive from surface closer to IP1. The SCL runs aside the triplet and then connect to the Connection Module (CM), aside the beam pipe

## Slide 12
12
12
Particle Fluencies (option 1) (From Q1 to the SCL 1 m above Q1)
Escaping from Q1
28% photons (1250 ph/event) 9% of the kinetic energy is from photons (3.2 GeV/event)
71% neutrons (3143 n/event) 65% from neutrons (22.8 GeV/event)
Entering the SCL
33% photons (12.5 ph/event) 14% of the kinetic energy is from photons (33.8 MeV/event
67% are neutrons (25.4 n/event) 68% from neutrons (170 MeV/event)

## Slide 13
13
13
Particle Fluencies (option 2) (To the SCL in the CM after D1)
Entering the SCL in the Connection Module
95% photons (126 ph/event) 35.8% of the kinetic energy is from photons (295 MeV/event)
2.4% neutrons (3.2 n/event) 6.3% from neutrons (51.6 MeV/event)

## Slide 14: Fluencies
Neutron and photon fluencies in the Horizontal part of the SCL inside the CM (at 3000 fb-1)

## Slide 15: Simulation progress
Definitive definition of the cable geometry and material
Cable layout
6x20kA , 7x3kA, 4x0.4kA, 8x.12kA
ext  65 mm
18 MgB2 wires
 = 6.5 mm
Cu
MgB2 ,  = 0.85 mm
Courtesy A. Ballarino
Considering 1 m Link length ; S=33.2 cm2, r=2.57 g cm-3 density
Being M=45.93 g/mol the MgB2 molar mass
Pure MgB2 atoms cm-3
10B atoms m-1

## Slide 16: Boron Consumption
Bnat= 80% 11B + 20% 10B
10B slow neutron cross section for this reaction is about 4×103 barn at room temperature (En=0.025 eV) and 1.5×104 barn at 20 K (En=0.0017 eV)
As from the data before the n entering the SCL inside the CM (Option 2) are about 3.2 n/event.
At an integrated luminosity of 3000 fb-1 LHC will collect about 3·1017 p-p events, so the
total amount of n in the SCL will be about 1·1018 .
The number of 10B atoms (see slide 15)is much higher than 1 · 1018 and even supposing 1 capture reaction per neutron
the 10B consumption is negligible

## Slide 17
n Boron capture reaction
What is the contribution of alpha particles and of Li ion to the DPA?

## Slide 18: Neutrons on MgB2 Simulations
Central section:
neutrons react at the surface (self shielding effect)
MgB2 with natural composition of B (80% 11B – 20% 10B)
Thermal Neutrons (isotropic source)
18
n
Target
TARGET (2x2x2 cm3)
x
z
The transport cut-off : hadrons 10-6 GeV neutrons 10-14 GeV
damage energy threshold = 25 eV

## Slide 19: Energy Deposition and DPA
19
Energy Deposition
1.11E-03(±0.03%) GeV/pr
DPA
3.66E-23 (±0.03%)
Tsukuba November 20th 2014

## Slide 20: a Fluence
20
20
Tsukuba November 20th 2014
Reactions occurring at the surface cause a high fluence of alfa particle outside

## Slide 21: Single contribution (of a and Li)
21
Simulation with single internal isotropic source
Target
n
a
Li
Li
n
a
For the other different cases studied (alpha and Li) there are similar plots
These plots have not any absolute meaning, they just show that all the energy is deposed inside the sample (and the corresponding DPA is all provided inside them) and so the results can be compared.

## Slide 22: Considerations
22
The most significant parameter for the DPA is its the peak value. As a matter of fact the mean value of the DPA, as it is defined, indicates that every atom undergoes to the given amount of displacement.
It is evident that it does not happen because from previous figures the energy deposition and DPA occur in a limited part of the target, so it is meaningless to attribute a DPA to the whole region.
Conversely the peak value gives an indication of the localized radiation damage and this can give effects on the material characteristics.

## Slide 23: Single contribution (of a and Li) Maximum and average DPA in the MgB2 target induced by the reaction products of the boron capture.
23
Reaction occurrence |  | Max DPA [DPA/primary]±Err% | Mean DPA [DPA/primary]±Err%
94% | Alpha (1.47 MeV) | 15.911∙10-22 ± 7.9 | 6.1633∙10-22± 0.001
 | Lithium (0.84 MeV) | 32.968∙10-22 ± 6.9 | 11.952∙10-22± 0.001
 | Photon (0.482 MeV) | == | ==
6% | Alpha (1.777 MeV) | 16.422∙10-22 ± 6.3 | 6.3141∙10-22± 0.002
 | Lithium (1.015 MeV) | 31.447∙10-22 ± 6.6 | 12.240∙10-22± 0.001

## Slide 24: DPA Evaluation (of a, Li and n)
24
Combining the data with the corresponding weight we have
 | Max DPA [DPA/primary]±Err% | Mean DPA [DPA/primary]±Err%
Alpha | 15.942∙10-22 ± 7.8 | 6.1724∙10-22± 0.001
Lithium | 32.876∙10-22 ± 6.8 | 11.969∙10-22± 0.001
Neutron | 46.295∙10-22 ± 5.0 | 18.345∙10-22± 0.001
Summing the contribution of the alpha particle with the Lithium one:
15.942∙10-22 + 32.876∙10-22 = 48.818∙10-22 ± 0.257 max DPA
6.1724∙10-22 + 11.969∙10-22 = 18.141∙10-22 ± 0.001 mean DPA
Internal neutrons
46.295∙10-22 ± 2.334∙10-22 max DPA
18.345∙10-22 ± 0.001∙10-22 mean DPA
The Lithium contribution to DPA is 66-67% of the total (the sum of the alpha and Lithium)
The contribution of the alpha is about 33-34%

## Slide 25: Considerations
25
PEAK VALUES
The peak value calculated by the sum of the alpha and Li contribution is about 6% higher that the values given by the neutrons.
This because we assume that every neutron reacts with 10B realizing one Li and one alpha particle.
MEAN VALUES
For the mean DPA calculated by the sum of the alpha and Li contribution is about 1% lower that the DPA induced by the neutrons.
This is probably due to the statistics, and anyway this value (the mean DPA) in our analysis is less important, as explained before.

## Slide 26: Conclusions and Perspectives
Irradiation tests vs. simulations comparison …. (lowering of the Tc enhancing of the upper critical field)
Code benchmarking
Correlations between DPA and SC properties …

## Slide 27: Acknowledgment
Thank You for Your attention
Michael Eisterer (ATI, Wien)