## Slide 1: The NOvA Medium Energy Target Design and Construction Experience
Patrick Hurh
Fermilab
24 September 2014
NBI Workshop 2014

## Slide 2: Overview
Origins
Design/Analysis
Construction
Summary
Many Thanks and Credit To:
M. McGee, R. Stewart, J. Wilson, FNAL design/eng team
R. Ford, M. Stiemann, F. Schneider, Keith Anderson, FNAL technical team
M. Fitton*, J. O’Dell, T. Davenne, RAL
V. Garkusha, IHEP
*Provided several slides

## Slide 3: Origins
Design originated at IHEP, Russia, in 2006-2009
  Medium Energy Target for NuMI beamline at higher beam power
  Resulted in analysis reports, a 3-D model, and associated drawings
Picked up by Michael McGee of Fermilab, who worked with Rod Stewart to “translate” the model/drawings
  Performed thermal and stress analysis of target components
  Modified/Re-designed several features
Manufactured, assembled and tested first target at RAL (STFC) under direction of Michael Fitton.
  Identified several improvements/corrections
  Developed construction techniques in parallel with Fermilab team led by M. McGee

## Slide 4: NuMI versus NOvA
NuMI- Low Energy Configuration
Target inserted into Horn 1 Inner Conductor
NOvA- Medium Energy Configuration
Target well US of Horn 1

## Slide 5: Design & Analysis

## Slide 6: Design & Analysis

## Slide 7: Design & Analysis

## Slide 8: Design & Analysis

## Slide 9: Target Fin Thermal Analysis
Table from 2006 IHEP Report assumes:
5.5e13 ppp
(9.0e13) ppp
1.2 s rep rate
Actual NOvA Beam:
Energy: 120 GeV
Sigma: 1.3 mm
4.8e13 ppp
1.3 s rep rate
Confirmed by RAL analysis:
672˚ C “steady-state”
226˚ C “jump”

## Slide 10: Target Fin Stress Analysis
2006 IHEP Report:
~32 MPa (@P4)
5.5e13 ppp
Confirmed by RAL analysis:
~30 MPa peak stress (R.T. properties)
Note Be fin is ~190 MPa (R.T. properties)
Note IG-43 is ~3 MPa (R.T. properties)

## Slide 11: Target Beam Windows - Thermal
US Window: (0.25 mm thick) 24 ˚C to 66 ˚C
DS Window: (1.25 mm thick) 57 ˚C to 67 ˚C
Analysis by M. McGee (FNAL)

## Slide 12: Target Beam Windows – Stress
Analysis by M. McGee (FNAL)
Safety Factor of ~4 on yield
US
DS

## Slide 13: Outer Vessel - Thermal
ANSYS CFX Simulation of natural convection and radiation inside target vessel. Used to estimate target fin operating temperatures and emissivity requirements of outer vessel.
Typical Heat Balance
Total Heat load =7482W
Heat conducting down fins to main cooling rail =6867W
Heat radiating from fins to the outer vessel =476W
Convection and conducted through helium from the fins to the outer vessel =139W
Analysis by T. Davenne (RAL)

## Slide 14: Construction
MET-01 Manufactured by STFC (currently installed)
MET-02 Manufactured by Fermilab
MET-03 Manufactured by STFC, Modifications, 1) Internal welds of outer vessel removed, 2) Outer vessel anodised
MET-04 Manufactured by Fermilab
Apologies to Fermilab Team – Slides are RAL-centric, but parallel development efforts were made at Fermilab!!
Slide provided by M. Fitton (RAL)

## Slide 15: NOVA tests and analysis
Measurement of heat transfer to target fins using thermal imaging camera. Consistent contact across all graphite fins confirmed but also identified thermal issue with cooling of horizontal budal monitor fin.
310°C
152°C
Horizontal budal bracket redesigned by thickening material and shortening conduction path. Simulation shows this more than halves the operating temperature.
Slide provided by M. Fitton (RAL)

## Slide 16: Outer vessel
Water cooled vessel of the NOvA target.
Design modified after MET-01 so there are no internal welds.
MET-03, Only 2 external welds
Slide provided by M. Fitton (RAL)

## Slide 17: NOVA welding development
High quality welds (NAS 1514 Class II or better) in 6061 aluminium proved very difficult to produce consistently for plug weld.
By visual inspection welds look very good.
Radiography reveals significant porosity
Parameters explored to optimise weld:
Cleaning (including etching)
Filler wire selection
Pre-heating
AC current/balance Gas (Helium/Argon Blend)
Slide provided by M. Fitton (RAL)

## Slide 18: NOVA welding development
First step – reduce number of Aluminium from water cooling circuit.
Original design – 9 Aluminium welds
Modified design – 3 Aluminium welds
Blind gun drilled holes, with single cross drill
Pipe stubs machined into rail
AL-SS Roll bonded plate replaced with friction welded blanks
Fermilab Notes:
Use of extruded bar resulted in better straightness of gun-drilled holes
Outside rail dimensions finished after drilling to put holes in best true location
Slide provided by M. Fitton (RAL)

## Slide 19: NOVA welding procedure
  CLEANING
  Applied to all parts and welding rods
  Degrease using Trichloroethylene (TCE) a vapor solvent for organic materials
  Alkaline bath w/ pH 11-11.5 (for 5 min)
  Tap Water Rinse (ambient) to remove residual alkaline solution (for 5 min)
  Nitric Acid Etch 38-48% Nitric, 0.7-0.9% HF-3 (for 2.5 min)
  DI water Rinse (for 5 min) at ~ 90 F
  Oven dry at 130 F (for 30 min)
  WELDING
  AC TIG (HF Impulse) Welding
  Plug Weld Parameters: Pos electro +170/ Neg. electro -180, balance 80% & 130 Hz frequency
  Socket Weld Parameters: Pos electro +100/ Neg. electro -120, balance 80% & 130 Hz frequency
  Tungsten cup #5, flow 25 – 30 scfm (75% He/25% Ar) gas purge
Note: This welding procedure was developed by Fermilab with input from RAL and the welding vendor, Alloyweld
Slide provided by M. Fitton (RAL)

## Slide 20: QA- Welding radiography
Achieved NAS-1514, Class I Certification for cooling rail
Slide provided by M. Fitton (RAL)

## Slide 21: QA - Hydrostatic Pressure testing
Cooling rail tested to 200 psig
Outer vessel tested to 90 psig
Much higher than expected operational pressure.
Testing for leaks and weakness
Slide provided by M. Fitton (RAL)
Photos of pressure testing at Fermilab

## Slide 22: QA – Helium leak check
All components and complete assembly helium leak checked.
Specification:
Total leak rate < 1x10-9atm.cm3/sec
Slide provided by M. Fitton (RAL)

## Slide 23: QA - Metrology
Careful measurements using Coordinate Measuring Machine (CMM)
Tooling balls
Roundness and position
Pressing plate (4.5mm flatness)
Graphite fin tip alignment and straightness
Slide provided by M. Fitton (RAL)

## Slide 24: Alignment
Target rail aligned in outer vessel using large CMM and long probe
Clocks used to ensure outer vessel has not moved during adjustment
Slide provided by M. Fitton (RAL)

## Slide 25: Conclusion
Release of Horn 1 insertion constraint enabled the design of a robust target capable of operation at 700 kW beam power
Successful completion of multiple targets was dependent upon developments and creativity of skilled teams at both Fermilab and Rutherford Appleton Laboratory (RAL-STFC)
MET-01 has seen:
  Average Beam Power of ~260 kW
  Max Beam Power of ~368 kW
  Resulting in 3.3 x 1020 POT
Upgrades still ongoing
  Latest is the thermometer based beam position monitor (see J. Hylen talk…. NEXT!)

## Slide 26
Back-up

## Slide 27: Radiation Damage in Graphite
Chart: Tensile Property Changes Vs DPA
| 0.103 | 0.131 | 0.056
POCO ZXF-5Q Tensile | 0.31244 | 0.31244 | 0.45509
POCO ZXF-5Q Elastic Mod | 0.23167 | -0.084572 | 0.27542
SGL R7650 Tensile | 0.61079 | 0.60007 | 0.54593 | 0.5352
SGL R7650 Elastic Mod | 0.74869 | 0.64797 | 0.47848 | 0.54163
IG-430 Tensile | 1.1134 | 1.0966 | 1.0289 | 1.2995
IG-430 Elastic Modulus | 1.5589 | 1.172 | 1.2233 | 1.3463
IG-430 Tensile 300 C Anneal | 0.44055
IG-430 Modulus 300 C Anneal | 0.83054
IG-430 Tensile 170 C Anneal | 0.80576
IG-430 Modulus 170 C Anneal | 0.89909
IG-430 Tensile 290 C Anneal | 0.50142
IG-430 Modulus 290 C Anneal | 0.93893