## Slide 1: Analysis of Radionuclide Activation in the NuMI Decay Pipe Shield
S. Diane Reitzner
NBI 2014
23-09-2014

## Slide 2: Outline
Introduction
NuMI beamline
Activity found in the NuMI decay pipe shield
Simple MARS model of NuMI for radionuclide production calculations
Comparison of data to MARS
Conclusion

## Slide 3: Introduction
Tritium is highly mobile.
  Can transmit as gaseous hydrogen (HT) or as water (HTO)
  Able to transfers from one medium to another.
  Is difficult to contain.
Important to understand tritium production and behaviour in beamline shielding.
  Use core samples collected in 2006 and 2010 from the NuMI decay pipe shield for tritium studies.
Test MC method to predict tritium production.
  Use non-tritium radionuclides as benchmark.

## Slide 4: NuMI Target Hall
120 GeV
proton beam
Decay
Pipe
Horn 2
Horn 1
Target/Baffle Carriage
Steel Shielding
Flowable Fill
ρ= 2.2 g/cm3
Graphite Target
Focus resultant
pions and kaons
NuMI Beamline is subject to inflow of ground water.
  Provides an easy route for tritium migration.
Dehumidifiers in target hall are used to remove water from the air.
Air from the target hall is moved down the decay pipe passageway.

## Slide 5
93 m
98 m
249 m
683 m
2 m diameter pipe
2.9 m outer
radius of shield
3.7 m outer
radius of shield
Dolomite
Decay Pipe Walkway
To Target
Hall
To Absorber Hall
Neutrinos to MINOS in Soudan MN
2.1 m outer
radius
NuMI Decay Pipe
675 m long
Pions and kaons
decay to neutrinos and muons

## Slide 6: Sample Locations
Decay pipe cross section. The red lines show locations of samples.
Face of the decay pipe shield where some core samples were collected
Decay pipe walkway

## Slide 7: Data Analysis
Several samples collected at different depths from each sample location.
  Sample collection occurred after several days of beam off.
Samples first analyzed using a high purity germanium detector for radionuclide activity.
  7Be, 22Na, 54Mn, 46Sc, 60Co, 134Cs and 152Eu where found.
Tritium’s low beta endpoint energy and no decay gamma means that it cannot be counted directly from the samples.
  Tritium was leached from the samples and the leachate analyzed using a Tri-Carb LSC analyzer.
    Not all tritium is collected from a single leaching process.
  22Na was also detected in the leachate

## Slide 8: Activity at Upstream End of Decay Pipe

## Slide 9: Tritium Activity at Upstream End of Decay Pipe in 2006
ST9.99 2006
Direct Production
Absorption
Depletion

## Slide 10: Tritium Activity at Upstream End of Decay Pipe
2006
No dehumidifiers in target hall
375 days total, 75 days beam off
2010
Dehumidifiers in target hall
1899 Days total, 28 days beam off

## Slide 11: Tritium Activity at Downstream End of Decay Pipe
2006
No dehumidifiers in absorber hall
2010
Dehumidifiers in absorber hall

## Slide 12: 22Na Gamma vs Leachate
2006
Upstream, thin shield
2010
Upstream, thin shield

## Slide 13: Leaching Fraction for 22Na

## Slide 14: MC Analysis
Direct inventory of tritium is difficult to do for shielding
  Diffusion effects at surface
  Not all tritium leached from shielding for analysis.
Try using MARS to predict tritium activity in shielding.
  Test against other radionuclide production found in the shielding.
  Deduce leaching fraction for tritium by comparing activity ratios of tritium to other radionuclides
Use simple geometry model of NuMI target hall and decay pipe.
Extract out star densities in decay pipe shield for nuclide spatial distributions.
Extract nuclide production per star for R>1.7 m.

## Slide 15
NuMI Target
Hall in MARS
Horn 1
Horn 2
Baffle
Target
Decay Pipe
Entrance

## Slide 16: Star Density per Proton in the Decay Pipe Shield
Radius (m)
stars/cm3 per proton

## Slide 17: Nuclide Production Calculation
Extract nuclide production per proton for R>1.7m
Use DETRA to calculate activity Atot.
Intensity based on NuMI POT data.
Integrate over 375 days to compare to 2006 results
  300 day beam on
  75 day s beam off
Use Ratio of stars per bin over stars for R>1.7 m to scale activity.

## Slide 18: 2006 7Be Radial Distribution

## Slide 19: Radial Distribution Fits
MARS Fit:
  Identify first term with rapid drop-off at small radius
  Identify second term with attenuation at large radius
  b1 = 0.077±0.002, b2 = 0.024±0.001
Data Fit:
  Core samples not deep enough to fit the first term
  b2 = 0.0229±0.0011

## Slide 20: Nuclide Activity Comparison
Nuclide | MARS Activity (pCi/g) | DATA Activity (pCi/g) | MARS Ratio 7Be/X | Data Ratio 7Be/X
7Be | 454±91 | 346±52 | 1 | 1
22Na | 111±22 | 78.7±11.9 | 4.1±0.7 | 4.4±0.9
54Mn | 25.1±5.0 | 19.7±3.0 | 18.1±3.4 | 17.6±3.7
3H | 229±46 | 57.9±0.9 | 2.0±0.4 | 6.0±0.9
The activity at R=2.1 m and Z=93m (from Horn 1) in the NuMI decay pipe for 300 days of beam on followed by 75 days beam off.
Activities for 7Be, 22Na, and 54Mn agree with the activity seen in the core samples.
Ratio of 7Be/22Na, 7Be/54Mn agree very well with data.
MARS reports greater activity for tritium
  Tritium underreported in data as a single leach cycle does not collect all of the tritium

## Slide 21: Prediction of Leaching Fraction using MARS
Unknown value of leaching fraction L3H
  Lower bound of 0.10 from 22Na data.
    Past experience with soil and sand show that L22Na is smaller than L3H
  Upper bound of 0.81 from multi leaching data assuming that all the tritium is collected in two leaching processes.
Use ratio of 7Be/3H from MARS to predict L3H

## Slide 22: Predicted Leaching Fraction
Location from Horn 1 | Year | Radius | 7Be/3H from Data | Estimate L3H
93 m | 2006 | 2.1 m | 6.0 | 0.33±0.09
683 m | 2006 | 1.5 m | 8.0 | 0.25±0.07
93 m | 2010 | 2.1 m | 2.9 | 0.41±0.11
98 m | 2010 | 3.0 m | 1.8 | 0.66±0.17
249 m | 2010 | 3.0 m | 2.9 | 0.41±0.11
693 m | 2010 | 1.5 m | 3.0 | 0.40±0.10
Average |  |  |  | 0.41±0.14
Ratio of 7Be/3H from MARS:
2006: 2.0
2010: 1.2

## Slide 23: Conclusions
Activity in samples taken from the NuMI decay pipe shielding in 2006 and 2010 demonstrate the mobility of 3H.
Fixed nuclides like 7Be and 22Na can be used to benchmark Monte Carlo codes used for radionuclide production in shielding.
  MARS prediction of nuclide distributions match data.
  Predicted activity of fixed nuclides agree with data.
Comparison of tritium activity predicted by MARS to the activity seen in the samples implies that only 41% of the tritium collected in the deep samples.