## Slide 1: Creating a reliable source of pure low-radioactivity argon
Henning O. Back – Princeton University
Fermilab Detector R&D Review

## Slide 2: Atmospheric Argon Limit
Atmospheric Argon (AAr) | Underground Argon (UAr)
Contains beta emitter 39Ar at a concentration of 8x10-16 Produced by cosmic ray neutrons Radioactivity of AAr = 1 Bq/kg | Hidden from cosmic rays Concentration of 39Ar is at least 150 times less than AAr Radioactivity of UAr < 7mBq/kg ref. (arXiv:1204.6011)

## Slide 3: Low-radioactivity Argon is a National Resource
Sole supplier of UAr to programs requiring low radioactivity argon
  Dark matter
    DarkSide – 152 kg target
    DEAP – No UAr
  Low-level radioactivity detection
    Argon radiometric dating (calibration gas)
      Argonne – ATTA
      Heidelberg, Germany – ATTA
      Bern, Switzerland – gas proportional counters(?)
    National Security
      PNNL – gas proportional counters
Radio-dating gas samples
Our gas – 10 racks 4000 psi each
Inches
Feet

## Slide 4: Terrestrial argon sources As I understand them
40Ar comes from 40K decay
Atmosphere
  39Ar produced by cosmic ray neutrons
  40Ar(n, 2n)39Ar
Crust
  No cosmic rays
  Neutrons from U and Th
Mantle
  Very low U and Th
  Lowest 39Ar levels
Mantle
Low U and Th
(lowest 39Ar)
Crust – 1ppm U and Th (low 39Ar)
Atmosphere (39Ar/40Ar = 8×10-16)

## Slide 5: CO2 well in SW Colorado
There are geological formations that trap gases underground
We found CO2 well in SW Colorado (near Cortez)
Contains ~500 ppm Argon
39Ar activity < 0.65% of atmospheric argon
(arXiv:1204.6011)

## Slide 6
Chart: Raw CO2 well gas

## Slide 7: Getting to the underground argon

## Slide 8: Getting to the argon
Extraction
  In Colorado we extract a crude argon gas mixture (Ar, N2, and He)
Purification
  The gas from Cortez is then sent to Fermilab for further purification

## Slide 9: Underground Argon Source
Carbon Dioxide well in SW Colorado
  contains ~500 ppm argon
Princeton operates an extraction plant to produce crude argon mix from CO2
Crude mix:
  Argon (3-6%)
  Helium (85-95%)
  Nitrogen (1-10%)
  Trace contaminants
    CO2
    CH4
    C2H6
    C3H8
    …
Gas is shipped to Fermilab for further processing and purification

## Slide 10: Purification at FNAL
Great Initial Success
First commissioning with atmospheric argon (from Airgas)
  input mix: 6% Ar, 55% He, 44% N2
  output: 100% Ar, <500ppm N2
Waste
Cryogenic Distillation Column (CDC)
Input
Product
Booster
Transportation cylinder racks
The 2010 plan – commissioned Oct. 2011

## Slide 11: First Underground Argon (UAr) purification Fall 2012
Processed 500k liters gas (at STP)
Reached 99.7% pure argon (12.3 kg)
Issues:
  Different gas mix stalled distillation – High He content
  Gas flow stopped abruptly – Clogging from impurities
  Very slow – Not enough cooling
  Never reproducible – Not without large UAr losses
  Column flooding – Column too small

## Slide 12: The early 2014 issues
Methane contaminated gas  kills scintillation light
  Actually an old problem (from early VPSA operations)
  BUT, need to recover this gas to make up for losses
Oxygen contaminated gas  kills electron drift
  Increased production at VPSA plant to make up for losses
  Production increase came with Oxygen contamination

## Slide 13: Plant Expansion

## Slide 14: Plant systems
Helium Separator
Waste Stream Argon Capture
Contaminant Freeze Out
Distillation
Oxygen
Gettering

## Slide 15: Plant systems simplified
Waste
Condenser Booster Helium Separator
(CB)
Input
Product
Waste
CB
Charcoal Trap
(CBCT)
Input
Product
Waste
CDF Organics Cold Traps
Input
Product
Reboiler
Input
Vent
Vent
pumped out
Buffer Volume
Transportation cylinder racks
Booster
Condenser
Booster
Storage
Product
Oxygen Getter
Input
Product
Cryogenic Distillation Column (CDC)
Colorado gas
3-6% Ar, 1-10% N2, 85-95% He
After He separation
order-of: 40% Ar, 60% N2
Final Product
~100% UAr
Issue #1
Removes helium
Issue #2
Removes freeze-out Impurities
Issue #7
Removes Oxygen
Issues #3,4, & 5
Distillation Column repairs and upgrades
Recover UAr from He
Issues #6
Distillation to remove Methane

## Slide 16: Where we stand with UAr mass
UAr cylinders mass total – 106.4 kg
UAr mass waiting for purification
  in buffer waiting for Distillation Column – 18.3 kg
  extracted in Colorado waiting for shipping – 5.3 kg
Mass requiring reprocessing – 75.0 kg
  recovered from CH4 and O2 distillation
  emergency recoveries
  did not effectively remove N2 or O2
  TOTAL UAr MASS – 152.5 kg
  152 kg required for DarkSide-50

## Slide 17: Final Polishing
UAr requires final polishing to become detector grade
Using heated Zirconium getters from SAES
1 getter column is enough for our estimated contamination levels (second is backup)
We will run all the UAr through the getters at one time
Under construction  expected ready for operation 1 month
Typical contamination in all UAr cylinders | 
Contaminant | Concentration
CO2 | 25 ppm
CH4 | 114 ppm
N2 | 80 ppm
O2 | 250 ppm
All gas analysis performed by Pacific Northwest National Lab

## Slide 18: Verifying UAr detector usability
Could there be a contaminant that makes it through all purification steps and is below our sensitivity?
Verify our UAr can scintillate and drift e- - before putting into DarkSide50
Using Scene-LAr detector – small dual phase TPC
  Discussion to come – Hugh Lippincott

## Slide 19: Schedule and conclusions
Schedule for Darkside-50 UAr target
  Production and validation of DarkSide target by end of year
Conclusions
  A reliable source of low-radioactivity argon has been established
  Extraction and purification of the UAr is possible on a large scale
  However, there have been issues along the way
  AND, we still have not shown that our UAr is detector grade
Future
  DarkSide would like to expand to a 1+ ton detector
  DEAP-3600 target (?)
  G3 argon detector
    single or dual phase
    50 ton (?)
  Need 100 kg/day source --- negotiations with Air Products
    In 2015 Air Products will extract He from the same CO2
>150 kg UAr collected
The world’s supply

## Slide 20: Future
UAr consumers:
  DarkSide would like to expand to a 1+ ton detector
  DEAP-3600 target (?)
  G3 Dark matter Argon detector
    single or dual phase?
    50 ton (?)
  Continuous consumer: low level radiation detection  negligible amounts
Bottom Line: We need 100 kg/day purified UAr
  Negotiations with Air Products to extract UAr from new He plant
  (In 2015 Air Products will extract He from the same CO2 as we are using)
  What can they provide us?
    Pure UAr?
      Almost certainly not
    UAr-N2-O2 mix? – Will there be CH4?
      Current R&D to produce DarkSide-50 target has been invaluable
      Build on current experience to create new plant – further R&D required
  Are there other sources of low radioactivity argon?  requires further investigations