## Slide 1: High-temperature superconducting (Bi-2212) magnet technology suitable for building final cooling solenoids for a muon collider and the conductors they depend on
Tengming Shen, Fermilab, presented at Muon Accelerator Program collaboration meeting, Stanford Linear Accelerator Center, December 5, 2014
With inputs from Pei Li (Fermilab), Liyang Ye (Fermilab & NCSU), Gene Flanagan (Muons Inc.), John Tompkins (Fermilab), Lance Cooley (Fermilab), and with collaboration with VHFSMC and BSCCo

## Slide 2: Muon collider designs demand 30-50 T solenoids
NMR communities need 30 T all superconducting magnets.
Challenges to 30+ T HTS magnets:
  Understand the complex HTS material behavior
  High Jc at 20-50 T is the key.
  Stress management and quench protection.
(Courtesy of J. Jiang)
Notes: A transformational opportunity for high-field science
  But it is also a quantum leap in technology
  Resistive magnets take 30 MW to reach 45 T;
  LTS conductors mature, reaching their limits at ~20 T.

## Slide 3: Magnet programs based on REBCO coated conductor
15 T / 250 mm
bore LTS magnet
17 T REBCO coils
NbTi
Nb3Sn
32 T NHMFL all superconducting
user magnet. Commissioning expected
in 2016
Cold Bore 32 mm
Uniformity 1 cm DSV 5·10-4
Total inductance 254 H
Stored energy 8.6 MJ
Courtesy of NHMFL
Superpower REBCO archietecture

## Slide 4: The secret to high Jc in industrial powder-in-tube wire: Removing porosity
Gas bubbles

## Slide 5: Jc in short-length samples was then quickly taken to 3500 A/mm2 using cold densification methods
Sample | Jc(4.2K, 5T) | Je(4.2K,20T)
PIT wires | 2000 A/mm2 | ~340
PIT+CIP wires | 3500 A/mm2 | ~530
Regular PIT wires, quenched@887C
PIT+CIP wires, quenched@887C
Cold isostatic processing of Bi-2212: Jiang et al. Supercon. Sci. Tech., 24, 082001 (2011)
Swaging of Bi-2212 (S. Hong HJC Enterprise, SBIR phase I): Jiang et al. IEEE Trans Appl. Supercond. 23, 6400206 (2013)

## Slide 6
For 20 years, the performance of long length Bi-2212 wires has been much worse than in short pieces.
Short pieces: JE=500 A/mm2 at 4.2 K and 20 T
Long pieces: JE<200 A/mm2 at 4.2 K and 20 T
Mysterious leakage appearing in long length wires during the forming reaction.
(U. Trociewitz, NHMFL)
Macor
NHMFL, 1999,
3 T insert
from tape
OST, 2006

## Slide 7
Internal gases are the culprit of the low Jc and leakage in the long-length wires
Gas species detected by a residual gas analyzer while heating Bi-2212 wires at 180 °C/h in vacuum.
Shen et al., J. Appl. Phys., 113,
213901 (2013)
Key understanding:
Silver creeps outward, producing more porosity in 2212 and lowering Jc in long-length wire
Leakage is a natural consequence of the creep rupture of AgMg at the strain of ~3%.

## Slide 8
10 bar OP; JE=252 A/mm2 at 33.8 T (coil quenched). Add 2.6 T to 31.2 T background.
Larbalestier et al.,
(Nature Materials, 2014)
12/5/14
8
Breakthrough in Jc: JE of 700 A/mm2 at 4.2 K and 20 T
New paradigm: Overpressure processing
Pi
Po
Po
Po
Po
Po
Po
Po
Po

## Slide 9: Zoo of Overpressure Processing Furnaces
Sumitomo Bi-2223 300 bar OP furnace: +/- 1C in a sample space of 1 m diameter x 1.2 m height
3.5 m
FSU – OP furnace: Hot Zone: 15 cm dia, 50 cm high at up to 100 bar (1 bar pO2)
Fermilab
FNAL 100 bar OP system
Hot zone – 16 cm x 50 mm diameter
OP 2-layer coil; conductor
length=11 m; nGimat insulation
Courtesy of NHMFL

## Slide 10: Prototype OP solenoids yielded Ic that is 2-2.6 times that of 1 bar solenoids
Muons Inc – Fermilab, U.S. DOE-OHEP STTR project
OP coil Ic(5 T)=250-320 A vs. typical 120±40 A in 1 bar coils (0.8 mm strand)
  400 A for the best witness sample (JE=900 A/mm2)
No electrical shorts – nGimat TiO2 insulation works well.
Survive more than 120 heater-induced quench using detect-and-dump technique.
OP 2-layer coil; conductor
length=11 m; nGimat insulation

## Slide 11: Jc – axial stress/strain relations for Bi-2212
Ag/Bi-2212 is mechanically weak and its Jc is sensitive to strain.
  High-strength, kA-class Bi-2212 cables
Yielding stress – 120 MPa

## Slide 12: Development of high-strength, kA-class Bi-2212 cables for high field magnets
High strength
Bi-2212 6+1 cable
Bi-2212 wire
Fe-Cr-Al
TiO2
coating
10 bar overpressure processing increased the Jc by 4 times.

## Slide 13: Quench degradation limit - A large pool of wires, including OP wires, shows a consistent Ic/Ico-Tmax behavior – conductor is safe below 350 K during a quench
OST 0.8 mm, 37x18
Ic(s.f)=450A
Bench marker
OST 1.0 mm, 27x7
Ic(s.f)=150A
No Bridging
OST 1.2 mm, 85x18
Ic(s.f)=950A
Liyang Ye, PhD thesis work
Justin Schwartz, Tengming Shen

## Slide 14: An all superconducting 30 T magnet design using overpressure processed Bi-2212
NbTi
Nb3Sn
HTS
LTS (19 T, 200 mm cold bore) and HTS on independent PS.
Jave(HTS coil)=240 A/mm2
Je(HTS wire)=283 A/mm2

## Slide 15: Stress management of the coil seems feasible
HTS inserts
2212
S.S. reinforcement
2212 – hoop stress less than 135 MPa
S.S. reinforcement

## Slide 16: Quench protection of the insert coils constructed from kA-cable seems feasible
HTS on a PS
Jave(HTS coil)=240 A/mm2
Je(HTS wire)=283 A/mm2
JAg(HTS wire)=376 A/mm2
Quench protection time constant=0.10 sec
Design 1: 1.2 mm wire, Io=271.3 A, Coil inductance – 1 H, dump resistor needs to be 10 ohm, ground voltage=2713 V – Not OK
Design 2: cable, Io= 1357 A, , Coil inductance – 0.04 H, dump resistor needs to be 0.4 ohm, ground voltage=543 V - Good
Detect-and-dump
Iwasa, Case studies in
superconducting magnets

## Slide 17: Summary
Bi-2212 is now a magnet-grade conductor.
  JE reaches 700 A/mm2 at 4.2 K and 20 T and 500 A/mm2 in prototype coils
Magnet technology is getting ready for a big-time show
  Insulation is good.
  Quench detection is feasible.
  Quench degradation limit - >350 K
A conceptual design of an all superconducting magnet for the final cooling of muon collider
  A feasible design with the use of the high-strength, kiloamphere cable developed for stress management and fast quench protection

## Slide 18: Supplement slides – quench detection and protection

## Slide 19: MQE determined from heater-induced quench experiments: a master plot
[1] Ye et al., SuST, 2013
[2] Yang et al., IEEE, 2012

## Slide 20: NZPV determined from heater-induced quench experiments: a master plot
[1] Trociewitz, SuST, 2008
[2] Ye et al., SuST, 2013

## Slide 21: Though comprised by the slow normal zone propagation, quench detection using resistivity voltage across a normal zone is still feasible
Temperatures derived from voltages across the 1.5 cm hot zone:
4.2 K, 7 T, coil experiment
Note: Temperature from voltage measurement, not from TCs.
TCs tend to underestimate Tmax when dT/dt>10 K/s.
1 bar processing 6-layer coil