## Slide 1: MQXF Quench Protection
G. Ambrosio
on behalf of the MQXF team
With special contribution by:
S. Izquierdo Bermudez, V. Marinozzi,
E. Ravaioli, T. Salmi, M. Sorbi, E. Todesco, …
HiLumi - LARP Collaboration Meeting
May 11-13, 2015
FNAL
Note: all results are preliminary

## Slide 2: Outline
Introduction
  Requirements
  Configuration
  Lay-outs
  Heaters
  CLIQ
Codes & Validation
Results
  Hot Spot Temperature
  Voltages

## Slide 3: MQXF Main QP Parameters
 | Unit | Value
Operating temperature | K | 1.9
Operating current | kA | 16.5
Peak field at op. current | T | 11.4
Op. overall current density | A/mm2 | 462
Stored energy/length | MJ/m | 1.17
Inductance/length | mH/m | 8.21
Dump resistor | W | 50
Heater units per magnet |  | 12
Heater units per magnet |  | 8
CLIQ units per magnet |  | 1 or 2
Baseline
Peak field including strand self field

## Slide 4: Quench Protection Requirements
Hot Spot Temperature < 350 K
  Target in operating condition: T < 300 K
Detection:
  Validation time in LHC: 10 ms
  Threshold: 100 mV
Delays:
  Current switch opening: 3 ms (~10 ms w present switch)
Max voltage Coil to Ground: 1 kV
  Target Max voltage at leads due to dump: < 825 V

## Slide 5: Quench Protection Configuration(s)
Baseline: Heaters on Inner & Outer Layers
  To show redundancy: many heater failure scenarios
Alternative: Heaters on Outer Layers + CLIQ
  To show redundancy: CLIQ

## Slide 6: Lay-outs
Q1
Q2a
Q2b
Q3
Two layouts for baseline design:
  Operation = Q1 & Q3 in series; Q2a & Q2b in series
    At operating current;
  Single magnet test (Q2)
    At higher than operating current during demonstration phase
Layout with diodes for CLIQ

## Slide 7: Heaters for MQXF
With copper-cladding
Trace with perforations
Several options
  Baseline: heaters used on MQXFS1 coils 103 & 104
Courtesy J. C. Perez
Courtesy M.Marchevsky, E.Todesco, D.Cheng, T.Salmi
If the 11T project successfully demonstrates inter-layer heaters,
we will be happy to test them
M. Marchevsky, "Design optimization and testing of the protection heaters for the LARP high-field Nb3Sn quadrupoles", presented at ASC2014.

## Slide 8: Post-HQ02b Test: Bore, viewed from RE
Coil 16
Coil 17
Coil 20
Coil 15
Heater bubble
Heaters on the Inner Layer may develop bubbles during operation

## Slide 9: Post-HQ02b Test: Bore, viewed from RE
Coil 16
Coil 17
Coil 20
Coil 15
Crazing/cracking of epoxy
Note: HQ02 was quenched many times, including several High-Temperature quenches

## Slide 10: CLIQ - I
Coupling-Loss Induced Quench System
Very effective on HQ02 test
Courtesy of E. Ravaioli
E. Ravaioli, et al., “Protecting a Full-Scale Nb3Sn Magnet with CLIQ, the New Coupling-Loss Induced Quench System”, to be published in IEEE Trans. Appl. Supercond. 2015.

## Slide 11: CLIQ - II
Very effective at mid-high current
Courtesy of E. Ravaioli
E. Ravaioli, et al., “Protecting a Full-Scale Nb3Sn Magnet with CLIQ, the New Coupling-Loss Induced Quench System”, to be published in IEEE Trans. Appl. Supercond. 2015.

## Slide 12: CLIQ Plans
Could provide perfect redundancy with heaters on outer layer
  In case of “bubble” issue with heaters on inner layer
To be demonstrated for long magnets:
  MQXFS1 with reduced CLIQ voltage
  MQXFL1 (4m) with reduced CLIQ voltage for sim. Q2
Study of “tunnel readiness” in progress:
  CLIQ units redesigned to improve safety
  Using diodes for magnets powered in series

## Slide 13: Codes and Validations

## Slide 14: CoHDA: Code for Heater Delay Analysis
Heat conduction from heater to the superconducting cable
Quench when cable reaches Tcs(I,B)
Each coil turn considered separately
  Symmetric heater geometry: Model half of the heater period
  2-D model (neglect turn-to-turn)
Thermal network method
Details: T. Salmi et al., ”A novel computer code for modeling quench protection heaters in high-field Nb3Sn accelerator magnets”, IEEE TAS 24(4), 2014
PH coverage / 2
PH period/ 2
H e a t
y, radial (in cosθ)
z, axial
by Tiina Salmi

## Slide 15: Validation using comparison with
Analytical solution for 1D case with constant material properties – OK.
Commercial FEM software COMSOL for a full heater simulation case (collaboration with Juho Rysti, CERN) – OK.
Experimental data from HQ01e, HQ02a-b, HD3b, and 11 T
  Outer layer heaters: Agreement within 20% for Imag above 50% of SSL
  Inner layer heaters have larger uncertainty: up to ~50% for Imag above 50% of SSL
  Details: T. Salmi et al., ”Analysis of uncertainties in protection heater delay time measurements and simulations in Nb3Sn high-field accelerator magnets”, accepted for publication in IEEE TAS (pre-print from tiina.salmi@tut.fi)
New heater design tested in LHQ,
Agreement with simulation with 10%

## Slide 16
QLASA*
QLASA[1] is a program developed by the University of Milan and the INFN/LASA for the simulation of quench evolution in solenoids.
Main features:
Pseudo-analytical: quench propagation is based on Wilson analytical formulas[2]; thermal calculations are made solving the heat equation in adiabatic approximation.
Magnetic field is given as input
  It is possible to simulate magnetic quadrupoles or other kind of magnets
Magnet inductance is given as input
  Iron saturation can be simulated
  It is possible to simulate dynamic effects (reduction of the inductance[3])
Protection circuit with external dump resistor
It is possible to simulate protection heaters with heating stations[4]
Material properties from MATPRO[5]
[1] “QLASA: a computer code for quench simulation in adiabatic multicoil superconducting windings”, L. Rossi and M. Sorbi, 2004.
[2] “Superconducting magnets”, M.N. Wilson, 1983.
[3] “Effect of coupling currents on the dynamic inductance during fast transient in superconducting magnets”, V. Marinozzi et al., 2015.
[4] “Guidelines for the quench analysis of Nb3Sn accelerator magnets using QLASA”, V. Marinozzi, 2013.
[5] “MATPRO upgraded version 2012: a computer library of material property at cryogenic temperature,” G.Manfreda et al., 2012
*
Slides by V. Marinozzi

## Slide 17
Validation of quench detection time and protection heaters simulations has been made for Nb3Sn quadrupoles, using experimental data from LQ and HQ (LARP prototype quadrupoles for MQXF)
Very good agreement
It is the first quench protection simulation program, based on Wilson’s method, which can simulate the effects of coupling currents on the magnet inductance

## Slide 18: Modelling strategy with SuperMagnet
“Break" the complex problem in simpler building blocks that are solved separately and then "joined" into a consistent solution.
The “key” ingredients are:
Longitudinal quench propagation
  Important because it determines the time needed to detect a normal zone
  Needs an accurate modelling. Heat equation is solved implicitly in space (finite elements) and time (multi-step finite differences) using an adaptive mesh algorithm to cope with the large disparity of length scales.
Heat transfer from heater to coil
  Important because it defines the time needed to induce a distributed quench
  Solved separately using a 2D FE COMSOL model and joined to the global solution.
Heat transfer within the coil
  Important because it determines the time needed to quench the whole magnet cross section
  Longitudinal conductor model coupled explicitly with a 2nd order thermal network.
SUPERMAGNET [Bot 2007]
What is not (yet) included in the model:
AC loss
Other transient effects, such as change of the apparent inductance due to dI/dt
By S. Izquierdo Bermudez

## Slide 19: Modelling heat propagation within the coil
Two principal directions:
1. Longitudinal
Length scale is hundreds of m
2. Transverse
Length scale is tenths of mm
Power exchanged between components in the conductor
Joule heating
External heat perturbation
The conductor is a continuum solved with accurate (high order) and adaptive (front tracking) methods
Longitudinal
Transverse
Power exchange between adjacent conductors
2nd order thermal network explicitly coupling with the 1D longitudinal model:
T
Mesh density
SUPERMAGNET [Bot 2007]

## Slide 20: Model Validation
Longitudinal quench propagation MQXF cable
Current decay and resistance growth in 11T-DS dipole
Hot spot temperature in SMC-11T
Quench heater delay in 11T-DS dipole
With the key contribution of H. Bajas, J. Fleiter, J. Rysti and G. Willering

## Slide 21: LEDET (Lumped-Element Dynamic Electro-Thermal) model and QSF
E. Ravaioli - CERN May 2015
2D model, magnet volume discretized in blocks corresponding to 1-3 turns
Novel, elegant modeling technique to model dynamic effects in a superconducting magnet
Emphasis on dynamic effects
    Inter-filament and inter-strand coupling losses
    Magnet differential inductance depending on current ramp-rate and frequency
    All energy transfers between electrical and thermal domains accounted for.
Includes models of QH and EE
Quench Simulation Framework (QSF), developed by M. Maciejewski and E. Ravaioli, used at CERN for quench simulation, CLIQ optimization, and LHC circuit modeling (20k+ simulations)
References
E. Ravaioli, “CLIQ”, PhD thesis, Chapter 4, June 2015, to be published.
E. Ravaioli et al., “Lumped-Element Dynamic Electro-Thermal model of a superconducting magnet”, CHATS-AS 2015, to be published.
M. Maciejewski et al., “Automated Lumped-Element Simulation Framework for Modelling of Transient Effects in Superconducting Magnets”, International Conference on Methods and Models in Automation and Robotics, to be published.
Open questions leading to the development of LEDET model – (Emphasis on dynamic effects)
How to reliably predict the complex electro-dynamic and thermal transients following a CLIQ discharge?
Why does the magnet differential inductance change with current ramp-rate? And with the frequency? How to model this?
Can inter-filament and inter-strand coupling losses help protecting a magnet? How much?
Can we use the same simulation environment to model macroscopic electrical transients and phenomena occurring at the level of superconducting strands?
By E. Ravaioli

## Slide 22: Validation – CLIQ discharge in the quad model magnet for the high luminosity LHC
E. Ravaioli - CERN May 2015
Current in the two sides of the magnet
Current introduced by CLIQ

## Slide 23: Results

## Slide 24: Hot Spot Temperature with Quench Heaters
IR quads in the LHC tunnel: 270 K
Single Q2 in test facility showing redundancy:
3 Q2 HFU non-operational
IR quads in the LHC tunnel showing high redundancy: 8 Q2 HFU non-operational
SuperMagnet: 270 K
Computed with QLASA by V. Marinozzi
(SuperMagnet by S. Izquierdo Bermudez)

## Slide 25: Parameters used by QLASA
Three heaters have been deactivated in one coil
Triplet in LHC
Q2 in test facility
Cu/NonCu = 1.1, which is the worst case for nominal Cu/nonCu = 1.2 +/- 0.1

## Slide 26: Hot Spot Temperature with CLIQ
Computed with LEDET by E. Ravaioli
Hot Spot Temp:
Adiabatic approximation
Peak field
Assuming diodes across each magnet and one CLIQ unit per magnet
Hot Spot Temperature: CLIQ only: 251 K
CLIQ + OL HT: 231 K

## Slide 27: Peak Voltages (operation layout)
 |  | Leads | Coil-Ground* | Layer-Layer | Midplane-Midplane | Turn-Turn
 |  | (V) | (V) | (V) | (V) | (V)
Q1-Q3 | Nominal | 800 | 970 / 570 | 201 | 151 | 24
 | OL heaters only | 800 | 1152 / 752 | 265 | 151 | 39
 | HF-OL coil 1 heater fail | 800 | 991 / 591 | 237 | 177 | 25
 | All coil 1 heaters fail | 800 | 1571 / 1171 | 937 | 855 | 31
Q2a-Q2b | Nominal | 800 | 677 | 273 | 335 | 37
 | OL heaters only | 800 | 780 | 361 | 357 | 58
 | HF-OL coil 1 heater fail | 800 | 661 | 394 | 319 | 40
 | All coil 1 heaters fail | 800 | 1369 | 1481 | 1131 | 47
 |  | Coil-Ground | Layer-Layer | Midplane-Midplane | Midplane IL - Midplane OL | Turn-Turn
 |  | (V) | (V) | (V) | (V) | (V)
Q2 | CLIQ + OL heaters | 500 | 500 | 500 | 1000 | 35
 | CLIQ | 530 | 500 | 500 | 1000 | 47
* For Q1-Q3: 1st case assumes ground on a lead; 2nd case assumes symmetric grounding
Can be prevented by having each heater of a coil connected to a different HFU =
6 HFU / 2 coils
Note: all results are preliminary
V. Marinozzi ROXIE
E. Ravaioli
LEDET

## Slide 28: Conclusions
The Hot Spot temperature appears under control in all scenarios:
  Lowering the operating current helped a lot
  Test of MQXFS1 will provide info for decision about IL heaters vs. CLIQ; overall system optimization & cost may be other important factors
The analysis of peak voltages is in progress:
  Showing importance of large number of HFUnits
  Could be important factors for choice of QP system

## Slide 29: BACKUP SLIDES

## Slide 30: First Attempt (presented at MT23)
Simulations performed with QLASA and ROXIE using MATPRO property database
  Using preliminary MQXF requirements
  Assuming heaters only on the outer layer
  With conservative assumptions
    Slow layer-layer propagation
    Only copper (no bronze) in strands
    No dynamic effects
 Hot spot temp. ~ 350 K (max acceptable temp.)
  Without margin and redundancy
G. Manfreda, et al., “Quench Protection Study of the Nb3Sn low-beta quadrupole for the LHC luminosity upgrade,” IEEE Trans. Appl. Supercond., vol. 24, no. 3, Jun. 2014, Art. ID. 4700405.
G. Ambrosio, “Maximum allowable temperature during quench in Nb3Sn accelerator magnets”, Yellow Report CERN-2013-006, pp. 43–46, WAMSDO 2013, CERN, Geneva, CH.

## Slide 31: Feedback from HQ02 test
Measurement of quench propagation OL to IL
Measurement of Quench Integral vs. dump res.
Degradation vs. Hot Spot temperature (incomplete)
H. Bajas, et al., “Cold Test Results of the LARP HQ02b magnet at 1.9 K”, to be published in TAS
120 mm aperture, 1 m long quadrupole
Reached 98% SSL at 4.5K & 95% SSL at 1.9K

## Slide 32: HQ02 – Max Hot Spot Temperature
380+ K hot spot temperature without significant degradation
H. Bajas, G. L. Sabbi, G. Chlachidze, M. Martchevsky, F. Borgnolutti, D. Cheng, H. Felice, et al.

## Slide 33: Protection Heater Studies
Both heaters are very efficient (delay < 10 ms) at operating current
Similar performance under similar conditions
B01
B02
G. Chlachidze, 11/14/14 LARP Mtg
Analysis in progress

## Slide 34
MQXF protection scheme
MQXF Quench Protection Analysis – Vittorio Marinozzi
Dumping resistance | 48 mΩ
Maximum voltage to ground | 800 V
Voltage threshold | 100 mV
Validation time | 10 ms
Heaters delay time from firing (inner layer) (CoDHA)[1] | 12 ms
Heaters delay time from firing (outer layer) (CoDHA)[1] | 16 ms
[1] T. Salmi et al., “A Novel Computer Code for Modeling Quench Protection Heaters in High-Field Nb3Sn Accelerator Magnets”, IEEE Trans. Appl. Supercond. vol 24, no 4, 2014.

## Slide 35
MQXF protection with IL-PH
MQXF Quench Protection Analysis – Vittorio Marinozzi
No inner layer PH | Inner Layer PH
330 K | 290 K
The MQXF hot spot temperature decreases of ~40 K inserting inner layer protection heaters
Dynamic effects are not yet considered in these simulations

## Slide 36
Updated MQXF protection w and w/o IFCC
MQXF Quench Protection Analysis – Vittorio Marinozzi
No inner layer PH | No inner layer PH+ IFCC | Inner Layer PH | Inner Layer PH + IFCC
330 K (365 K) | 306 K (342 K) | 290 K (311 K) | 266 K (288 K)
IFCC dynamic effects decrease the MQXF hot spot temperature of 20-30 K. The effect is therefore appreciable, but we do NOT take it into account because it is not yet demonstrated in MQXF magnets, and the powering system is still under design.
Further improvements could come from quench back, which has not been considered (work in progress)
The numbers between parentheses show impact of failure of half of the heaters

## Slide 37
Protection assumptions | 
Voltage threshold | 100 mV
Dump resistor | 46 mΩ
Validation time | 10 ms
IL heaters | Yes
Dynamic effects | yes
Quench back | no
MQXF Quench Protection Analysis – Vittorio Marinozzi & Tiina Salmi
Peak Temperature vs. Location and Current