## Slide 1: Structure Session Outline
From HQ to MQXFD1 Hélène Felice
Lessons learned at LBNL Dan Cheng
Experience from MQXFD0 Mariusz Juchno
Preliminary Target for MQXFS1 assembly Hélène Felice

## Slide 2: From HQ to MQXFD
H. Felice – D. Cheng – M. Juchno – P. Ferracin

## Slide 3: Outline
HQ01 to HQ03
  Preload history
MQXFD1 assembly and cool-down
  Structure validation
  Recommendation toward MQXFS1
2010
2011
2012
2013
2014
HQ01a-b-c
HQ01d-e
HQ02a-b
HQ03
2015

## Slide 4: Preload Challenges
Objective 1
  Preload the magnet to avoid coil/pole detachment at operating condition
  While remaining conservative
    Safe azimuthal stress range defined by TQS03 study
Objective 2
  Maximize alignment
    Pole key to collar gap
Yoke master
Pad
master
Al alloy bolted collars
Pad master to yoke master

## Slide 5: Typical Assembly steps
Ground plane insulation layout
Coil CMM measurements
Nominal Radial shims
Nominal pole key shims
Actual coil OD
Fuji paper inspection
Measurement of pole gap dimensions along the length using measurement pins
OK
Assembly with Fuji paper
No shimming of the pole key
Actual pole key shims
Actual radial shims
Kapton
G10

## Slide 6: Typical Assembly steps
Ground plane insulation layout
Coil CMM measurements
Nominal Radial shims
Nominal pole key shims
Measurement of pole gap dimensions along the length using measurement pins and feeler gages
Assembly with actual G10 and Kapton radial shims
Actual pole key shims
Pole shims
Actual radial shims
Actual coil OD
Assembly
2 possible regimes:
Pole key to collar contact or no contact

## Slide 7: HQ Preload overview
 | HQ01a/b | HQ01c | HQ01d | HQ01e | HQ02a-a2 |  | 
Target preload to |  | 219 T/m | 200 T/m |  | 200 T/m |  | 
eq shell target (300/4.2K) |  | 1028/2086 me | 863/1905 me |  | 863/1905 me |  | 
eq pole target (300/4.2K) |  | -536/-828 me | -450/-720 me |  | -450/-720 me |  | 
Coil generation |  | 1 overcompacted | 1 overcompacted |  | 2 |  | 
Comment |  | Mid-plane quenches | Pole unloading in one coil |  |  |  | 
Axial preload:
sz rod = 60 / 160 MPa
ez rod = 880 me / 2000 me
Axial preload was never an issue in HQ
Likely related to coil fab
Lack of magnet performance
prevents from checking other coil preload
HQ01 disregarded
HQ02: reference magnet

## Slide 8: HQ02a Behavior
Test performed at FNAL, Guram Chlachidze
Training slows down at 15 kA = 170 T/m
A possible explanation:
Lack of preload starts at 15 kA => more interception than predicted by model
Coil SG behavior unreliable during test (See Dan Cheng’s talk)
Preload increase for HQ02b was based on shell SG measurement and training performance

## Slide 9: HQ Preload overview
 | HQ01a/b | HQ01c | HQ01d | HQ01e | HQ02a-a2 | HQ02b | 
Target preload to |  | 219 T/m | 200 T/m |  | 200 T/m |  | 
eq shell target (300/4.2K) |  | 1028/2086 me | 863/1905 me |  | 863/1905 me | 1300/2300 me | 
eq pole target (300/4.2K) |  | -536/-828 me | -450/-720 me |  | -450/-720 me | -675 me | 
Coil generation |  | 1 overcompacted | 1 overcompacted |  | 2 | 2 | 
Comment |  | Mid-plane quenches | Pole unloading in one coil |  | Pole unloading | Reached 95% Iss | 
Starting at 15 kA (170 T/m)
More force interception?
Lack of SG at cold prevents comparison with model
Preload adjusted based on test performance
Sufficient to 95% at 1.9 K
Axial preload:
sz rod = 60 / 160 MPa
ez rod = 880 me / 2000 me
Axial preload was never an issue in HQ
Likely related to coil fab
Lack of magnet performance
prevents from checking other coil preload

## Slide 10: HQ02b Preload and stress summary
Azimuthal stress (MPa)
4.2 K
Azimuthal stress (MPa)
205 T/m – 18.2 kA – 1.9 K HQ02 Iss
Azimuthal stress (MPa)
188 T/m – 16.6 kA – 4.2 K HQ02 Iss
Coil SG at room T
Shell SG

## Slide 11: HQ02b performance
Chart: Quench #
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13
HQ02b - 1.9 K | 15126 | 15444 | 16127 | 16130 | 16351 | 16442 | 16616 | 16855 | 17069 | 17206 | 16775 | 17024 | 17162
HQ02a-2 - 2.2 K | 15072 | 15204 | 15147 | 15202 | 15248 | 15336 | 15409 | 15450 | 15460 | 15435 | 15605 | 15538 | 15608 | 15608 | 15685 | 15565 | 15600 | 15675 | 15745 | 15750 | 15718 | 15785 | 15832 | 15935 | 15902 | 15964 | 16004 | 16032
HQ02a - 4.5 K | 11882 | 13278 | 13700 | 13672 | 13690 | 13804 | 13727 | 14192 | 14184 | 14302
HQ02a - 1.9 K | 14662 | 14865 | 15000 | 14992
Test performed at CERN
Preload increase => Improved training rate in HQ02b
Azimuthal stress range: 180-200 MPa
Top-head limit
95% Iss – 195 T/m

## Slide 12: HQ Preload overview
 | HQ01a/b | HQ01c | HQ01d | HQ01e | HQ02a | HQ02b | HQ03
Target preload to |  | 219 T/m | 200 T/m |  | 200 T/m |  | HQ02b
eq shell target (300/4.2K) |  | 1028/2086 me | 863/1905 me |  | 863/1905 me | 1300/2300 me | 1300/2300 me
eq pole target (300/4.2K) |  | -536/-828 me | -450/-720 me |  | -450/-720 me | -675 me | -675 me
Coil generation |  | 1 overcompacted | 1 overcompacted |  | 2 | 2 | 2
Comment |  | Mid-plane quenches | Pole unloading in one coil |  | Pole unloading | Reached 95% Iss | 
Starting at 15 kA (170 T/m)
More force interception?
Lack of SG at cold prevents comparison with model
Preload adjusted based on test performance
Sufficient to 95% at 1.9 K
Axial preload:
sz rod = 60 / 160 MPa
ez rod = 880 me / 2000 me
Axial preload was never an issue in HQ
Likely related to coil fab
Lack of magnet performance
prevents from checking other coil preload

## Slide 13: HQ03
Same preload condition as HQ02b
Same expected stress distribution as HQ02b
SG procedure was fixed => 3 out of 4 coils
Rate of unloading
measured~ 450-500 me/108 kA2
ANSYS ~ 400 me/108 kA2
Coil EpsT (me)
I2
1st quench at 81.5 % at 1.9 K
Possible start of unloading in coil 26 uncorrelated to quench to be confirmed in HQ03a2
Test performed at FNAL, Guram Chlachidze

## Slide 14: Coil overall dimensions F. Borgnolutti (CM22 – May 2014)
+50 μm
-50 μm
Coil 23
Coil 22
Coil 20
Coil 17
Coil 16
+250 μm
-250 μm
All measurements performed with Zeiss
Bowed coils
Mid-plane under or oversized
Mid-plane consistency along the length
Lead End
Aligned on OD
Lead End
Absolute position

## Slide 15: Summary – part 1
From HQ:
  HQ02 and HQ03: coils consistent in terms of size
  HQ02 and 3 showed contact between collar and pole key
  HQ02 showed low preload potentially due to larger interception by the pole key
  Range of safe azimuthal stress reached in the HQ02b and HQ03: 180-200 MPa
  Appropriate level of preload to improve training

## Slide 16: MQXFD1
Motivation for ½ +1+ ½
  Minimize the stress variation
  along the coil: +/- 5 Mpa
Implemented in MQXFD1
76 mm pin slot
25 mm welding block gap
25 mm tool block
45 mm pin slot
385 mm
775 mm
385 mm
M. Juchno

## Slide 17: MQXFS structure procurement
2 structures procured by CERN
  MQXFD0 used at CERN
  MQXFD1 shipped to LBNL
Shell 1 + 1 initially
  Cut at LBNL ½ + 1 + ½

## Slide 18: Strain gauges
Station 1
Station 2
LBNL+CERN
Station 3
LBNL SG instrumentation
  On shell and dummy coils: Vishay Type WK-13-125PC-350/W
  DC current powered
  k factor variation not characterized on Vishay SG
CERN SG instrumentation
  On shell: HBM 1-LC11-6/350 (uniaxial)
  On dummy coils: HBM 1-XC11-3/350 (biaxial)
  AC voltage powered
  SG characterized at cold => k factor variation by 6.5 % from RT to 77 K and 8 % to 4.2 K
  (Report from Thibault Dijoud, CERN)
LBNL + CERN
In collaboration with M. Guinchard, P. GrosClaude, CERN,
EN/MME/Mechanical meas. Lab.

## Slide 19: MQXFD1 timeline
Feb 1st 2015
March 1st 2015
April 1st 2015
May 1st 2015
Yoke-shell subassembly completed
Collar pack with Fuji paper completed
Final coil pack completed
MQXFD1 Preload completed
MQXFD1 77K test completed

## Slide 20: Coil pack assembly
Zposition RE to LE | 1290 | 980 | 680 | 380 | AVG | AVG (mm)
Height side 1-2 | 12.539” | 12.545” | 12.547” | 12.54” | 12.54275” | 318.59
Height side 4-3 | 12.545” | 12.544” | 12.547” | 12.548” | 12.546” | 318.67
Width side 1-4 | 12.541” | 12.55” | 12.553” | 12.541” | 12.54625” | 318.67
Width side 2-3 | 12.556” | 12.553” | 12.563 | 12.553” | 12.55625” | 318.92
1
2
3
4
Radial shim: 1.57 mm (1.62 mm target)
Pole key gaps: none except one quadrant 230 mm
  ~60 mm per quadrant
Nominal pack size: 319 mm
Actual pack smaller than nominal by about 150 mm per side
Actual coil pack size wider at the bottom

## Slide 21: Shell eq versus time (LBNL SG data)
All bladders at 1500 psi (10.3 MPa)
All bladders at 3000 psi (20.6 MPa)
All bladders at 4000 psi (27.6 MPa)
Bladder pressure by quadrant
Max: 4000 psi (27.6 MPa)
Gap keys tight
Effective shim: 460 mm
Load keys: 13.556 mm
Average strain: 923 +/- 35 me

## Slide 22: Coil station 2 eq versus time (LBNL data)
Average azimuthal strain
-1457 +/- 58 me

## Slide 23: MQXF Loading Transfer function LBNL and CERN data
Station 1
Station 2
Station 3
CERN -1416 +/- 92 me
-1457 +/- 58 me
Coil preload consistent with a “no-pole key” case
Alignment within 60 microns

## Slide 24: Axial Preload
Rods Adjustment
Average axial strain
830 +/- 34 me

## Slide 25: MQXFD1 preparation for cool-down

## Slide 26: Shell Strain
Good consistency between LARP and CERN Strain gauge data
ANSYS Model: f=0.3
  Some inconsistency axially
  0.2 < f < 0.3
Chart: Azimuthal strain (me)
| Azimuthal preload | Axial preload | Magnet on header | 77 K | Warm-up
SHTT | 896.8765 | 908.5086 | 894.2048 | 1577.2217 | 996.8504
SHRT | 888.3458 | 901.0569 | 888.7009 | 1572.7285 | 974.1953
SHBT | 948.4439 | 962.4745 | 951.2048 | 1550.4604 | 1038.02
SHLT | 959.2122 | 971.725 | 959.776 | 1685.1168 | 1012.1976
SHTT-CERN | 897 | 898 | 900 | 1457.665 | 987
SHRT-CERN | 897 | 901 | 903 | 1474.495 | 967
SHBT-CERN | 949 | 953 | 952 | 1512.83 | 1027
SHLT-CERN | 970 | 973 | 968 | 1582.955 | 1007
ANSYS | 870.5 | 873.1 | 873.1 | 1601.1 | 980.9
Chart: Axial strain (me)
| Azimuthal preload | Axial preload | Magnet on header | 77 K | Warm-up
SLTZ | -123.2289 | -120.6374 | -127.3501 | -191.164 | -257.2668
SLRZ | -123.2289 | -120.6374 | -127.3501 | -191.164 | -257.2668
SLBZ | -149.5862 | -148.6331 | -157.797 | -220.9515 | -307.7944
SLLZ | -161.5772 | -159.062 | -163.8737 | -161.9646 | -338.3927
SHTZ-CERN | -133 | -134 | -126 | -229.075 | -280
SHRZ-CERN | -150 | -152 | -148 | -223.465 | -325
SHBZ-CERN | -106 | -111 | -110 | -232.815 | -261
SHLZ-CERN | -155 | -157 | -150 | -84.15 | -322
ANSYS | -112.5 | -119 | -119 | -44.6 | -512.6

## Slide 27: Coil Strain
Good consistency between LARP and CERN Strain gauge data
Model: f=0.3
Good consistency overall
Chart: Azimuthal strain (me)
| Azimuthal preload | Axial preload | Magnet on header | 77 K | Warm-up
CL022T | -1418.5667 | -1395.6914 | -1407.5409 | -2144.1583 | -1290.3357
CL052T | -1390.205 | -1371.2753 | -1386.0627 | -2224.5866 | -1314.0343
CL062T | -1545.5638 | -1521.6116 | -1539.1499 | -2350.9934 | -1374.2486
CL072T | -1477.5196 | -1455.7229 | -1473.3874 | -2275.2383 | -1351.9213
C022T-CERN | -1391 | -1367 | -1370 | -2043.91 | -1300
C052T-CERN | -1324 | -1303 | -1310 | -2080.375 | -1297
C062T-CERN | -1545 | -1518 | -1524 | -2254.285 | -1405
C072T-CERN | -1407 | -1372 | -1366 | -2035.495 | -1298
ANSYS | -1258 | -1254 | -1254 | -2009 | -1231
Chart: Axial strain (me)
| Azimuthal preload | Axial preload | Magnet on header | 77 K | Warm-up
CL022Z | 259.3118 | 238.4233 | 188.2769 | 1615.4721 | -40.2724
CL052Z | 302.3517 | 280.9659 | 224.7461 | 1637.7881 | -34.2983
CL062Z | 331.4118 | 311.8741 | 267.9266 | 1698.1833 | 17.9953
CL072z | 313.9921 | 297.1681 | 256.9468 | 1706.984 | 11.4057
C022Z-CERN | 171 | 140 | 105 | 1628.77 | -120
C052Z-CERN | 220 | 187 | 145 | 1627.835 | -85
C062Z-CERN | 270 | 243 | 210 | 1715.725 | -38
C072Z-CERN | 367 | 342 | 314 | 1783.98 | 57
ANSYS | 45 | 39 | 39 | 1295 | -496

## Slide 28: Shell Stress
Model: f=0.3
Axial stress below model computation
Optimal friction coefficient in the model being investigated
Chart: Axial stress (MPa)
| Azimuthal preload | Axial preload | Magnet on header | 77 K | Warm-up
SLTZ | 14.3613 | 14.9374 | 14.0289 | 30.8063 | 6.4337
SLRZ | 10.6959 | 11.2954 | 10.0883 | 28.4139 | 0.61937
SLBZ | 13.6652 | 14.1207 | 13.0718 | 27.3806 | 3.5424
SLLZ | 13.007 | 13.5555 | 12.8556 | 36.7288 | 0.53273
ANSYS | 14.5 | 14.1 | 14.1 | 44.7 | -14.2
Chart: Azimuthal stress (MPa)
| Azimuthal preload | Axial preload | Magnet on header | 77 K | Warm-up
SHTT | 67.6099 | 68.7706 | 67.4807 | 135.0244 | 71.8892
SHRT | 65.707 | 66.8894 | 65.6221 | 133.8548 | 68.472
SHBT | 70.9889 | 72.1325 | 70.9342 | 131.8698 | 73.7882
SHLT | 71.5218 | 72.6172 | 71.5494 | 145.6589 | 71.2359
ANSYS | 65.9 | 65.9 | 65.9 | 141.7 | 63.8

## Slide 29: Coil Stress
Model: f=0.3
Axial stress showing some inconsistency
Also seen in MQXFD0
Optimal friction coefficient in the model being investigated
Chart: Azimuthal sress (MPa)
| Azimuthal preload | Axial preload | Magnet on header | 77 K | Warm-up
CL022T | -105.1357 | -104.0788 | -106.2847 | -142.307 | -103.1457
CL052T | -102.0114 | -101.0142 | -103.6435 | -148.7137 | -104.8763
CL062T | -113.3743 | -112.0951 | -114.4788 | -158.422 | -108.192
CL072T | -108.4481 | -107.3355 | -109.6096 | -151.4954 | -106.6709
ANSYS | -98.5 | -98.3 | -98.3 | -140.3 | -98.3
Chart: Axial sress (MPa)
| Azimuthal preload | Axial preload | Magnet on header | 77 K | Warm-up
CL022Z | -17.5943 | -18.6972 | -22.9574 | 79.2379 | -3.7889
CL052Z | -13.5192 | -14.6772 | -19.5065 | 78.8226 | -3.8059
CL062Z | -15.3484 | -16.2811 | -20.1679 | 80.293 | -3.5526
CL072z | -14.8929 | -15.6923 | -19.281 | 83.3433 | -3.547
ANSYS | -30.4 | -30.8 | -30.8 | 54.5 | -72.6

## Slide 30: Rod axial Stress
Chart: Axial stress (MPa)
| Azimuthal preload | Axial preload | Magnet on header | 77 K | Warm-up
rod1 | 0 | 60.4814 | 57.9355 | 118.5216 | 53.1551
rod2 | 0 | 59.875 | 55.5803 | 113.047 | 47.9384
rod3 | 0 | 55.8147 | 54.0132 | 111.2297 | 48.3779
rod4 | 0 | 56.3064 | 52.6506 | 110.703 | 45.3013
ANSYS | 0 | 57.7 | 57.7 | 115.6 | 41.2
Model: f=0.3
Good consistency between model and SG data

## Slide 31: Summary
From HQ:
  HQ02 and HQ03: coils consistent in terms of size
  HQ02 and 3 showed contact between collar and pole key
  HQ02 showed low preload potentially due to larger interception by the pole key
  Range of safe azimuthal stress reached in the HQ02b and HQ03: 180-200 MPa
  Appropriate level of preload to improve training
From MQXFD1
  Mechanical model assembled and cooled-down at 77 K
  Alignment coil to structure achieved within 60 mm
  Consistency between LARP and CERN strain gauges measurements at warm and cold
  Consistency between Strain gages measurements and ANSYS model
    Fine tuning of the friction coefficient between 0.2 and 0.3 is required
    The friction coefficient affects marginally the coil preload
The stage is set for MQXFS1 assembly

## Slide 32: Back-up slides

## Slide 33: HQ03a preload summary Comparison with HQ02 Azimuthal preload
HQ03
eq shell avg meas= 1197+/-78 me
eq coil avg meas =-556 +/-91 me
HQ02b
eq shell avg meas= 1270+/-107 me
eq coil avg meas ~-600me

## Slide 34: HQ03a Cool-down Shell
Axial slippage
Average reached: 2079 me
Target: 2100 me

## Slide 35: Ramp to 15 kA 01/08/2015
SG Coil 23Z lost after cool-down
SG coil 23T lost during excitation
Signs of unloading in coil 26 => not quenching so far
Rate of unloading
measured~ 450-500 me/108 kA2
ANSYS ~ 400 me/108 kA2
Coil EpsT (me)
I2

## Slide 36: Coil pack insertion and master shimming
Load keys nominal: 13 mm (2x5+3)
Shimming calculated based on our coil-pack measurements:
  Load keys: 0.120” = 3.05 mm
  Bladders : 0.080” = 2.03 mm
Actual
Bottom master => calculated
Other masters
  => load keys shims: 0.100”
  => bladder shims: 0.060”
1st step of bladder => bring load keys shimming to nominal shimming

## Slide 37: Coil station 3 eq versus time (LBNL data)

## Slide 38: MQXF Loading Transfer function LBNL data per coil
Station 1
Station 2
Station 3

## Slide 39: Coil station 1 azimuthal strain

## Slide 40: Shell ez (LBNL data)