## Slide 1: Coil fabrication experience for the 1st generation SQXF coils
Susana Izquierdo Bermudez, Juan Carlos Perez, Eugenio Cavanna, Paolo Ferracin
Joint HiLumi LHC-LARP Annual Meeting/24th LARP Collaboration Meeting
12th May, 2015

## Slide 2: Outline
SQXF overview coil design & manufacturing process
SQXF coils production summary
Destructive inspection of coil 101
  Acknowledgments
TE/MSC
E. Cavanna, N. Bourcey, P. Ferracin, R. Gauthier, L. Lambert, J. Mazet, N. Perey, E. Rochepault, J. C. Perez, F-O. Pincot, M. Semeraro and S. Tavares.
EN/MME
B. Favrat, J. Parrilla, T. Sahner

## Slide 3: Outline
SQXF overview coil design & manufacturing process
SQXF coils production summary
Destructive inspection of coil 101

## Slide 4: Cable Insulation
Samples | Insulation thickness – Sample S1 (µm) | Insulation thickness – Sample S2 (µm) | Insulation thickness – Sample S3 (µm)
Coil 001 | 152 | 144 | 150
Coil 101 | 143 | - | 143
Coil 102 | 145 | 144 | 146
Coil 103 | 147 | 147 | 147
Coil 104 | 142 | 145 | 143
Measured insulation thickness within specifications
AGY S2-glass fibers
  66 tex with 933 silane sizing
32 bobbins
Variables: # of yarn per coil and of picks/inch
Target: 145 μm ± 5 μm per side

## Slide 5: Coil Insulation
2 x 0.175 mm S2 glass around winding pole
0.125 mm S2 glass sleeve around wedges
0.5 mm S2 glass inter-layer insulation
0.125 G11 + 0.125 polymide mid-plan shim (per quadrant)
250 µm coating on end parts
175 µm S2 glass between end parts and the cable

## Slide 6: Winding
Winding tension:
25 kg
Winding Direction Inner Layer
favourable (clockwise)
Winding Direction Outer Layer
unfavourable (anti-clockwise)
Winding Technique
winding tool used systematically
no binder applied on the ends
no twist applied on the cable
End parts
produced by SLS (mat. 316L).
slits to make parts flexible
coated using Al2O3
Wedges
two wedges per side and per layer, insulated using a 0.125 mm sleeve
(the two wedge segments are insulated in a unique sleeve)
No particular problems during winding

## Slide 7: Curing
Curing cavity designed considering the cable dimensions after heat treatment
Assumed growth during HT :4.5% (thickness), 2% (width)
  Bare width x thickness before reaction: 18.150 x 1.525 mm
  Bare width x thickness after reaction: 18.513 x 1.594 mm
Azimuthal additional room per side:
1.5 mm for the inner layer
1.9 mm for the outer layer
Quantity of ceramic binder:
Central part = 33 g (per layer)
Coil ends = 12 g (per end)
Curing cycle parameters:
Pressure to close the mould = 40 bars
Curing temperature = 150°C (2 hours)
Curing pressure
  60 bars for inner layer
  80 bars for outer layer

## Slide 8: Reaction
Step | Type | From temp [°C] | To temp [°C] | Rate [°C/h] | Duration [h] | Comments
1 | Ramp | 20 | 300 | 50 |  | 
2 | Dwell | 300 | 300 | 0 | 4.5 | 
3 | Cool-down | 300 | 210-215 |  |  | 
4 | Dwell | 210 | 210 | 0 | 48+15 | As requested by SCD
5 | Ramp | 215 | 500 | 50 |  | 
6 | Dwell | 500 | 500 | 0 | 1.5 | 
7 | Cool-down | 500 | 400 |  |  | 
8 | Dwell | 400 | 400 |  | 48+3.5 | As requested by SCD
9 | Ramp | 400 | 640-665 | 50 |  | 
10 | Dwell | 640 | 640 | 0 | 50+12 | As requested by SCD
11 | Cool-down | 640 | 20 |  |  | 
Coil 101 (practice coil, low grade Nb3Sn) was reacted three times to optimze the reaction oven parameters
  First full heat treatment
  2nd heat treatment done with short plateaus
  3rd heat treatment done only with first plateau
Take 103

## Slide 9: Splicing
Soldering alloy: Sn96Ag4
Soldering flux: MOB39 (non activated)
  Access to both sides of the Nb3Sn cable during splice operation to remove oxidation
Copper stabilizer in the NbTi connection lead

## Slide 10: Impregnation
Epoxy CTD 101 K | Temp [C°] | Time | Press. [mbar]
Bake out | 60 | 48 h (minimum) | ~10-3
Agitated Degas | 55-60 | 60 min | ~7.5x10-2
VPI (ΔP) | 60 | 25-35 min resin across mould 65-110 min in total | ~10-3 (chamber) 10-2 - 5x10-2 (mould) 500-800 (reservoir)
Gel |  | 3 h | ~10-3
Cure | 3 h ramp, 6 h at 110° C, 1 h ramp, 16 h at 125° C |  | 
In general, the quality of the impregnation is good

## Slide 11: Post-impregnation
After impregnation, quench heater and voltage taps wires are soldered to the pads.
The connection box is then impregnated with Ecobond (same material as the one used broadly in the LHC)

## Slide 12: Coils at different manufacturing stages
After curing
After reaction
After impregnation

## Slide 13: Outline
SQXF overview coil design & manufacturing process
SQXF coils production summary
Destructive inspection of coil 101

## Slide 14: SQXF coils production summary
Coil 001 | Coil 101 | Coil 102 | Coil 103 | Coil 104
Copper | Nb3Sn low grade | Nb3Sn | Nb3Sn | Nb3Sn
Practice coil | Practice coil | Spare coil | Coil for SQXF1 | Coil for SQXF1
Aim of the coil: Development manufacturing process Tooling Commissioning Electrical QA limits | Aim of the coil: Study of conductor position Coil ends validation Mechanical mock-up Electrical QA limits | Issues during production? Overshoot on the VAMAS during reaction treatment Problem on the splice | Issues during production? No | Issues during production? No
Coils for the first short model

## Slide 15: Pole gap
Coil # | Initial [mm] | After curing [mm] | Before HT [mm] | After HT [mm]
001 | 3 | 2.7 |  | 0.1
101 | 7.5 |  | 6 | 5.6
102 | 5 | 4.1 | 3.8 | 3.37
103 | 4.5 | 3.4 | 3.11 | 2.64
104 | 2 | 0.75 | 0.4 | 0.5
Gap reduces by 1.2 to 1.6 mm when releasing the winding tension.
During heat treatment, longituindal coil contraction 0.4 – 0.5 mm
For coil 104, no contraction of gap during heat treatment

## Slide 16: Overall coil dimensions
mm | Inner layer | Inner layer assuming pole gap =0 | Outer layer | Outer layer assuming pole gap =0
101 |  |  |  | 
102 | -- | -- | 5.4 | 2.03
103 | -- | -- | 9 | 6.36
104 | 4.65 | 3.9 | 5.16 | 4.66
Coil overlength (mm)
Coils are 2 – 5 mm longer than nominal
Coils are typically 100 µm smaller than nominal in the radial direction and about 200 µm smaller in the azimuthal direction
Average deviation from nominal radial thickness ~100 µm
Average azimuthal deviation ~100 µm
Average azimuthal deviation ~100 µm

## Slide 17: Electrical QA
Coils 001 and 101 have been used to check the limits in terms of coil electrical integrity.
  Discharge test coil 001~ 3.5 kV
  Discharge test coil 101> 5 kV
From coil 102, standard electrical tests
  Coil 102 passed all the tests (only a weak point on the insulation QH to end shoe)
  Coils 103 and 104 to be tested in the coming days
MQXF Set-point test |  | 
MQXFS_102 | coil | 
All QHs | 2500 / 2500 | All QHs
Endshoe CS | 1000 / 1000 | 2500/ 2500
Endshoe NCS | 1000/ 1000 | 2500/ 2000
Central post | 500 / 500 | 
U1 / U2 = MQXF Target (V) / measured (V)

## Slide 18: Outline
SQXF overview coil design & manufacturing process
SQXF coils production summary
Destructive inspection of coil 101

## Slide 19: Coil Ends – Coil 101

## Slide 20: Coil Ends – Coil 101
Comparison to nominal conductor position shows good agreement
(only small deviation in the last blocks)

## Slide 21: Coil cross section – Coil 101
Radially, there is ~ 600 µm of free space filled by epoxy (due to the overestimation on conductor expansion due to heat treatment). Conductor are aligned in the outer diameter.
Pole turns and mid-plane are well aligned, but conductors in between are tilted (up to ~ 500 µm) when compared to the nominal conductor position

## Slide 22: Summary
Coil 001 (Copper) and coil 101 (Low Grade RRP Nb3Sn) have been used to validate the manufacturing process/tooling
The splice region of coil 102 (RRP) is partially damage, but is potentially a good coil to be tested in a mirror structure.
Coil 103 (RRP) and 104 (RRP) will be used in the first MQXFS1 short model if electrical checks are OK.
Two additional practice coils for the first generation MQXF design will be produced using PIT conductor.

## Slide 23: Additional slides

## Slide 24: Coil cross section – Coil 101
AZIMUTHAL ALIGNMENT
Chart: turn #
Chart: Deviation [mm]

## Slide 25: Coil cross section – Coil 101
RADIAL ALIGNMENT
Chart: Radial deviation (mm)
Chart: Deviation (mm)

## Slide 26: Coil compaction
mm | IL after curing | IL after reaction | OL after curing | OL after reaction
101 |  |  |  | 
102 | -0.75 | -- | -0.43 | 0.95
103 | 1.94 | -- | 2.55 | 3.06
104 | 0.79 | 1.15 | 0.72 | 1.53
mm | IL after curing | IL after reaction | OL after curing | OL after reaction
101 |  |  |  | 
102 | 1.15 | -- | 1.4 | 1.37
103 | 3.12 | -- | 3.38 | 3.94
104 | 1.44 | 2.17 | 2.4 | 2.92
Difference (mm) in coil compaction return end with respect to nominal:
(>0 means ends less compacted than nominal)
Difference (mm) in coil compaction lead end with respect to nominal
(>0 means ends less compacted than nominal)
IL RE
OL RE
IL LE
OL LE

## Slide 27: Coil insulation – Coil 101
1
2
# |  | Nominal (µm) | Measured (µm) | Δ (µm)
1 | IL IR pole | 250 | 200 | -50
2 | IL OL pole | 500 | 460 | -40
3 | OL OR pole | 250 | 250 | 0
4 | IL PT | 500 | 445 | -55
5 | OL PT | 500 | 480 | -20
6 | MP IL | 275 | 290 | 15
7 | MP OL | 275 | 260 | -15
8 | IL IR MP | 400 | 900 | 500
9 | IL OL MP | 800 | 930 | 130
10 | OL OR MP | 400 | 350-590 | 
3
4
5
6
7
8
10
9
A
B
C
A
B
C

## Slide 28: Coil Ends
Position and inclination of the conductors in the end regions during winding and compared to the nominal turn location.
The measurements are usually within give number (I think is about 0.5 mm)
In general, good fitting of coil end parts.

## Slide 29: Electrical QA – Coil 001 - Limits
MQXFS Dielectrique measurement |  |  |  |  | 
equipment : | Megger |  |  |  | 
Time : | 30s | insulation (GOhm) |  |  | 
 | 5min | current leakage (nA) |  |  | 
U1 / U2 / U3 = LHC quality standard (V) / max setpoint tested (V) / Breakdown voltage (V) |  |  |  |  | 
MQXFS_001 |  |  |  |  | 
 | coil | QH inner | QH outer | Endshoe inner CS | Endshoe inner NCS
QH inner | 2350 / 4000 / 5000 |  |  |  | 
QH outer | 2350 / 5000 / 5500 |  |  |  | 
Endshoe inner CS |  | 2350 / 2000 / xxxx |  |  | 
Endshoe outer CS |  |  | 2350 / 2000 / xxxx | xxxx / 1000 / 2000 | 
Endshoe inner NCS |  | 2350 / 2000 / xxxx |  |  | 
Endshoe outer NCS |  |  | 2350 / 2000 / xxxx |  | xxxx / 1000 / 1500
Central post | xxxx / 500 / 1000 |  |  |  | 
Remarks : |  |  |  |  | 
LHC quality standard |  |  |  |  | 
Vq = 1000 | Vq maximal voltage in the coil during quench |  |  |  | 
Vtest between QH and coil around 2350V |  |  |  |  | 
Vtest between coil and ground around 3500V |  |  |  |  | 

## Slide 30: Coil 001 – Discharge test

## Slide 31: Electrical QA – Coil 101 - Limits
MQXFS Dielectrique measurement |  |  |  |  | 
equipment : | Megger |  |  |  | 
Time : | 30s | insulation (GOhm) |  |  | 
 | 5min | current leakage (nA) |  |  | 
U1 / U2 / U3 = LHC quality standard (V) / max setpoint tested (V) / Breakdown voltage (V) |  |  |  |  | 
MQXFS_101 |  |  |  |  | 
 | coil | QH inner | QH outer | Endshoe inner CS | Endshoe inner NCS
QH inner | 2350 / 2000 / 3000 |  |  |  | 
QH outer | 2350 / 5000 / 6000 |  |  |  | 
Endshoe inner CS | xxxx / short / short | 2350 / 2000 / xxxx |  |  | 
Endshoe outer CS | xxxx / 3000 / 4000 |  | 2350 / 2000 / xxxx | xxxx / 3000 / 4000 | 
Endshoe inner NCS | xxxx / 500 / 1000 | 2350 / 1000 / 2000 |  |  | 
Endshoe outer NCS | xxxx / 3000 / 4000 |  | 2350 / 2000 / xxxx |  | xxxx / 2000 / 3000
Central post | xxxx / 500 / 1000 |  |  |  | 
Remarks : |  |  |  |  | 
LHC quality standard |  |  |  |  | 
Vq = 1000 | Vq maximal voltage in the coil during quench |  |  |  | 
Vtest between QH and coil around 2350V |  |  |  |  | 
Vtest between coil and ground around 3500V |  |  |  |  | 

## Slide 32: Coil 101 – Discharge test

## Slide 33: Electrical QA under QXF criteria (1)
MQXFS_001 | coil |  |  |  | 
QH inner | 2000 / 2000 |  |  |  | 
QH outer | 2000 / 2000 | QH inner | QH outer | Endshoe inner CS | Endshoe inner NCS
Endshoe inner CS |  | 1000/ 1000 |  |  | 
Endshoe outer CS |  |  | 1000 / 1000 | 600 / 600 | 
Endshoe inner NCS |  | 1000 / 1000 |  |  | 
Endshoe outer NCS |  |  | 1000 / 1000 |  | 600 / 600
Central post | 500 / 500 |  |  |  | 
MQXFS_101 | coil |  |  |  | 
QH inner | 2000 / 2000 |  |  |  | 
QH outer | 2000 / 2000 | QH inner | QH outer | Endshoe inner CS | Endshoe inner NCS
Endshoe inner CS | 0 / 1200 | 1000/ 1000 |  |  | 
Endshoe outer CS | 1200 / 1200 |  | 1000 / 1000 | 600 / 600 | 
Endshoe inner NCS | 500/1200 | 1000 / 1000 |  |  | 
Endshoe outer NCS | 1200 / 1200 |  | 1000 / 1000 |  | 600 / 600
Central post | 500 / 500 |  |  |  | 

## Slide 34: Damage on splice region
In coil 102, some strands broken at the splice region while dismounting the mould for pre-tinning.
The space has been filled with strands of NbTi

## Slide 35: Wedges
Wedge insulation
  S2 Sleeve 0.125 mm thick
  1 sleeve for 2 pieces
  Extremities insulated to “lock” better the sleeve

## Slide 36: Wedge dimensions
Outer layer
  Layer-jump side
    nominal in the CAD model 1004.06 mm
    800 mm + 203 mm
      1 mm (0.5 mm per extremity) shorter
  Side opposite to layer jump
    nominal in the CAD model 1014.24 mm
    800 mm + 213 mm
      1 mm (0.5 mm per extremity) shorter
Inner layer
  Layer-jump side
    nominal in the CAD model 1038.37 mm
    800 mm +237 mm
      1 mm (0.5 mm per extremity) shorter
  Side opposite to layer jump
    nominal in the CAD model 1042.85 mm
    800mm + 241mm
      1 mm (0.5 mm per extremity) shorter
We have to keep in mind that we have 3 mm pole gaps
~ 800
~200

## Slide 37: End Spacers Selective Laser Sint.
2. Stress relief treatment
650˚C 2h
(heating up 1.5 h, cooling 13 h in the oven)
5. Sand blasting
Step 1: Glass bead blasting to remove adhered grain
Step 2: Metal ball blasting to compress surface
7. Wire EDM grooves
3. Supports removal
4. Holes and threads
1. Parts build up by SLS
Design file with a detailed description of the manufacturing parameters.
Any modification on the parameters shall be communicated and approved by CERN
6. 3D scan + re-work if required

## Slide 38: Coating (Al2O3)
Electrical tests performed on 18 qualifying samples Parameters varied:
Bonding agent  Ni80Cr20, NiCrAlY or none
Thickness of the bonding agent  0.03 mm or 0.05 mm
Roughness of the stainless steel substrate  NK16, NK20 or NK40
Temperature of the metallic substrate during deposition  no preheating or 200-300°C
The measured breakdown voltage was always above 750 V
(even after reaction at 650°C + cool-down at 77K).
No cracks in this region after reaction and cool down to 77K
After cool down to 77K, cracks in this region in 15 samples out of 18
Notes: No cracks were ever observed in the groove of the samples (inner cylinder or walls) neither after reaction at 650 C, nor after cool-down at 77K. Only cracks were detected in the outer diameter of sample #4 after reaction. After cool-down at 77K cracks appeared in this region in all the samples except #7, #9 and #18. The presence of cracks in this region didn’t affect the electrical tests.
ELECTRICAL TESTS
The insulation resistance at 500, 750, 1000 and 1250 V during 30 s was measured for all samples as well as the breakdown voltage. Very similar trends are observed in all samples. The measured breakdown voltage was always above 750 V (even after reaction at 650 C + cool-down at 77K).
The highest insulation resistance and breakdown voltage were recorded for sample #12 (NK 16 finishing, 0.01-0.03 mm of NiCrAlY). However, sample #11 was coated using exactly the same parameters and didn’t perform as well as #12.
#15 and #16 are the pair of samples sharing the same coating parameters (NK 40 finishing, 0.01-0.03 mm of NiCrAlY) that performed marginally better than the rest: highest values of insulation resistance at 1kV after reaction, and breakdown voltage above 1 kV after the 650 C thermal cycle.

## Slide 39
Too long to reach the dwell… decision to use SQXF-101 to optimize the cycle!
Remarks:
No ventilation in the retort
Argon flow 2500-3000l/h in the retort

## Slide 40: Instrumentation layout SQXF-101
tc19
tc20
tc14
Position of the thermocouple in block 5, 16 and 28.

## Slide 45
NbTi / copper stabilizer soldering lay out
Splice soldering lay-out