## Slide 1: TESLA SRF Cavities (as used for LCLS-II)
F. Marhauser
13-May-2014
LCLS-II Production Cryomodule Final Design Review

## Slide 2: Outline
Why TESLA cavities?
Technical specifications used for solicitation and project responsibilities
Brief cavity development history
Design and operational parameters
Performance goals
Cavity process flow recipes (LCLS-II vs. X-FEL)
Higher Order Mode (HOM) damping
How well does cavity industrialization work? – X-FEL status
LCLS-II cavity procurement status

## Slide 3: Tesla Cavities
courtesy of DESY
  Why TESLA cavities for LCLS-II ?
    Long history at DESY: TTF, FLASH, now utilized for European X-FEL under construction > 20 years experience
    Cavities employed successfully worldwide: > 1000 TESLA cavities produced
  DESY successfully transferred SRF technology to industry
    Cavities can be delivered fully dressed in Helium vessels ready to test
LCLS-II relies on ‘Build-to-Print’ manufacturing
  Production follows precise specifications (heavily based on X-FEL)
  LCLS-II bears responsibility for cavity performance (like X-FEL)
LCLS-II prototype CM cavity

## Slide 4: Technical Specifications (LCLSII-4.6-TS-0092)
  With permission from DESY, the technical specifications as currently employed for the manufacturing of the XFEL (mostly created 2008/2009) have been used as reference and modified for LCLS-II
Sufficient for vendor proposals (scheduling and cost assessment)
Number | Modified XFEL Documents
XFEL/002 | Technical Specifications for the Series Mechanical Fabrication Superconducting 1.3 GHz Cavities for LCLS-II
XFEL/003 | Quality Assurance and Quality Control Specifications (modified for LCLS-II)
XFEL/004 | Descriptions, Abbreviations, Drawing and EDMS numbers (modified for LCLS-II)
XFEL/005 | Helium Leak Tests (modified for LCLS-II)
XFEL/006 | Special Tools and Equipment (modified for LCLS-II)
XFEL/009 | Flow Chart Dumb-Bell Production (modified for LCLS-II)
XFEL/010 | Recommendations for the Machining of Niobium and Niobium-Titanium (modified for LCLS-II)
XFEL/011 | Recommendation for the Treatment of Niobium Parts (Handling, Cleaning, Etching, Welding)
XFEL/012 | Overview List and Detailed Inspection List of Tests and Demonstrations
XFEL/014 | Frequency Measurement on Dumb-Bell, Half Cell, End Group and Cavity (modified for LCLS-II)
XFEL/015 | Technical Specifications for the Series Production of Helium Tanks (modified for LCLS-II)
XFEL/016 | Technical Specifications for Welding the Helium Tank to the Cavity (modified for LCLS-II)
XFEL/017 | DESY Work Instructions for Welding a Cavity into a Helium Tank (modified for LCLS-II)
XFEL/018 | Standards
XFEL/A-D | Series Surface and Acceptance Test Preparation of Superconducting Cavities for the LCLS-II Project
Number | Additional LCLS-II documents
LCLS-II-4.6-TS-0092 | LCLS-II Nitrogen Doping Processing Procedure
LCLS-II-4.6-TS-0092 | LCLS-II Cavity Process Flow
LCLS-II-4.6-TS-0092 | LCLS-II Frequency Tuning Recipe

## Slide 5: Cavity Design Efforts and Responsibilities
  FNAL leads the design effort
  JLab leads the procurement effort for the production cavities
Description | JLab | FNAL | Vendor
Cavity design drawings |  | X | 
Cavity specification |  | X | 
QC and supply of cavity fabrication materials (Nb, NbTi) | X | X | 
Cavity procurement (266 cavities + 32 optional) | X |  | 
Government furnished material & equipment | X |  | 
Manufacturing drawings |  |  | X
Labor, equipment, facilities, all other materials |  |  | X
Fabricate, assemble, process, document, deliver cavities |  |  | X
Cavity inspection upon delivery | X | X | 
Cavity final acceptance | X |  | 

## Slide 6: Brief TESLA Cavity Design History
1990 – Cavity design work started by 1st TESLA workshop at Cornell
1997
1993
1992
cell geometry finalized (URMEL code)
tube steps down for TM012, TE121 HOM damping, but 20% higher loss factor
cell stiffeners
asymmetric design (different end cups)
to untrap HOMs
welded
HOM coupler
(conduction
cooled)
demountable
HOM coupler
(LHe cooled)
Nb reinforcement bars for stiffening
Ti transition ring to SS collar at end for SS helium vessel
Nb weight ~20 kg
cavity flange connection
(Nb, Helicoflex gaskets)
1993/94 1st series fabrication
HOM coupler concepts
Ti helium vessel
3 mm Nb sealing flanges
bent over tubes
HOM coupler options
new flange material proposed:
NbTi (45/55 by weight) flanges
with O-ring type Al gaskets
(maintains hardness after high-T
treatment, gaskets cleaned in ISO 4)

## Slide 7: Brief TESLA Cavity Design History
2001
Present
LCLS-II
AlMg hexagonal gasket
The angle between the 2 HOM coupler is not 90°but 115 °to provide also damping of quadrupole modes
Prototype CM cavities: “Short-Short” L = 1247.4 mm
Production CM cavities: “Short-Long” L = 1283.4 mm
LCLS-II prototype CM cavity

## Slide 8: Cavity RF and Mechanical Parameters
Parameter | Unit | Value
frequency | GHz | 1.3
N (# of cells) |  | 9
Lact (nominal) | m | 1.036
R/Q = Veff2/(ω*W) | Ω | 1036
G | Ω | 270
R/Q∙G/cell | Ω2 | 31080
Iris ID | mm | 70
Beam tube ID | mm | 78
kcc (cell-to-cell coupling) | % | 1.87
Epk/Eacc |  | 2.0
Bpk/Eacc | mT/(MV/m) | 4.26
wall thickness (before chemistry) | mm | 2.8
LFD w. stiffeners (Lorentz Force Detuning) | Hz/(MV/m)2 | ≤ 1.5
Δf/ΔL | kHz/mm | 315
# of HOM couplers |  | 2
real estate L~N~1/f, beam loading ~ (Eacc∙Lact(N))2  RF generator power/cavity
RBCS ~ f2 key deciding factor. Thermal instability limit (option to reach higher fields), exact f=1.3 GHz originally motivated by availability of high power klystrons, cavity surface area ~1/f2  capital costs, also likelihood to sustain higher fields with smaller area based on statistical model of defects
Cryogenic RF losses in wall ~ 1/(R/Q∙G)  capital/operational costs
wakefields (κǁ~1/ID3, κ~1/ID4), confined HOMs
field emission/dark current
thermal breakdown
cavity stiffness (LFD static in CW mode), tuner force/motor
tuner range
cell geometry  Rs=Q0/G
cell geometry  acc. efficiency, tradeoff with HOM impedance/loss factors ~R/Q
fundamental field flatness (δAcell ~ N2/kcc* δfcell,error)
cutoff  trapped HOMs
max. number mainly determined by HOM requirements (trapped modes, HOM Qext, δAcell ~ N2/kcc* δfcell,error), ancillary components (power/HOM couplers, tuners, He vessels) ~1/N  capital costs
Nb stock  capital costs, impacts stiffness of cavity
Minimum # of couplers to damp different polarizations of HOMs

## Slide 9: Relevant Geometrical Parameter (Design Comparisons)
Field Emission- relevant
Quench-relevant
Cryogenic loss-relevant

## Slide 10: Operational Parameters Main Linac Cavities (vs. CEBAF cavities)
Parameter | Unit | LCLS-II TESLA cavities | CEBAF C100 LL cavities
Frequency | GHz | 1.3 | 1.497
Mode of operation |  | CW | 
Material |  | Fine grain RRR ≥ 300 | 
Eacc | MV/m | 16*/18** | 19.2
T | K | 2.0 | 2.07
Epk | MV/m | 32/36 | 41.7
Bpk | mT | 68.2/76.7 | 71.8
<Q0> |  | 2.7e10 | 7.2e9
Rs | nΩ | 10.0 | 38.9
Pwall | W | 9.8/12.4 (when same Q0) | 29
* <Eacc> rounded, slightly less than 16 MV/m, yields 4.14 GeV with nominal phasing for 100 pC and 6% cavities unpowered
** max. (14-18 MV/m range)

## Slide 11: Tesla Cavity Design Changes (LCLS-II vs. XFEL)
  Hardware:
    No geometrical design changes to TESLA cavity itself
    Modifications concern cavities’ ancillary components (He vessel, tuner, HOM RF feedthroughs, magnetic shielding <5mG) and cryomodule component design (e.g. adaption to CW operation, magnetic flux expulsion)
  Surface post-processing:
    Nitrogen-doping as part of high-T baking process added
      High-Q0 recipe developed at FNAL yields consistent results among partner labs
      Goal was to develop robust recipe that can be transferred to industry achieving Q0=2.7e10 at 16 MV/m for production cavities
    Slower (temperature-controlled) Electropolishing

## Slide 12: Cavity Process Flow (LCLS-II vs. XFEL Recipes)
Cavity after mechanical fabrication
EP 110 um (temperature controlled)
US Degrease
External 20 um BCP
Short HPR
800C HT Bake + N2 Doping
RF Tuning
EP 5 um
Long HPR
Final Assembly
US Degrease
Long HPR
Helium Tank Welding Procedure
VT Assembly
Standard HPR
HOM Tuning
Ship to FNAL/JLab
Leak Check
Cavity after mechanical fabrication
EP 110 or
EP 140 um
Ethanol Rinse
External 20 um BCP
Short HPR
800C HT Bake
RF Tuning
EP 40 um or
Flash BCP 10 um
Ethanol Rinse when final EP applied
Long HPR
Final Assembly
Long HPR
Helium Tank Welding
Procedure
VT Assembly
Standard HPR
HOM Tuning
Ship to DESY
Leak Check
120C bake
US Degrease
X
X
X
LCLS-II Recipe
XFEL Recipe

## Slide 13: HOM Damping
HOM damping requirements: Qext < 106 -107 for high impedance HOMs (no hard limit) (LCLSII-1.1-DR-0251-R0, Table 6-5)
Damping requirements rather relaxed (Iavg,max =0.3mA at Q=300 pC, frep=1 MHz) compared to X-FEL
Probability of HOMs close to spectral lines is small
Boundary conditions above tube cutoff matter, more HOM couplers can contribute to damp critical propagating modes (e.g. TM111, TE121)
LCLS-II probe tip used

## Slide 14: HOM Damping – Dipole Modes only

## Slide 15: HOM Damping QC
F. Marhauser, C. Potratz, “Automatization of Quality Factor Measurements in RF Structures”, JLAB-TN-11-008
External/loaded Qs can be measured in vertical Dewar to check integrity of cavities
Time-saving pole-fit routine enables HOM QC check of all cavities during production phase

## Slide 16: History – Cavity Performance Goals at ~2K

## Slide 17: History – Cavity Performance Goals at ~2K

## Slide 18: LCLS-II high-Q0 “Revolution”
N-doping

## Slide 19: JLab’s Vertical Tests Results for Prototype Cryomodule
at 2K - results corrected for NbTi flanges (-1.4 nΩ from SS)
A. D. Palczewski et al., Proc. of IPAC 2015, WEPWI029.
LCLS-II spec
6 cavities qualified, 2 not yet tested
Result for cavities obeying present LCLS-II doping recipe (N2A6 EP5):
<Q0> = 4e10 at 16 MV/m (FNAL graphs missing here, all Lab’s data combined in slide 24 )

## Slide 20: How well does industrialization work?
71 CMs worth of cavities (~2x LCLS-II = 35 CMs)
courtesy of Nick Walker – DESY
from LLC-PAC meeting - LAL -, April 2015
XFEL status and state-of-the-art of vendor-delivered cavities

## Slide 21: How well does industrialization work?
courtesy of Nick Walker – DESY
from LLC-PAC meeting - LAL -, April 2015
In general:
1st retreatment is a standard High-Pressure Rinse (HPR)
2nd (if required) is BCP
XFEL status and state-of-the-art of vendor-delivered cavities

## Slide 22: How well does industrialization work?
courtesy of Nick Walker – DESY
from LLC-PAC meeting - LAL -, April 2015
XFEL status and state-of-the-art of vendor-delivered cavities
Usable gradient, i.e. minimum of the following gradient values:
a) Max (i.e. quench)
b) Q0 = 1e10
c) X-ray 1 (top) threshold
d) X-ray 2 (bottom) threshold
As “received” test

## Slide 23: History – Vertical Cavity Performance Milestones at ~2K
note : only data included as published/presented by DESY

## Slide 24: History – Vertical Cavity Performance Milestones at ~2K

## Slide 25: Performance Preservation in Cryomodule
4 old
cavities
used

## Slide 26: Performance Preservation in Cryomodule
prototype CM work in progress
4 old
cavities
used

## Slide 27: Quality Assurance and Quality Control
Hold Points: Red
This process chart was developed by the cavity procurement team and the High-Q0 team (Rev. 3)
After cavity mechanical fabrication
  Check of all fabrication and inspection data prior to release for chemical/heat treatment processing
After chemical/heat treatment processing
  Check of all process and inspection data prior to release for final chemistry, welding of helium vessel and assembly for vertical test qualification
After all cavity steps are complete
  Check of all data prior to release for shipping to FNAL & JLab

## Slide 28: Procurement Timeline and Status
16 cavities
250 cavities








cavities = 2 x # vendors
Phase | Purpose | Duration (months) | Cavity count
 | Prototype CMs | in progress | 16*
I | Vendor Qualification | ~6 | 2 x (# of vendors)*
II | 1st Articles | ~6 | 16
III | Full Production | ~13 | 250
IV | Optional units |  | 32
Order: 266 cavities (FNAL 137, JLab 129), 264 required for 33 CMs, 2 spares Optional: 32 cavities if required for up to 298 cavities * From FNAL inventory |  |  | 

approval pending

## Slide 29: Summary
  LCLS-II leverages from industrialized cavity fabrication
  More than 35 X-FEL CMs have been built and cavities tested exceed specifications in the cryomodules (on average)
  X-FEL technical specifications used for production with only slight modifications
  QA/QC implemented to inspect cavities and process data at ‘hold points’
  Present N-doping recipe yields cavities with vertical performance beyond LCLS-II specification
  Margin to horizontal specs similar to X-FEL, which yields some confidence that CM performance specifications can be met for LCLS-II
  First horizontal test of dressed cavity in ‘demonstration’ ¼ cryomodule successful
  We are prepared for Phase I (vendor qualification)
    Approval pending at DoE
  Prototype activities heavily in progress at labs

## Slide 30
Backup Slides

## Slide 31: Procurement Status
Date | Milestone
2014/09/26 | - Source Selection Plan (SSP) established to evaluate vendor proposals and capabilities in the competitive acquisition for the LCLS-II production cavities - SSP the Source Selection Board (SSB) officially appointed to evaluate vendor proposals including the voting members of the Technical Evaluation Team (TET)
2014/10/01 | Request for Proposal (RFP) released (solicitation JSA-14-R346481 LCLS-II Production Cavities)
2014/10/08 | Pre-proposal/vendor outreach conference - briefed prospective vendors before proposal submission
2014/12/01 | Bidders’ proposals received
2015/02/26 | Technical evaluation summary completed by TET – price proposal released
2015/03/04 | Vendor scenario recommendation presented to SSB Request for Final Proposal Revision to each vendor (FPR)
2015/03/11 | FPRs received
2015/03/12&19 | DOE presentations (JLab and Oak Ridge)
2015/03/31 | TET award recommendation completed
2015/04/07 | Proposal Analysis Report (PAR) approved by SO, TET chairperson, SSO and SSOA
2015/05/04 | PAR submitted to DOE for approval

## Slide 32: Best Value Evaluation
  Permits tradeoffs among cost and non-cost factors
  Multiple vendors scenarios analyzed
    Acceptability  based on whether all required documentation in place
    Capability  Based on technical evaluation criteria factors and subfactors
      Factor 1: Experience & Past Performance
        Subfactor A: Experience
        Subfactor B: Past Performance
      Factor 2: Resources: Facilities, Planning, & Management
        Subfactor A: Production Facilities & Equipment
        Subfactor B: Manufacturing Planning & Management
        Subfactor C: Production & Delivery Schedule
        Subfactor D: Commitment to R&D Technology
      Factor 3: Understanding of the Requirement
        Subfactor A: Conformance with Specification
        Subfactor B: Change Suggestions are useful & well supported
      Factor 4: Quality Assurance
Subfactor A: QA Plan assures quality product:
Subfactor B: Methodology for Problem Avoidance & Resolution
Subfactor C: Approach to Documentation, Calibration & Inspections
    Price and price-related factors:
    Total price weighed against apparent advantages of individual technical proposals (e.g. determine if superior technical proposals, excluding price considerations, are worth increased price differentials (if any)). Buy American Act applied for non-domestic vendors