## Slide 1: Ferromagnetic Josephson Junctions for Cryogenic Memory
Norman Birge, Michigan State University
in collaboration with Northrop Grumman Corporation and Arizona State University
(with thanks to D. Scott Holmes, Booz Allen Hamilton & IARPA)
Work supported by IARPA and the US Department of Energy
Notes: 1

## Slide 2: A subset of the workers
Eric Gingrich, Bethany Niedzielski, Joseph Glick, Yixing Wang, Bill Martinez, Josh Willard, Sam Edwards, Reza Loloee, William P. Pratt, Jr.,
plus many earlier students!
summer 2013
Notes: 2

## Slide 3: Outline
The need for energy-efficient computing
Superconducting computing: logic and memory
Superconducting/ferromagnetic hybrid systems
Demonstration of phase control of an S/F/S Josephson junction – the basic memory device
Future prospects

## Slide 4: The need for energy-efficient computing
Opened in 2013
Cost: ~760 M$
Nearby Lule River generates 9% of Sweden's electricity (~4.23 GW)
Average annual temperature: 1.3 C
Copyright Facebook
 | Specifications
Performance* | 27-51 PFLOP/s
Memory* | 21-27 PB RAM 1900-6800 PB disk
Power | 84 MW avg* (120 MW max)
Space | 290,000 ft2 (27,000 m2)
Cooling* | ~1.07 PUE
* estimated
Slide courtesy of Scott Holmes
Facebook Data Center, Luleå, Sweden

## Slide 5: Superconducting Computing Approach
Low temperature operation (~4 K)
  Allows different physics
  Commercially available refrigeration
Logic
  SFQ (Single Flux Quantum)
  Switching energy ~ 2x10-20 J
Memory
  compatible with SFQ logic
Interconnects
  Superconducting in the cold space
  Input/Output: electrical or optical
Major energy reductions in all 3 areas!
~2 mV
~1 ps



~c/3, nearly lossless
S
F (soft)
I
F (hard)
S
0
Slide courtesy of Scott Holmes

## Slide 6: Superconducting computing looks promising
Tianhe2
Titan
K-Computer
Sequoia
Mira
Chart: 
| 33.862699999999997 | 17.59 | 17.173224000000001 | 10.51 | 8.5866120000000006 | 6.2709999999999999 | 5.1681100000000004 | 5.0088569999999999 | 4.2933060000000003 | 2.8969999999999998 | 2.843 | 2.5659999999999998 | 2.34578 | 2.09809 | 1.788878 | 1.54129 | 1.5149999999999999 | 1.41547 | 1.359 | 1.2709999999999999 | 1.2576149999999999 | 1.2522139999999999 | 1.2370000000000001 | 1.1100000000000001 | 1.0733269999999999 | 1.054 | 1.05 | 1.0429999999999999 | 1.03311
Top Computers | 17.808 | 8.209 | 7.89 | 12.659 | 3.945 | 2.325 | 4.51 | 2.301 | 1.972 | 3.422 | 1.398 | 4.04 | 1.384 | 2.118 | 0.821 | 2.015 | 3.575 | 1.606 | 2.251 | 2.58 | 1.436 | 0.575 | 2.2 | 3.98 | 0.493 | 2.91 | 4.59 | 1.176 | 1.26
DOE Exascale Goal | 20
Coral Goal (2017) | 20
Superconducting, Projected | 0.015 | 0.03 | 0.02 | 0.04 | 0.08 | 0.2 | 1 | 2
Tianhe-2
Titan
K-Computer
Sequoia
Mira
Coral
Power (MW)
Performance (PFLOP/s)
D.S. Holmes et al.,
IEEE Trans. Appl. Supercond. 23, 1701610 (2013)
Slide courtesy of Scott Holmes
Notes: 2015-09-02

## Slide 7: Superconducting “SFQ” Logic
A new superconducting logic family:
“SFQ” = Single flux quantum
RS flip-flop
OR gate
Josephson junctions
K.K. Likharev & V.K. Seminov, IEEE Trans. Appl. Supercon. 1, 3 (1991)

## Slide 8: The need for superconducting memory
“Random access memory (RAM) has been considered the Achilles heel of superconductor logic.”
-- Superconducting Technology Assessment, NSA 2005

## Slide 9: Our approach to superconducting memory:
Josephson Magnetic Random Access Memory (JMRAM)
Anna Y. Herr & Quentin P. Herr, US Patent 8,270,209 (2012)
A.Y. Herr, Q.P. Herr & Ofer Naaman, US Patent 9,208,861 (2015)
Northrop Grumman Corporation
Memory cell is a SQUID loop
One junction has two stable phase states for “0” and “1”
Magnetic states are written using standard MRAM techniques

## Slide 10: JMRAM is a Superconducting MRAM
www.freescale.com
Memory cell is a magnetic tunnel junction with superconducting electrodes:
underlining physics demonstrated on SFS Josephson junction
memory state – critical current or phase, w/ magnetic hysteresis
write – spin reversal
read – Josephson effect
www.everspin.com
MRAM (Everspin)
No idle/static power dissipation, read energy is dissipated only for logical “1”
JMRAM (Northrop Grumman)
Slide courtesy of Anna Herr

## Slide 11: Outline
The need for energy-efficient computing
Superconducting computing: logic and memory
Superconducting/ferromagnetic hybrid systems
Demonstration of phase control of an S/F/S Josephson junction – the basic memory device
Future prospects

## Slide 12: Superconductor/Ferromagnet proximity effect
ballistic
diffusive
S N
D = diffusion constant
2Eex
S F
“FFLO-type” physics

## Slide 13: Consequence: S/F/S Josephson junctions oscillate between 0 and p junctions as dF increases:
Ryazanov et al., PRL 86, 2427 (2001); PRL 96, 197003 (2006).
Weak F: Cu48Ni52 alloy
Robinson, Piano, Burnell, Bell, Blamire, PRL 97, 177003 (2005)
Strong F: Co
0.0 1.0 2.0 3.0 4.0 5.0
dCo (nm)
IcRN (mV)
0-state: Is = Ic sin(f2-f1)
p-state: Is = Ic sin(f2-f1+p)
S F S
dF
f1 f2
Buzdin, Bulaevskii, & Panyukov (1982).
Notes: 13

## Slide 14: Handwaving explanation for Ic oscillations
S
S F1

## Slide 15: Handwaving explanation for Ic oscillations
short-range triplet component
S
S F1
Conventional superconductor only accepts singlet component
 Ic  |cos(QdF)| = |cos(dF/F)|
S F1 S
dF
singlet component
cos(dF/F) > 0  0-junction
cos(dF/F) < 0  -junction

## Slide 16: The Ic and phase of an S/F/S JJ are fixed by dF
Ryazanov et al., PRL 86, 2427 (2001); PRL 96, 197003 (2006).
Weak F: Cu48Ni52 alloy
Robinson, Piano, Burnell, Bell, Blamire, PRL 97, 177003 (2005)
Strong F: Co
0.0 1.0 2.0 3.0 4.0 5.0
dCo (nm)
IcRN (mV)
S F S
dF
f1 f2
Can we control Ic or phase state of a single Josephson junction?
cos(dF/F) > 0  0-junction
cos(dF/F) < 0  -junction
Notes: 16

## Slide 17: Add a second ferromagnetic layer: S/F1/F2/S Ic and phase depend on relative magnetization direction
Parallel state:
Antiparallel state:
S
S
dF1
dF2
Electron pair accumulates phase  while traversing junction
S
S
dF1
dF2
Ic  exp[-(dF1/F1 + dF2/F2)] cos(dF1/F1  dF2/F2)

## Slide 18: Memory choice: control Ic amplitude or phase?
Control amplitude: JJ must have large IcRN product to switch quickly. The switching time is inversely proportional to IcRN
Control phase: JJ acts as passive phase shifter; no need for large IcRN
Example: Feofanov et al., Nature Phys. 6, 593 (2010)
S
S
F
F
N
Ryazanov et al., PRL 86, 2427 (2001); Oboznov et al., PRL 96, 197003 (2006).
P state: Cooper pair phase shifts add
AP state: Cooper pair phase shifts subtract

## Slide 19
Selection of Materials for Sample Development
19
S
S
F
F’
N
N
N
Superconductor (S)
Tc > 4 K
Use Nb
Ferromagnets
Appreciable Jc but not too thin
Fixed Layer (F)
Magnetized by moderate Hext
Use Ni, NiFeCo?
Free Layer (F')
Reliable switching at low Hext
Large single domain size
Use NiFe, PdFe?
Spacer Layers (N)
Normal metal, very smooth
Helps connect bcc Nb to fcc F-layers
Center layer thick enough to magnetically decouple F and F'
Use Cu
Hext
Lots of work to optimize design parameters!
Notes: 19

## Slide 20
Cross-section of a single F-Layer JJ sample
From Sandia National Lab
c/o Nancy Missert & Paul Kotula
Verifies the fabrication process:
Smooth and continuous F- Layer (NiFeCo shown here)
Smooth Nb/Al base electrode
Good junction isolation
b) Energy Dispersive X-ray Spectroscopy (EDX) to identify elements
STEM
EDX
a) Focused Ion Beam (FIB) Cuts + Scanning Transmission Electron Microscopy (STEM)
20
50 nm

## Slide 21: Outline
The need for energy-efficient computing
Superconducting computing: logic and memory
Superconducting/ferromagnetic hybrid systems
Demonstration of phase control of an S/F/S Josephson junction – the basic memory device
Future prospects

## Slide 22: S/F1/N/F2/S Josephson Junction Composition
Nb
Nb
F2
Cu
Cu
F1
Cu
F1 = Ni (1.2 nm)
fixed layer
F2 = NiFe (1.5 nm)
free layer
Nb(100)/Cu(5)/NiFe(1.5)/Cu(10)/Ni(1.2)/Cu(5)/Nb(150)
Choose NiFe thickness to put F2 close to 0 -  transition.
Ni provides additional small push to right or left.

## Slide 23
Perform interference experiment to measure relative junction phase
S
S
F
F’
N
N
N
S
S
F
F’
N
N
N
Different aspect ratio JJs have different switching fields
Junction sizes:
Both have Area = 0.5 m2 Aspect Ratios = 2.2 and 2.8
F-Layer Materials:
F : Ni, 1.2 nm
F’ : NiFe, 1.5 nm
Switching
field H1
Switching
field H2
H1 < H2
Side View
Side View
Top-Down View
Top-Down View
Two JJs in a SQUID Loop:
23
Can We Observe a Controllable -Phase Shift?
Notes: Change Hext subscripts and shape of jj

## Slide 24: Two junctions in a SQUID loop used to measure relative junction phase
Switching field H1
Switching field H2
H1 < H2
Schematic:
Junction sizes:
Both have Area = 0.5 m2 Aspect Ratios = 2.2 and 2.8
Switch magnetization with in-plane field
Cartoon of Actual Device:
On-chip current line couples magnetic flux into SQUIDs
Different aspect ratio pillars have different switching fields

## Slide 25: At Relatively Low External Fields, Two Phase Changes Should Be Observable
Hext
Initialize with large field in -z direction, then slowly increase Hext in +z direction
Constructive Interference
Φ
P
P

## Slide 26: At Relatively Low External Fields, Two Phase Changes Should Be Observable
Hext
Φ
Hext
AP
P
Initialize with large field in -z direction, then slowly increase Hext in +z direction
Destructive Interference
Constructive Interference
H1 < Hext < H2
Φ
P
P

## Slide 27: At Relatively Low External Fields, Two Phase Changes Should Be Observable
Hext
Φ
Hext
AP
P
Φ
Hext
AP
AP
Initialize with large field in -z direction, then slowly increase Hext in +z direction
Destructive Interference
Constructive Interference
Constructive Interference
H1 < Hext < H2
Hext > H2
Φ
P
P

## Slide 28: Data show clean switching between the four expected states
Switching Fields: +30 Oe, +50 Oe, -35 Oe, -100 Oe
0-0
0-π
π-π
0-0
π-0
π-π
Gingrich, Niedzielski, Glick, et al., Nat. Phys. 12, 564 (2016)

## Slide 29
Data cuts for the four magnetic states
Icave = (Ic+ - Ic-)/2
Ic+ , Ic-
 - 
0 - 
0 - 0
 - 0
Gingrich, Niedzielski, Glick, et al., Nat. Phys. 12, 564 (2016)

## Slide 30: Ic() curves have tilted ratchet shape when loop inductances and/or critical currents are asymmetric
L1
Ic1
L2
Ic2
Ic+
Ic-
Ic+ and Ic- shift by equal amounts and in opposite directions along the  axis
Ic+
Ic-
Ic
Φ
Ic+() and Ic-() oscillations are asymmetric when L1 ≠ L2 & Ic1 ≠ Ic2
Analyze Ic+ and Ic- peak shifts to extract JJ phase shifts

## Slide 31
Quantitative fits to SQUID modulation data for the four magnetic states
Icave = (Ic+ - Ic-)/2
Ic+ , Ic-
 - 
0 - 
0 - 0
 - 0
Gingrich, Niedzielski, Glick, et al., Nat. Phys. 12, 564 (2016)

## Slide 32: Quantitative Analysis Consistently Assigns the Inductance and Critical Currents of Each State
state | Ic1 (mA) | Ic2 (mA) | L1 (pH) | L2 (pH)
 -  | 0.292 | 0.217 | 5.73 | 11.38
0 -  | 0.565 | 0.203 | 5.64 | 11.33
0 - 0 | 0.567 | 0.419 | 5.63 | 11.55
 - 0 | 0.294 | 0.420 | 5.71 | 11.56
Fitting parameters from independent fits of 4 magnetic states are highly consistent
  Exception: critical current of JJ #2 changes slightly in  state when JJ #1 switches from  to 0 state
 |  | ave | 5.68 | 11.46
 |  |  | 0.05 | 0.12
FastHenry simulations:
L1  7 pH, L2  13 pH
Gingrich, Niedzielski, Glick, et al., Nat. Phys. 12, 564 (2016)

## Slide 33: Improved SQUID Design
Symmetric Layout
No inductance asymmetry
L1 = L2
Lower critical currents so less shift in Ic+ and Ic-
Free layer = NiFe (1.0 nm)
Changed the fixed layer from Ni (1.2 nm) to NiFeCo (1.1 nm)
  More reliable magnetic properties
  Lower field required for initialization
Φ
L1
L2

## Slide 34: 3D plots show phase transitions but also intermediate states
Reliable phase switching through multiple sweeps and cooling cycles
Intermediate states present
Ic+ curves much less asymmetric
Switching fields: +14 Oe, +28 Oe, -44 Oe, -70 Oe
Up 1
Down 1

## Slide 35: Quantitative analysis confirms π phase switch between successive curves
State | Ic1 (mA) | Ic2 (mA)
 -  | 0.007 | 0.016
0 -  | 0.023 | 0.015
0 - 0 | 0.027 | 0.037
 - 0 | 0.006 | 0.042
Individual pillars have very small critical currents in the π state

## Slide 36: What needs to be done - 1
Us:
  Optimize magnetic materials
    Lower Msat  lower Eswitch
    Reduce extrinsic sources of anisotropy in thin films
    Find better material for fixed layer (Ni has issues)
  Minimize underlayer roughness
  Develop read and write electronics & interface to RQL
    (RQL is Northrop version of SFQ logic)
  Make the rest of the computer!

## Slide 37: What needs to be done - 2
The rest of the field:
  Develop reliable Nb fabrication foundry (MIT Lincoln Labs)
  Develop design tools for superconducting circuits (new IARPA program)
  Develop high-bandwidth communication from room temperature to cryogenic space (new IARPA program)

## Slide 38: Conclusions
Magnetic Josephson junctions have demonstrated potential for ultra-low-power cryogenic memory
Much more work needs to be done!

## Slide 39: Bibliography
E.C. Gingrich, B.M. Niedzielski , J.A. Glick , Y Wang , D.L. Miller , R. Loloee R, W.P. Pratt Jr, N.O. Birge, “Controllable 0- Josephson junctions containing a ferromagnetic spin valve,” Nature Phys. 12, 564 (2016). DOI: 10.1038/nphys3681
D.S. Holmes, A.M. Kadin, M.W. Johnson, “Superconducting Computing in Large-Scale Hybrid Systems”, Computer, 48, 34, December 2015. DOI: 10.1109/MC.2015.375
D.S. Holmes, A.L. Ripple, and M.A. Manheimer, “Energy-efficient superconducting computing – power budgets and requirements”, IEEE Trans. Appl. Supercond., 23, 1701610 (2013). DOI: 10.1109/TASC.2013.2244634
Q.P. Herr, A.Y. Herr, O.T. Oberg, and A.G. Ioannidis, “Ultra-low-power superconductor logic”, J. Appl. Phys. 109, 103903 (2011). DOI: 10.1063/1.3585849

## Slide 40: Extra Slides

## Slide 41: How to generate spin-triplet supercurrent
with F, F = PdNi, d = 4 nm
without F,F
Khaire, Khasawneh, Pratt, & Birge, Phys. Rev. Lett. 104, 137002 (2010)
Nb
F
Co
Ru
Co
F
Nb
Cu
Cu
Cu
Cu

## Slide 42: Microscopic mechanism for triplet generation (from discussion with M. Eschrig)
S
S F1
S F1 F2
long-range triplet components in F2
short-range triplet component
rotate basis:

## Slide 43: Proposal by Berezinskii (1974):
What does this mean?
Fermions require:
If F is odd in time:
then F is even under exchange of space and spin:
F(r1,r2,s1,s2,t1,t2 )  “anomalous Green’s function” = pair correlation function

## Slide 44: Josephson junctions: 0 and p junctions
F
S1 , f1
S2 , f2
standard Josephson junction
p-junction
ground state: f = 0
ground state: f = p
Josephson energy:
Supercurrent:
phase difference f = f2 - f1

## Slide 45: What is a Josephson junction (JJ)? Two superconductors separated by a “barrier:” (I = insulator, N = normal metal, F = ferromagnet)
I, N or F
S1 , f1
S2 , f2
Josephson relations:
dc: supercurrent flows with no dissipation
ac: phase changes when V  0
phase difference f = f2 - f1
See The Feynman Lectures, Volume III, Chapter 21

## Slide 46: RSJ model of current-biased Josephson junction
Josephson relations:
dc: Is = Ic sin()
ac: V =
If Is < Ic, then V = 0
= -  - EJsin() + 0Ibias
Damped motion of particle in
tilted washboard potential
m = ,  = , EJ = 0Ic, 0 =
Ibias
R
C
JJ
, V
U() = EJ(1-cos()) - 0Ibias
2
Ibias = + C + Icsin()

## Slide 47: Pendulum analog of RSJ model
Josephson relations:
dc: Is = Ic sin()
ac: V =
If Is < Ic, then V = 0
Ibias
R
C
JJ
, V

= -  - mgL sin() + torque
torque  Ibias/Ic

Ibias < Ic
 = constant
V = 0
Ibias > Ic
 runs
V  0

## Slide 48: Emission of single flux quantum (SFQ) pulse by overdamped Josephson junction
Quiescent state:

Ibias < Ic
 = constant
V = 0
Iin
JJ
, V
Ibias
Time
Voltage
~1 mV
~2 ps
Iin pulse: Ibias + Iin > Ic   jumps by 2
Voltage pulse has area Vdt = 0 = h/2e
Single Flux Quantum (SFQ)
0 = IL = Vdt
V =
Simulation by Kirill Moskovtsev

## Slide 49: SFQ gate: set-reset (SR) flip-flop (case 1)
Ibias
J0
Ls
J1
J3
J2
Reset
Out
Transfer Block
Storage Block
Decision
Block
Single Flux Quantum (SFQ)
0 = IL = Vdt
t
V
Set
t
V
t
V
Slide courtesy of Scott Holmes
Notes: 2016-05-12

## Slide 50: SFQ gate: set-reset (SR) flip-flop (case 2)
Ibias
J0
Ls
J1
J3
J2
Reset
Out
Transfer Block
Storage Block
Decision
Block
Single Flux Quantum (SFQ)
0 = IL = Vdt
Set
t
V
Slide courtesy of Scott Holmes
Notes: 2016-05-12

## Slide 51
Fraunhofer Pattern of S/F/S Josephson Junctions
51
Standard overdamped Josephson junction I-V curves.
Measure I-V curves in a magnetic field, applied parallel to the plane, to record a Fraunhofer pattern.
H=140 Oe
Ic
Notes: 51

## Slide 52
Fraunhofer Pattern of S/F/S Josephson Junctions
52
NiFeCo=1.6 nm
Standard overdamped Josephson junction I-V curves.
Measure I-V curves in a magnetic field, applied parallel to the plane, to record a Fraunhofer pattern.
Fraunhofer pattern is shifted due to NiFeCo magnetization
H=140 Oe
Ic
Hshift = 75 Oe
H (Oe)
Notes: 52

## Slide 53
Fraunhofer Pattern of S/F/S Josephson Junctions
53
NiFeCo=1.6 nm
Standard overdamped Josephson junction I-V curves.
Measure I-V curves in a magnetic field, applied parallel to the plane, to record a Fraunhofer pattern.
Fraunhofer pattern is shifted due to NiFeCo magnetization
Due to elliptical geometry, fit to an Airy function :
  J1: Bessel function of the 1st kind
  H: Magnetic Field
  w: Junction width
  dF, dN : F-layer and N-layer thicknesses
  λ : London penetration depth of Nb (85nm)
  Ic0: Maximum critical current
  Ф0: Flux quantum
H=140 Oe
Ic
Hshift = 75 Oe
H (Oe)
Notes: 53

## Slide 54
Estimating the NiFeCo 0-p Transition
54
Estimate location of 0-π transition by fitting Ic,Max*RN vs NiFeCo thickness, d, to:
Best fit parameters: V0 =29 µV, ξf1= 1.11 nm, ξf2= 0.48 nm, d0-π= 1.2 nm
The first 0 - π transition occurs near 1.2 nm, and a π - 0 transition near 2.7 nm.
Measure the Fraunhofer patterns of many samples with increasing NiFeCo thickness, d.
0
π
0
H (Oe)
since RN ~1/Area
Notes: 54

## Slide 55
Hshift
Hshift
Hshift
Observing the Fraunhofer Pattern Shift: Hshift
55
Extract F-layer magnetization from the shift in the Fraunhofer patterns
Good agreement between experiment and theory
Compute magnetization, from slope: MNiFeCo = 947 55 emu/cm3
Confirms the nanomagnet is fully magnetized
Observe the switching behavior of a single nanomagnet
The NiFeCo magnetic dead-layer is 0.24 0.07 nm, from the x-intercept.
Notes: 55

## Slide 56
0-Pi Transition Data From Four Different F-Layers
56
(3% Fe)
Fixed Layer
Fixed Layer
Free Layer
Free Layer

## Slide 57
Sample Fabrication
Coat in Resist
Electron Beam Lithography + Development
Ion Mill
Sputter Material
2.5 aspect ratio
area ~0.5 μm2
Top Down View:
Why elliptical junctions? Shape anisotropy helps orient the magnetization along the long axis.
57
Deposit SiOx
Side Mill
Lift-off
Coat and Develop Resist
Sputter Top Leads
Final Lift-off
Sample fab takes about 3 weeks (for 8-16 chips).
I)
J)