## Slide 1: QXF Coil Fabrication: A Forward Look
Joint LARP CM20/HiLUMI Collaboration Meeting
April 8-10, 2013 • Napa, CA USA
Dan Cheng
April 9, 2013

## Slide 2: Outline
Overview
Standing Issues in Coil Fabrication
Summary

## Slide 3: The LARP QXF Coil Task: At a Glance
FNAL
LBNL/BNL
CERN

## Slide 4: The LARP QXF Coil Task: A Second Look

## Slide 5: Background to QXF Coil Fabrication Issues
Fabrication review of HQ/LHQ coils was held in March 2013; recommendations given
  Fabrication of future coils were covered in talks by M. Yu and F. Borgnolutti
QXF Coil fabrication
  HQ/LHQ coil fabrication experiences provide a basis for QXF coil fabrication processes
  But some outstanding issues remain to be addressed

## Slide 6: Qxf coil fabrication: standing Issues

## Slide 7: Coil Parts & Design
Rapid design iterations are necessary
  Parts design
  Rapid prototype fabrication (DMLS, FDM, etc.) for quick turnaround
  Test fit spacers, end saddles, etc. using coil winding tests (this is different from cable windability tests)
  Measure and CMM modified parts
  Apply fit feedback to the analytical (Roxie/Bend) models of coil shapes for final designs
Plasma sprayed parts
  Issues of durability and repeatability on surfaces where deemed useful (and/or necessary)
Coil alignment keys
  Question of Titanium or G11 still must be examined
Courtesy: G. Kirby
Design
Fab.
Fit

## Slide 8: Coil Processing: Winding
Popped strands during winding
  What is the most effective method of prevention and/or repair?
    Winding tool, curing matrix, or…?
Winding tension & cable twist
  Fixed tension, or dynamic tension during turns
  Coil winding infrastructure may be unable to introduce cable twist
Intralayer insulation layers
  Cured glass fabrics exhibit brittle behavior after reaction—leave layer uncured or cured?
Coil packaging and clamping (see curing issues in next slide)
Cured S-glass in HD3 Coil 1
Crumbled after reaction

## Slide 9: Coil Processing: Curing
Curing operations
  Not all infrastructure supports applying separate mandrel and platen operations
The addition of extra shims on midplane:
  Does overcompressing the coil at the midplane during curing affect the final coil package size in any appreciable way?
  What are the risks/rewards of doing this?
Final parts fit
  Historically, many spacers, endshoes did not fit after winding--required curing operation for correct fit
  Use replaceable “curing” endshoes? (Does not apply to spacers) Or, improve winding processes to keep layers compressed?
Can the curing operation be eliminated entirely in QXF coil fabrication with redesigned tooling?

## Slide 10: Coil Processing: Reaction
Gaps
  Pole islands, wedges optimization
  HQ Coils 17 and 21 did not close gaps after reaction
    All other coils used insulation sleeve
    Seems to indicate that directly braided insulation on cables needs more data
  Practice QXF coil(s) should be designed so that gaps remain in the islands after reaction
Mica slip planes
Can two coils be reacted effectively in one oven cycle?
HQ Coil 17
post-reaction pole gap

## Slide 11: Coil Processing: Impregnation
Does CTD 101K epoxy exhibit acceptable radiation hardness?
  What are the requirements?
  What is the real data?
Technical challenges for impregnation using Cyanate Ester blends (or other materials) must be overcome for long coils
Instrumentation traces
  Do laminated polyimide trace materials pose problems for impregnation?
  Trace behavior (bubbles) on inside bore after testing cycle have continued
Bubbles on inside bore of
LQS03 after magnet test
Inside bore of HQ02a during
assembly (Coil 15 was previously
tested in HQ mirror)

## Slide 12: Coil Processing: Instrumentation
Strain gages
  Bonding, protection of SGs
Instrumentation/heater traces
  Are thicker (>25 µm) polyimide layers acceptable for quench protection? (HQ02a results pending)
Wiring
  Most Teflon insulated instrumentation wires (VT & SGs) currently used are rated for 600V; what is acceptable for high voltage performance (~5kV coil hipot testing)?
  Can the packaging of instrumentation wires be optimized in magnet assemblies for axial loading
Connectors
  Plain Hypertronics connectors are not polarized—easy to flip connectors
  Manuf. stated specs say ~1600V – 3000V breakdown voltage (<5kV hipot testing)
Instrumentation wire routing
of LQS03 at Lead End.

## Slide 13: Coil Processing: Inspection & Electrical QA
Determine what QA steps are necessary throughout all process steps to sufficiently document behaviors
Mechanical inspections
  CMM
    All Labs to use same reference models
    Develop database of pre- and post-compression measurement data for coils
  Coil Autopsies (for practice coils and other)
    Develop a clear definition of what features, interfaces, profiles need to be inspected and how this feeds back into real coil production
Electrical QA
  Is it beneficial to use the same hardware systems and software for QA steps (impulse, hipot, Sequential R tests) at different Labs?

## Slide 14: Open Issues Summary
The QXF coil task has standing issues and/or technical decisions that need to be made through all stages of design and fabrication
  Some experimental data exists, but we need more data points to make technically sound decisions
We may be able to leverage pre-existing tasks efficiently in order to solve many of these issues
  HQ, LHQ, and Base Programs (GARD) may already be positioned to answer some of these

## Slide 15: QXF Coils: Begin with the end in mind…
Primary outcome of LARP (and QXF Coil Fabrication) should be Documentation
  Of Designs
  Of Processes
  Of Performance and Behaviors
  …independent of infrastructure and/or Laboratories
Our experience with QXF coil fabrication as a “pre-prototype” must provide a solid foundation for the prototype and the production IR quads that follow
  Develop processes and procedures now to begin addressing increased uniformity, throughput, and yield in coil fabrication
Family Tree of LARP model magnets
QXF
IR Quad Prototype
IR Quad Production

## Slide 16: Appendix

## Slide 17: The LARP QXF Coil Task: External Inputs