## Slide 1: Generating very high magnetic field using a round-wire HTS conductor & Quench protection of HTS magnets
Tengming Shen
Fermi National Accelerator Lab
Presented at Muon Collider 2011, Telluride, CO
June 29, 2011
I want to thank collaboration with BNL, NCSU, NHMFL/FSU, NIST, LANL, LBNL, TAMU, and Oxford Superconducting through Very High Field Superconducting Magnet Collaboration, and funding support from DOE and Fermilab/MAP through the Peoples Fellowship.

## Slide 2: Muon collider designs demand 30-50 T solenoids
A transformational opportunity for high-field science
  But it is also a quantum leap in technology.
Challenges to 30+ T HTS magnets:
  Engineering the conductor to carry >200 A/mm2 in 20-50 T
  Managing stress >200 MPa
  Protecting magnet from quenches
  We recently significantly improved the Je of a round-wire HTS conductor to 600 A/mm2 at 4.2 K, 20 T.
  Quench is an old problem but needs new solution in HTS magnets
  Finding a novel quench detection method is the key.
NMR communities need 30 T all superconducting magnets.

## Slide 3
(Courtesy of J. Jiang, FSU)
A transformational opportunity to go to fields beyond NbTi and Nb3Sn
  NbTi~10 T
  Nb3Sn~22 T
But imposes new restrictions because HTS materials are so much more complex.
  Complex material processing
  Stress tolerance
  Quench detection and protection
Ongoing high field magnet projects
  32 T all superconducting, NHMFL, NSF
  30.5 T NMR, all superconducting, MIT, NIH
  20+20 T, PBL/BNL, DOE-SBIR
  VHFSMC, DOE
Resistive magnets take 30 MW to reach 45 T;
LTS conductors mature, reaching their limits at ~20 T.
HTS conductors have the ability to approach the grand challenge of 50 T

## Slide 4: VHFSMC aims to bring HTS-high field magnet technology forward
Address all important aspects of the technology, from conductor,
cabling, protection, to demonstration coils.
Very High Field Superconducting Magnet Collaboration (VHFSMC):
Now focus on 2212 technology.
PI: David Larbalestier and Alvin Tollestup

## Slide 5
2212 coils reach 32 T
OST
Bmax = 22.5 T
ΔB = 2.5 T
NHMFL
Bmax = 32 T
ΔB = 1.1 T
Wind and react magnet fabrication is
feasible.
VHFSMC focuses on magnet tech based on
a round-wire HTS conductor
Ag-sheathed multifilamentary
Bi2Sr2CaCu2Ox (2212)
A round-wire conductor is preferred for
magnet and HEP applications.
Allow Rutherford cable and 20+ T dipoles

## Slide 6: We have met and solved many problems
Early conductor bleaks at high temperatures.
  Solved by industry at processing level.
Conductor has very sensitive high-temperature reaction.
  New understanding gave heat treatment control protocols.
Je of long-length conductor varies from batch to batch, ranging from 137 A/mm2 to 480 A/mm2 at 4.2 K, 20 T.
  Understood at microscopic levels.
  We increased Je to 600 A/mm2 using an industry-scalable approach
Developing mechanically robust conductor
  Managing stresses in coils using cable-based magnet.
Exploring approaches to quench protection
T. Shen et al., Muon Winter Meeting, Virginia, 2011

## Slide 7: Why is quench protection of HTS magnets difficult?
Quench is an event of losing superconductivity locally and spreading the normal zone.
  Leading to fast temperature rise
  Requires nearly-instantaneous protection
Quench is an old problem
  Though challenging, it has been tackled well in LTS magnets.
Why is protecting HTS magnets difficult?
  Because quench detection is difficult.

## Slide 8: Quench is induced by local energy disturbances, amplified by joule heating, and propagated by heat transfer
B
Jc
T
Tc
A
B
C
A to B: Q  T
B to C: Current flows into stabilizer, creating joule heating.
Temperature continues to rise.
C: Superconductor is not superconducting anymore. All
current flows into stabilizer.
I
Normal zone
Stabilizer
Superconductor
Case C:
Q > Minimum quench energy
(MQE)

## Slide 9: Unprotected quenches can damage superconducting magnets
A YBCO-short sample case:
  It=160 A (70% Ic), 37 K
  Conduction-cooled, nearly-
  adiabatic situation
  Tpeak=450 K in 2 sec
  50% Ic degradation
Mbaruku et al., IEEE Trans. Appl. Supercond. 17 3044, (2007)
A meltdown in LHC main bending magnet
due to a quench
Consequences of quenches:
  Temperature rising to >200 K
- within seconds.
  Inducing high internal voltage
  Inducing thermal strains
- Nb3Sn and HTS are strain sensitive.
J. Schwerg, PhD thesis, 2010

## Slide 10: Conductor temperature rises fast after unprotected quench
Temperature rise can be estimated by assuming that joule heating is absorbed by conductor,
ignoring the conduction and cooling effects:
Depending only on
Material properties
Quench is essentially a heat transfer problem:
Heat absorption by coil
Heat conduction into hot spot
Joule heating
Initial energy disturbance
Jm is stabilizer current density, ρ is resistivity of stabilizer.

## Slide 11: Allowed protection time is only several seconds
Cases | Je | Jm | Minimal quench energy at 4.2 K | tp (assume Tm<200K)
 | A/mm2 | A/mm2 | J | Sec
NbTi round wire | 200 | 357 | 0.005 | 1.8
2212 round wire | 200 | 266 | ~1 | 2.4
YBCO coated conductor* | 200 | 625 | ~1 | 0.54
The rate of hot spot temperature rise is proportional to Jm2.
tp is inversely proportional to Jm2; it sets a limit for detecting quench and shutting magnet current off.
YBCO needs more Cu but adding Cu lowers Jave.
* 40 mm Cu.

## Slide 12: Quench protection relies on detecting quench and turning current off fast
And to take energy out of cold mass.
Quench detected
Protection measures
taking effects
Current decay characteristic time:
L
R
Passive protection:
Energy stays in cold mass
Relies on fast normal zone propagation.
Cold mass
Heater
L
R
Active protection
Take energy out of magnet
May induce high voltage
Cold mass
Quench initiated

## Slide 13: Example: parameters of quench protection systems for NMR magnets
900 MHz NMR (21 T) magnet at NHMFL, with stored energy of 38 MJ
  1.5 m tall, 0.144 m ID, and 0.878 m OD
  With eight LTS-coils stacked concentrically, and two more shimming coils
  Jm in NbTi-Cu is 274 A/mm2, giving a tp of 3.1 sec
  0.2 sec for detecting quench
  0.2 sec for activating quench protection
  ~2 sec for discharging
I.R. Dixon et al., IEEE Transcations on Applied Superconductivity, 14, (2004), 1260

## Slide 14: Successful quench protection relies on detecting quench fast, in <0.2 s
How robust is conductor against quenches?
  LTS
  2212: Ag-sheathed round wire, slightly Ic-degradation when T>800 K
  YBCO: Cu-laminated YBCO, slightly Ic-degradation when T>370 K
Assume quench is detected, can we protect the coil?
  Yes for LTS.
  Yes for Bi-2212
  Yes for YBCO if tp>2 sec.
Can we detect a quench event locally, in <0.2 sec, before the hot spot temperature rises to a dangerous level?
  Easy for LTS
  Difficult for Bi-2212
  Very difficult for YBCO
Y. Iwasa, Case studies in superconducting magnets, 2nd edition.
Quench-induced degradation experiments (Iwasa, Lue, Ishiyama, Wang, Effio, Ye, Song, Schwartz, …)

## Slide 15: How to detect quench events in LTS coils?
The circuit of a
superconducting magnet
Maximum detection voltage:
Vmax =VQ(t)=I(t) x RQ(t) x (1-M/L)
< I(t) x RQ(t)
= Jm x ρ x U x t
Quench detection relies on quick voltage development across normal zone
U is normal zone propagation velocity.
Jm is stabilizer current density, ρ is resistivity of stabilizer.
L is self-inductance of the whole magnet, M is mutual-inductance between
normal zone and the rest of magnet.
Iop
I(t)
Superconducting coil
Quench
I(t)
Quench zone
VQ(t)
RQ(t)
Iop

## Slide 16: Normal zone voltage in HTS conductor develops slowly, due to very low NZP velocity
Superconductor | Ul [mm/s]
NbTi | ~1000
Nb3Sn | ~500
Bi-2223 | ~3-10
YBCO | ~3-10
Bi-2212 | ~3-10
Longitudinal NZP velocities UHTS<<ULTS.
For Vmax to reach a detection limit (e.g. 0.1 V),
NbTi will need <10 ms, during which hot-spot temperature rises <30 K.
HTS will need >1 s, during which hot-spot temperature rises to >100 K.
To detect a quench zone in mm-order of length, it will require to put voltage taps
throughout the coil, which is not very practical…
NZP velocities:
This makes voltage-based quench detection difficult, if it is not impossible, for HTS
Y. Iwasa, Case studies in superconducting magnets, 2nd edition.

## Slide 17
Chart: Time (sec)
| 0.9 | 1.1000000000000001 | 1.3 | 1.5 | 1.84 | 2.2999999999999998 | 2.44
Estimated Tmax,RW,I/Ic=0.8,B=25T | 50 | 100 | 150 | 200 | 300
Effio-Tmax, 19-filament tape, I/Ic=0.78, s.f. | 95 | 125 | 155 | 195
Estimated Vmax,RW,I/Ic=0.8,B=25 | 0.49 | 0.81 | 0.99 | 1.24 | 1.32
Effio-Vmax, 19-filament tape, I/Ic=0.78, s.f. | 0.05 | 0.08 | 0.13 | 0.2
Quench detection in HTS is very difficult: slow voltage growth vs. fast temperature rise
T
Bi-2212
T. Effio, Superconductor Science and
Technology, 2008

## Slide 18: Many methods have been evaluated
Voltage-based detection (BNL)
  To detect quench in less than 5 msec
  Low voltage threshold of 1mV
Non-voltage-based detection techniques:
  Acoustic emission (Y. Iwasa, MIT)
  Fiber-optics (NCSU-Muon Inc.)
Techniques to promote the normal zone propagation transverse to conductor:
  Thin ceramic insulation coating with high thermal conductivity (NCSU-nGimat)
  No turn-to-turn insulation winding (Y. Iwasa, MIT)
  Stainless-steel as turn-to-turn insulation (BNL-PBL)
But the problem is a hard one

## Slide 19: Additional resources
Superconducting Magnets by Martin Wilson
Case Studies in Superconducting Magnets by Yuki Iwasa
Mini-workshop on quench protection of HTS magnets, High Field-Low Temperature Superconductor Workshop, Monterey, CA (2010)

## Slide 20: Summary
  LTS conductors approach their limits. Bringing HTS to applications will be revolutionary.
    30 T NMR (all SC)
    60 T hybrid (R+SC)
    50 T muon cooling magnets
We increased Je of 2212 to 600 A/mm2 at 4.2 K, 20 T.
  Given this increase in Je, paths to 30+ T all superconducting magnets based on 2212 open up.
To reliably operate 30+ T HTS magnets, we need
    Novel quench detection strategies