## Slide 1: R&D Towards 40 T at BNL
Presented by Ramesh Gupta for
M. Anerella, G. Ganetis, P. Joshi, H. Kirk, L. Lalitha, R. Palmer, J. Schmalzle, W. Sampson, Y. Shiroyanagi, P. Wanderer
Brookhaven National Laboratory
and
D. Cline, J. Kolonko, R. Scanlan, R. Weggel
Particle Beam Lasers, Inc.

## Slide 2: High Field Solenoid Projects at BNL
~35 T HTS/Nb3Sn s.c. solenoid for Muon Collider (PBL/BNL SBIRs)
        34 HTS coils already built and tested using over 3 km of conductor
~40T (~20+T HTS) insert coil PBL/BNL SBIR (~20+T comes from HTS)
    23 T already demonstrated in the background field of NHMFL
~25 T large aperture HTS solenoid for SMES (ARPA-E funded)
    R&D would directly benefit high field solenoids for SMES
A very brief summary of selected HTS R&D on related topics (e.g. quench protection, stress limit, radiation damage) and other HTS programs at BNL

## Slide 3: PBL/BNL SBIR for Muon Collider
SBIRs from Particle Beam Lasers (PBL) with BNL as partner:
~10 T HTS solenoid (middle): Phase II funded
~12 T HTS (inner): Phase II funded
12-15 T Nb3Sn (outer): Phase I funded, Phase II will be applied
1
2
3
20+ T All HTS Solenoid (1 & 2):
  addresses challenges with high field HTS solenoids
35+ T All Superconducting Solenoid (1, 2 and 3):
  addresses challenges with high field superconducting solenoids

## Slide 4: Status of BNL/PBL SBIR #1 (10 T HTS Outsert)
29 coils for 100 mm aperture solenoid have been wound with stainless steel insulation
Each coil is made with 100 meters (total: ~2.9 km) of second generation (2G) HTS
All coils have been individually tested at 77 K ; 24 good coils selected
We should have the test result of the completed ~10 T solenoid in about four months

## Slide 5
Coil i.d. ~25 mm; o.d. ~95 mm (can go inside 100 mm solenoid)
Inner solenoid needs 12 pancake coils
5 coils built and tested (3 with Kapton and 2 with ss insulation)
Each coil is made with 50 meters of 2G HTS
All coils tested at 77 K and four at 4 K
Status of BNL/PBL SBIR #2 (10+ T HTS insert)

## Slide 6: HTS PBL/BNL Insert Coil Test in the Background Field of NHMFL
Four HTS coils built for inner solenoid were used for insert coil test at NHMFL
4 T @4K self field, and 23 T in 20 T background field
First demonstration of technology for 20-22 T HTS solenoid, as targeted in SBIR.
Self-field
In 20 T applied field
23 T

## Slide 7: High Field HTS Solenoid for SMES (Partners: BNL, SuperPower & ABB)
  Field: ~25 T
  Inner Diameter : ~100 mm
  Conductor: ~10 km, 12 mm wide 2G tape
  Stored Energy: 2.5 MJ
R&D has just started on this high field, large aperture HTS solenoid for SMES
There is going to be a significant R&D effort on conductor and magnet technology – funded by ARPA-E but very relevant to MAP
If demonstrated, then 50 T can be targeted with HTS insert and LTS outsert – relatively less challenging (funding must come from elsewhere)
Quench protection of a large magnetic energy storage device is a major issue

## Slide 8: HTS Technology Development Program at BNL

## Slide 9: HTS Quench Protection R&D at BNL (development of hardware and understanding)
Quench protection in HTS poses a major challenge. BNL has a comprehensive R&D program with funding from several sources – FRIB, SMES, PBL/BNL SBIR, base program and possible LDRD (all small but they add up)

## Slide 10: Influence of ~107 MPa Pressure on the Narrow Face of Conductor in 2G HTS Coil
Load ON, Load OFF:
Measure change in Ic every ~1 m over ~6 m
A negligible change in Ic means that at least 100 MPa load is acceptable
~0.5% reversible change in Ic
HTS Coils

## Slide 11
Radiation Damage Studies for FRIB
2G HTS from SuperPower and ASC
SuperPower
ASC
Next step: In field measurements at 40-50 K. MAP could be interested at 4 K
ASC2008 – self field 77 K
PAC2011- in field 77 K

## Slide 12: Wide Range of HTS Magnet R&D at BNL
The level of involvement in this field may be gauged by the amount of HTS wire/tape coming in. Net total in all programs (normalized to 4 mm tape):
  Obtained so far: ~20 km
  Next two years (based on funded programs): ~35 km
Successfully designed, built & tested a large number of coils & magnets:
  Number of HTS coils built: ~100
  Number of HTS magnet structures built and tested: ~10
HTS Magnet R&D for a wide range of operating conditions:
  High field (>20 T), low temperature: two funded programs
  Medium field, medium temperature: three funded programs
  Low field, High temperature: several in house, built and tested
HTS Magnet R&D at BNL is about an order of magnitude more than in other labs

## Slide 13
http://www.bnl.gov/magnets/staff/gupta/

## Slide 14: PAC 2011 Papers on HTS from BNL
A wide range of HTS R&D @ BNL presented at PAC2011:
Engineering Design of HTS Quadrupole for FRIB – Cozzolino, et al.
Design, Const. and test of Cryogen-free HTS Coil Structure – Hocker, et al.
Influence of Proton Irradiation on Second Generation HTS in Presence of Magnetic Field – Shiroyanagi, et al.
Novel Quench detection system for HTS Coils – Joshi, et al.
Measurements of the Effect of Axial Stress on YBCO Coils – Sampson, et al.
Open Midplane Dipole for Muon Collider – Weggel, et al.
Design Construction and Test Results of HTS Solenoid for ERL – Gupta, et al.
HTS Magnets for Accelerator and Other Applications – Gupta
A significant number of papers and presentations:
http://www.bnl.gov/magnets/staff/gupta/Talks/hts-talks.htm
    htp://www.bnl.gov/magnets/staff/gupta/Publications/htS-papers.htm

## Slide 15: SUMMARY (1) PBL/BNL Related
High field HTS solenoids are very challenging with a number of technologies yet to be demonstrated. However, over the years we have made some progress.
We have built and tested a large number of HTS coils (34) for PBL/BNL SBIR.
We have demonstrated these coil will survive 23 T (NHMFL has demonstrated HTS coils to ~35 T).
We hope to demonstrate a ~100 mm, 10 T HTS solenoid in a few months.
We hope to demonstrate 10-12 T, ~25 mm insert HTS solenoid in ~6 month.
We hope to demonstrate ~20-22 T HTS solenoid by combining two in ~10 month.
We hope to test above in ~20 T resistive solenoid at NHMFL to test HTS magnet technology to field approaching 40 T in about a year or so.
There is also a Phase I SBIR for ~15 T Nb3Sn outsert. If that results into Phase II funding, then we plan to demonstrate ~35+ T all superconducting solenoid.
If successful, then we would have solved a major technical issue of MAP.

## Slide 16: SUMMARY (2)
We are also building a large aperture ~25 T HTS solenoid for SMES. This is funded by ARPA-E as a high risk, high reward project. Technology developed in this program should directly benefit MAP.
In addition BNL is pursuing a wide ranging R&D which provides a good synergy and brings overall progress in HTS magnet technology.
Most of above projects are being carried out on a shoestring budget with no direct support from MAP. MAP could perhaps benefit more with a direct involvement and/or participation of BNL magnet division in various technical and strategic planning of magnet R&D. Surprisingly it is not currently despite its unique expertise with HTS technology.
We all benefit from sharing our experiences in developing new technology when the funding is limited. We have already established a good collaboration with NHMFL – they have unique experience with high field solenoids and we have with HTS. We invite other groups to join us to work on specific topics.